## Slide 1: Imaging x-ray generation and Scattering
Tabletop soft x-ray coherent imaging microscopes

## Slide 2
Regenerative amplifier
3mJ, 35fs, 1kHz
Amplifier pump
Diode pump
Ti:sapphire seed laser
Vacuum chamber
Gas cell
CCD camera
Sample
XUV multilayer mirror
Al foil filter
Pump beam
High Harmonic Generation for ultrafast soft x-rays

## Slide 3
Diffraction from self assembled 200 nm PMMA spheres showing domain structures
Allowing the complex refractive index to be determined to high precision
SEM
X-Ray diffraction image
Mie Scattering comparison
The sate of play at our last COST talk

## Slide 4
Microscopy in XUV is hard because of lack of optics
  Possible using zone plates, or multilayer mirror objectives
Imaging without a lens
Phase retrieval algorithms can be used to replace the objective lens
CCD detector
X-Ray Microscopy

## Slide 5
Take FFT
Reverse FFT
replace intensity with known pattern (Fourier space constraint)
is the outer region black? – make it black (real space constraint)
Guess object from autocorrelation & random phase
Log10 of scattered intensity from pinhole/mask object
Fourier space
Real space
Computational phase retrieval
Make use of constraints

## Slide 6
Several versions of the algorithm, run with range of staring phases, typically for 100’s of cycles

## Slide 7
Test sample Au on SiN made using ORC FIB
200 nm

## Slide 8
Coherent Scattering/Diffraction Image showing features out to better than 100 nm resolution. New camera position now able to achieve 50 nm resolution
Double line is 100 nm resolution

## Slide 9
Reconstructed intensity image

## Slide 10
Phase of the reconstructed image
The sample is either transmitting or blocking but the x-ray pulse may have a non-uniform phase front.

## Slide 11
Image of a diatom fragment
Taken without using a focussing mirror, some issues of laser scatter to be resolved

## Slide 12
By comparing diffraction images taken at slightly different positions and at different proportions of the harmonics then we can begin to separate the diffraction from the 2D crystal lattice from the scattering image of the defects.
We are looking at how to reconstruct the defect image
Back to the spheres……

## Slide 13: Issues
Flux
Multiple wavelengths
Sample size
Optimize using x-ray and visible diagnostics and via a model of the HHG process

## Slide 14
Capillary
Optimizing Ar pressure and laser power to give a dominant single harmonic peak

## Slide 15
JET
Diagnostics – X-Ray Generation

## Slide 16
Cell

## Slide 17
Diagnostics – X-Rays
Advanced diagnostics - Spatio-spectral beam imaging using Fresnel diffraction

## Slide 18
Generating X-rays using nonlinear optics
High harmonic generation – X-rays using very nonlinear optics
Now close to a full model of the process for capillary, jet and cell HHG

## Slide 19: The Future
4 nm Water Window source for table top 2D and 3D cellular imaging
Spectroscopic Imaging
Time resolved spectroscopy
1 A coherent source?

## Slide 20
The Group
(…….well some of them)
The start
2010
EPSRC
RCUK

## Slide 21
Next COST Meeting 18-19 Nov 2010
University of Southampton
ORC Buildings
Southampton Airport, Good connections to London and Heathrow via train & Coach