The PTCR Effect in Donor-doped Barium Titanate: Review of Compositions, Microstructures, Processing and Properties

Yulong Chena  and Shoufeng Yangb*

aSchool of Engineering and Materials Science, Queen Mary, University of London, Mile End Road, London, E1 4NS, U.K.

bSchool of Engineering Sciences, University of Southampton, Southampton, SO17 1BJ, UK

Abstract: Barium titanate is widely used in the fabrication of thermistors with a positive temperature coefficient of resistivity (PTCR). The resistivity can increase by several orders of magnitude near the phase transition temperature (Tc) for the ferroelectric tetragonal to the paraelectric cubic phase transformation. There is general agreement that the anomaly in the change of electrical resistivity of donor-doped BaTiO3 around Tc is due to the grain boundary effect. The Heywang-Jonker model and other mechanisms involving the nature of the electrical barrier formed across the grain boundaries of polycrystalline BaTiO3 are reviewed. The compositional effect on BaTiO3-based PTCR properties is listed and discussed. The influences of manufacturing methods under different stages including the initial doping methods, sample forming methods and final heat treatments on PTCR properties are compared. The complex interrelationship between compositions, microstructures, processing and PTCR characteristics are well discussed.

Keywords: positive temperature coefficient of resistivity (PTCR), barium titanate, composition, microstructure

- Introduction

Positive temperature coefficient of resistivity (PTCR) materials are widely used in the electronics industry for, inter alia, applications including temperature sensors, time delay circuits and current limiters for overvoltage or overcurrent protection, overheat protection, current stabilizers. There are four main materials groups in the PTCR family: BaTiO3-based or quasi-BaTiO3-based ternary perovskite compounds,1-9 ceramic composites,10, 11 polymer composites,12, 13 and V2O3-based compounds.14, 15

BaTiO3 is an insulator at room temperature but donor-doped BaTiO3 with ions such as La3+, Y3+, Sb3+, Nb5+ presents semi-conducting behaviour at room temperature and an anomalous increase in resistivity near the ferroelectric-paraelectric Curie transition temperature Tc.16 This PTCR effect (shown schematically in Figure 1) in barium titanate was first developed in the early 1950s in the Philips Research Laboratories in the Netherlands.17 Over the past 50 years, diverse applications have triggered research efforts directed toward understanding compositional and structural issues that govern the electrical properties. The screening of dopant candidates from the periodic table has been well scrutinized18-20 and several models to explain the temperature-resistivity relation have been derived.21-25

In the past five decades, there have been few reviews on the PTCR effect in doped barium titanate. Saburi21 first reviewed semiconducting properties and their relations to the composition of BaTiO3 doped by a variety of donor dopants. He26 also described and surveyed the processing techniques, fundamental characteristics and applications of PTCR BaTiO3 ceramics. In a review by Daniels et al.27 the nature of the PTCR effect of donor-doped barium titanate as determined by the conditions of the lattice defects including the oxygen vacancies or/and cation vacancies was described. The thermodynamic and kinetic aspects were discussed. In Nowotny’s review,7 models that have been developed to explain the PTCR phenomenon were compared and discussed. He also listed some materials and processing procedures that could affect PTCR characteristics. In Huybrechts’ review,6 the resistivity-temperature behaviour of PTCR materials by the Heywang-Jonker model was explained. The type and origin of trapped electrons at the grain boundary which cause the PTCR effect were analyzed and the influences on the PTCR effect of changing the processing parameters were presented. Besides those reviews, articles introducing the PTCR effect in BaTiO3 can also be found in several books.16, 28 However, what is elusive is an explanation of the interrelationships between compositions, microstructures, processing and PTCR properties of donor-doped BaTiO3 materials and a systematic description of all the factors that can influence the PTCR effect. Moreover, there has been tremendous progress in investigating the PTCR effect in barium titanate materials in the last 15 years without a proper review article; a new review in this field is therefore appropriate.

This paper is an attempt to provide a more complete understanding of the interrelationship of compositions, microstructures, processing and PTCR properties. In section II, several mechanisms, including the well-acknowledged Heywang-Jonker model and others which interpret the PTCR effect in donor-doped BaTiO3 are summarized, noting that there is still controversy in terms of the origin of the semiconductivity at room temperature. In the following three sections, the influence on the PTCR effect by altering the composition (Section III), the processing (IV) and the microstructure (V) are discussed in turn. In the final section, the emerging trends of research of advanced donor-doped BaTiO3 PTCR materials are briefly addressed.

- Theory

There is a general agreement that the anomaly in the change of electrical resistivity of donor-doped BaTiO3 around Tc is due to the grain boundary effect. No PTCR effect has been observed in BaTiO3 single crystal.29 Furthermore, it is clear from impedance-plane analysis that the semiconducting characteristics of bulk grains is independent of either temperature or donor concentration.30-32

      - The Heywang-Jonker Model

The most accepted model to explain the PTCR behaviour in donor-doped BaTiO3 materials is the Heywang-Jonker model proposed by Heywang22 and extended by Jonker.24 Since this model is a fundamental guideline for the understanding of PTCR effect in BaTiO3-based materials, it is necessary to be reviewed again here. There is a bi-dimensional layer of electron traps, i.e. acceptor states, along the grain boundaries of BaTiO3 (shown in Figure 2) exhibiting different electrical properties from those of the bulk phase. The potential barrier  is caused by a two-dimensional electron trap along the grain boundary where acceptor states attract electrons from the bulk resulting in an electron depletion layer with thickness of b. The relation between the density of trapped electrons at the grain boundaries and the thickness of the depletion layer can be expressed as:

... ... ... 1

where Ns is the concentration of trapped electrons and Nd is the charge carrier concentration. This depletion layer results in a grain boundary barrier,

... ... ... 2

where e is the electron charge, ε0 the permittivity of free space and εgb the relative permittivity of the grain boundary region.

The overall resistivity, ρ, is related to the height of the potential barrier by

... ... ... 3

where A is a geometrical factor and k the Boltzmann constant. Because BaTiO3 is ferroelectric, the dielectric constant, ε, obeys the Curie-Weiss law above its Curie temperature and is given by

... ... ... 4

where C is the Curie constant and T the absolute temperature. Incorporating equation (2) and (4) into (3) and rearranging yields:

... ... ... 5

Above the Curie point when doped BaTiO3 is in the paraelectric phase, the grain-boundary permittivity which follows the Curie-Weiss law decreases with increasing temperature. The corresponding potential barrier increases proportionally and results in steeply increasing resistivity which depends exponentially on the potential barrier as denoted by equation 3. The energy of the trapped electrons in the grain boundary rises with temperature together with the potential barrier. When the energy of the electron traps reaches the Fermi level, trapped electrons start to jump to the conduction band, which can depress the increase in  and ρ, thus ultimately enhance the conductivity. This also explains the negative temperature coefficient resistivity (NTCR) effect when passing the point ρmax (Figure 1) in the high temperature range.

However, Heywang’s model was not able accurately to explain the PTCR behaviour below Tc. Hence Jonker’s model24 was developed as a refinement. Below the Curie point, BaTiO3 is ferroelectric with its polarization along the tetragonal crystal axis. The polarization direction is different from grain to grain because each adjacent grain has a different crystal orientation. Therefore, it creates a net polarization vector (PN) normal to the grain boundaries, producing surface charges at the grain boundaries which are illustrated in Figure 3. In the areas with negative surface charges, which are around 50% of the grain-boundary area depending on the nature of the ferroelectric material, potential barrier height diminishes or even disappears resulting in the disappearance of the grain boundary resistance. For the other half of the domains containing positive charges, the potential barrier is, of course, getting higher. However, this does not matter as the conducting electrons always follow the path with the lowest barriers so that the material as a whole has low resistivity. This theory is experimentally supported by Huybrechts’ work.33 Furthermore, according to the Heywang-Jonker’s model, the electrical resistivity profile ρ(T) above the ferroelectric Curie point of donor-doped barium titanate ceramics can be modelled and was verified successfully using experimentally determined permittivity data reported by Brzozowski8 and Zubair34.

            - Other Theories

In donor-doped BaTiO3 PTCR ceramics, Heywang-Jonker’s model has effectively elucidated the change of resistivity with temperature in PTCR characteristics. Based on this model, the PTCR effect increases with increase of potential barrier by which is affected the trapping of electrons (from ionized donors) by acceptor-type species such as some 3-d elements,35 chemisorbed gases36-38 or cation vacancies39, 40 at the grain boundary. Those barriers make the grain boundary more resistive than the bulk grain. However, the model does not fully explain the mechanisms by which electrical properties are influenced adding different amounts or kinds of donor dopants or changing the processing parameters.

It is believed that, for donor-doped BaTiO3, the initial drop in resistivity with increasing donor concentration is generally attributed to an electronic compensation mechanism that induces n-type semiconductor characteristics.39 Choosing a trivalent ion (R3+) as a donor dopant, free electrons in the BaTiO3 lattice can be generated according to equations (written in Kröger-Vink notation):

... ... ... 6

and/or

………7

Based on equation 6, the free electrons are generated by oxygen deficiency as occurs when sintering at high temperature and/or in reducing atmospheres.36 Based on equation 7, the electrons are associated with the replacement of barium ion by R trivalent ion. However, if there is a shift to an ionic compensation mechanism (cation vacancy compensation) at high donor contents, this would result in increasing resistivity at room temperature due to the immobility of cation vacancies. It was first suggested by Jonker and Havinga40 and the corresponding equation is:

………8

and/or

………9

According to equations 8 and 9, barium vacancies and/or titanium vacancies can be produced at the grain boundaries and diffuse from the grain boundaries into the grains during sintering. Because the diffusion speed of cation vacancies is very slow in grains at high temperature, this results in a sample with heterogeneous electric profiles in grains as the cation vacancies act as electron traps and there is an increase in the potential barrier at the grain boundaries. Chan et at.41 inferred that titanium vacancies were favoured defects compared with barium vacancies in the ionic compensation scheme according to a microstructural investigation of highly donor-doped BaTiO3 by TEM. The preference for titanium vacancies is also supported by atomistic simulations which show lower energy of formation than that of barium vacancies.42

Smyth43 believed that equations 7 and 8 can be connected by an exchange reaction:

………10

where the donor centres are charged-compensated by electrons if the extra oxygen is expelled. Clearly, electron compensation is preferred in reducing conditions during sintering resulting from the tendency for oxygen loss, while ionic compensation by generated Ti vacancies is favoured by an oxidation environment. This theory explains well the observation that for light donor-doped BaTiO3 material processed in air by slow cooling or annealing at a lower temperature may be superficially or completely oxidized to an insulating state but have low resistance at room temperature if cooled rapidly from the sintering temperature because of the ‘frozen-in’ composition, avoiding reoxidation that occurs at lower temperature. For higher donor concentrations, materials can become electrical semi-conducting only if sufficiently reduced. The quantitative analysis44 of the oxygen exchange of donor-doped BaTiO3 both under equilibrium and non-equilibrium conditions by the oxygen coulometry method45 has directly proved that the carrier concentration is equal to the net donor content which is in agreement with the conclusion that the equilibrium conductivity is dependent on the electronic compensation that is proportional to the donor concentration. Furthermore, evidences for precipitation of secondary phases in donor-doped BaTiO3 when alternated between the oxidizing and reducing environments during firing support the validity of charge compensation mechanism.46, 47

There are still some controversies in the well-accepted ideas of changing compensation mechanisms affecting the conductivity of donor-doped BaTiO3. According to the charge compensation theory, the donor-doped BaTiO3 should contain an electrically heterogeneous structure regardless of both the composition and subjecting processing parameters because of the cation-stoichiometric difference between the grain core and grain boundary as compared with the electrically homogeneous structure of undoped BaTiO3. However, Morrison et al.48, 49 observed by impedance spectroscopy that there is no semiconducting grain interior in lightly donor-doped BaTiO3 after sintered in O2, which suggested that the material was electrically homogeneous. They also announced that there was no finding of change in cation stoichiometry or precipitation of secondary phase in donor-doped BaTiO3 samples with varied donor concentrations which were sintered in air or argon. Yet it is generally believed that, according to the conventional charge compensation mechanisms, the appearance of a change in cation stoichiometry is required in donor-doped BaTiO3 when a switch from insulating to semiconducting and vice versa occurs. They50 hence proposed an alternative explanation: the oxygen nonstoichiometry, which is dependent on the oxidized/reduced state at the grain boundary is the main reason for the semiconducting behaviour of donor-doped BaTiO3. Furthermore, the production of semiconducting undoped cation-stoichiometric BaTiO3 which exhibits a modest PTCR effect by losing a small amount of oxygen51 supports their view.

In spite of these discrepancies, there is one common theme that the overall origin of the electrical properties of donor-doped BaTiO3 is a grain boundary effect and greatly influenced by the defect structure on the BaTiO3 perovskite crystal lattice.52, 53 The proposed grain and grain boundary structure of donor-doped BaTiO3 is schematically displayed in Figure 4.54 According to the results of measurements of complex-impedance spectra and microstructural analysis by TEM,54, 55 the grain system’s structure is postulated as having three distinct regions (Figure 4(b)) and its equivalent electric circuit model is shown in Figure 4(a). The outer layer is an oxidised, insulating grain boundary region; the intermediate layer is reoxidized, semiconducting outer grain region and the inner layer is an oxygen deficient grain interior, again, a semiconducting inner grain region. This heterogeneous structure in grains system is supported by both the phenomenon of heterogeneous electric structure of donor-doped BaTiO3 and direct imaging from conductive atomic force microscopy technique.56, 57

- Effect of Composition of BaTiO3-based Materials on the PTCR Properties

Pure BaTiO3 sintered in air is an insulating material at room temperature and no PTCR effect can be observed; however, it turns to a semiconductor at room temperature by doping with various donor dopants such as trivalent ions (e.g. La3+, Sb3+, Y3+) which substitute for the Ba2+ site or pentavalent ions (e.g. Sb5+, Nb5+, Ta5+) which substitute for Ti4+ site at relatively low doping level. It can revert back to behaving as an insulator when the donor content exceeds the critical concentration (normally less than 1 mol.%) as illustrated in Figure 5,50 noting that the solubility limits of most of the dopant elements in BaTiO3 perovskite lattices are far higher than this critical concentration.58 Moreover, the resistivity versus temperature characteristic is very sensitive to the composition of dopants especially for some 3-d elements acting as acceptors. For example, very small additions ranging between 0.01-0.04 mol.% of Mn can increase the PTCR jump of donor-doped BaTiO3 as much as nine orders of magnitude in comparison with three to five orders of magnitudes for donor-doped only BaTiO3.59 In addition, the additives which play a crucial role in the fabrication of BaTiO3-based PTC thermistors can be mainly distinguished as two kinds: aliovalent dopants and isovalent dopants.

- Aliovalent Dopants

The effect of the aliovalent dopant on the bulk electrical conductivity is strongly dependent on its substitution site in the BaTiO3 perovskite structure. The type of the incorporated dopant is determined by the difference in valence charge between the dopant and the replaced host ion. Site replacement in the crystal lattice mainly depends on the dopant’s ionic radius.18 Many (3d, 4d and 5d) elements in Table 1 which could act as aliovalent dopants in BaTiO3-based PTC thermistors have been extensively investigated. Among them, the group of rare-earth elements is a rich resource for providing donor dopants.19, 20, 60, 61

Three regimes of element (expressed in Table 1) can be identified in terms of site occupancy in BaTiO3 and are summarized as:

- For small ions, with ionic radii r ≤ 0.09 nm, dopants preferentially occupy the Ti-site.

- For intermediate ions, with ionic radii 0.09 nm < r < 0.099 nm, dopants can substitute for either Ti or Ba site depending on dopant concentration, sintering conditions and Ba/Ti molar ratio.18, 42, 60, 62

- For larger ions, with ionic radii r ≥ 0.099 nm, dopants preferentially occupy the Ba-site.

The Ba/Ti ratio of the starting materials seems to play a crucial role in affecting the incorporation of dopant elements into the BaTiO3 lattice. It was observed by electron paramagnetic resonance spectra that Ce3+ partially occupied the Ti4+ sites when Ba/Ti>1.63 Electrical conductivity measurement has shown that Er-doped BaTiO3 is weakly semi-conducting at room temperature when Ba/Ti =1. It behaves as an acceptor (preferential substitution at Ti4+ sites) when Ba/Ti >1 but as a donor (preferential substitution at Ba2+ sites) when Ba/Ti <1.18 The recent study of Zhi64 on BaTiO3 with heavily doped Y3+  leads to a similar conclusion. Moreover, dopant substitution at the Ti4+ site can also be enhanced by high dopant concentration partly because the solubility at Ti4+ sites is higher than that at Ba2+ sites.58 For transition metals, like Mn, Co, Fe and Ni, it is well established that they preferentially substitute for the Ti4+ sites regardless the Ba/Ti ratio. Sintering atmosphere likewise has an effect on the preference of the incorporation site of some donor elements such as holmium.65  Significant substitution of Ho onto Ba sites as a donor occurred in a reducing atmosphere while Ti replacement as an acceptor was preferred when sintered in air.

It is generally observed that the room-temperature resistivity of donor-doped BaTiO3 rapidly increases beyond the critical donor concentration because donor ions are preferentially segregated at the grain boundaries.31, 66 Desu et al.67, 68 found that at low donor concentration, the donors are compensated electronically, giving a high conductivity. When the donor concentration increases, the donor concentration at the grain boundaries increases even faster due to the segregation until it exceeds a critical level; the compensation mechanism thereafter shifts from electronic compensation to ionic compensation of the donor centre in the grain-boundary region. Hence it creates an insulating layer at the grain boundaries. The total resistivity of the sample can be represented by the grain bulk resistivity and the resistivity from the dopant-segregation-induced insulating region in the grain boundary. The greater the difference in ionic radius between the substitutional dopant and the host ion, the higher is the tendency for such interfacial segregation to occur. Therefore, the difficulty in preparing semiconducting donor-doped BaTiO3 increases with the radius misfit between the donor and the host ion.68 Furthermore, Peng69 and Ting70 found that when acceptors were added into donor over-doped BaTiO3 insulating material, in which the concentration of donor had exceeded the critical level, the specimen was able to recover some of its semiconducting property. This phenomenon might be explained by assuming that those acceptors inhibit donor segregation at grain boundaries.71 Nevertheless, the nature of the acceptor states is still little known.

- Isovalent Dopants

Divalent ions such as Pb2+, Ca2+ and Sr2+ are extensively used as additives to substitute the Ba ions in the BaTiO3 lattice.72-76 The replacement by lead can increase the Tc by 4.3(C per percentage atomic replacement, whilst replacement by strontium reduces the Tc by 3.5(C per percentage atomic replacement (shown in Figure 6). Since the Curie temperature for BaTiO3 is 120-130(C, this offers the potential to prepare thermistors with PTCR regions anywhere between -100(C and 250(C. Calcium is frequently used in moderate amount but does not shift the Tc by much, alternatively influencing the grain size of the product.77 On the other hand, tetravalent ions such as Zr4+, Hf4+ and Sn4+ have been used as substitutes for Ti ions in the BaTiO3 lattice.78-80 All those tetravalent dopants substitutions can significantly reduce Tc and readily make the phase transformation of tetragonal-cubic occur at room temperature. Zirconium added to BaTiO3 results in lowering the dielectric loss and broadening the dielectric peak near Tc.81 Similarly, Hf and Sn exhibit strong ferroelectric-relaxor behaviour at high contents.82

- Effect of Processing on the PTCR Properties

It is well known that impurities and lattice imperfections play an important role in the exhibition of the PTCR effect in doped-BaTiO3 materials.83 Their conductivities are considerably influenced by both the intrinsic defects such as oxygen vacancies as well as cation vacancies and the extrinsic defects produced by adding dopants.69 Furthermore, not only can the equilibrium behaviour of these defects but also the way of defect formation affected by varying sample preparation methods play a crucial role with respect to the semiconducting properties.

  - Effect of Doping Methods

Electrical performance in donor-doped BaTiO3 ceramics is strongly related to the grain structure. Significant differences in microstructure were observed in samples with the same nominal composition prepared by different doping methods even with the same sintering procedures and hereby different PTCR characteristics were exhibited.84 Hydrothermal synthesis or sol-gel methods can be used to produce donor-doped BaTiO3 systems contained nano-size grains, with high crystallinity and well-dispersed dopants. However, very high room-temperature resistivities and poor PTCR jumps were observed in materials prepared by such method compared with the conventional solid state reaction route.85-88  A similar phenomenon was observed for donor-doped BaTiO3 prepared by mixing the dopant salt into BaTiO3 powder via solution coating method;89 in addition, PTCR ceramics prepared by this doping method has lower critical concentration of donor compared with the same compositional system prepared by the solid state route.89

Besides the different doping methods which cause disparities in PTCR behaviour as described above, a variety of unique mixing techniques have been investigated in order to obtain a controllable, microstructurally stable, BaTiO3-based PTCR material. Mukherjee90 made a donor-doped BaTiO3 system by blending Ba-excess BaTiO3 powder with Ti-excess BaTiO3 powder in different ratios, finding that these blended systems had homogeneous grain size distribution but lower PTCR jumps than those from stoichiometric non-blended batches. Furthermore, Park91 used a seeding technique to produce a heavily niobium-doped BaTiO3 PTCR material by adding BaTiO3 seed particles which contained double twins produced via preceding heat treatment. Semiconducting and PTCR characteristics were achieved by this seeding method compared with fine grained and insulating material for Nb-doped BaTiO3 at the same doping level produced by a conventional, unseeded route.

Some dopants which are commonly used in making PTC thermistors have high vapour pressure particularly at high temperature so that the possibility of incorporating these dopant ions into the barium titanate crystal lattice by vapour phase diffusion exists. A variety of dopants such as Sb3+, Mn2+, Cd2+, Bi3+ and Pb2+ have been tested using such methods92-95 and this resulted in more enhancement of the PTCR jump than doping from conventional solid sources. This is partly because, in diffusion doping from a dopant vapour phase, dopant ions can be more effectively distributed at grain boundaries resulting in increasing the potential barrier at grain boundaries and hence increase of resistivity. In addition, diffusion in polycrystalline BaTiO3 depends on not only the vaporisation rate or vapour pressure of dopants, but also other factors including the sample’s porosity, sample’s thickness, the nature of grain boundary and grain size.

- Effect of Fabrication Methods and Heat Treatment

Not only the various doping techniques, but also the fabrication methods for producing donor-doped BaTiO3 can alter its PTCR performance. In thin-film forming, the electrical properties of the films are significantly different from the bulk, regardless of the techniques of preparation. For Y-doped BaTiO3 thin film (≈2 μm in thickness) deposited by RF-magnetron sputtering as a example,96 the film has a significant change of PTCR characteristics including a shift to lower Tc and smaller PTCR jump in comparison with the same composition prepared by a solid-state route. Large fluctuations in doping concentration dependent resistivity were also observed among those films themselves with the same composition. Nb-doped BaTiO3 films prepared by laser molecular beam epitaxy (LMBE) show extremely low resistivity (≈10-4-10 Ωcm);97 films grown by metal-organic chemical vapour deposition (MOCVD) exhibit intermediate resistivity (≈10-1-107 Ωcm);98, 99 similarly, the resistivity is around 102-104 Ωcm for films deposited by pulse laser deposition.100 This phenomenon may be due to the significant change in microstructure and phase content of the deposited thin film compared with its target material. In addition, the evidence that donor element segregates to the surface and the amount of dopant is drastically reduced below the near-surface region of the thin film sample indicates that the ineffective doping is the cause of the contrasted resistivity values for thin film form and bulk sample.101 BaTiO3-based PTCR ceramics fabricated by thick film methods such as tape-casting,102 slip-casting and roll forming103 have similar microstructure and PTCR characteristics compared with those made by conventional die-pressing methods; nevertheless samples produced by these thick film techniques have higher room-temperature resistivity which is partly due to the high porosity caused by the burning of larger amount of organic additives which were added to facilitate the forming processing.

The PTCR effect in donor-doped BaTiO3 is very sensitive to firing conditions.104-106 Pure stoichiometric BaTiO3 which is an electrically insulating material at room temperature after sintering in air can become semiconducting and exhibit a PTCR effect when sintered at 1450°C in nitrogen and subsequently quenched.51 Unlike the segregation of extrinsic defects introduced from foreign dopant elements accommodating in grains and grain boundaries which change the PTCR profiles directly, changing the sintering parameters can change the PTCR characteristics by introducing intrinsic defects such as oxygen vacancies or cation vacancies. Oxygen from the BaTiO3 lattice is gradually lost at high sintering temperature resulted in increasing electrical conductivity; however, the oxygen-deficient material rapidly reoxidizes either on reheating at lower temperatures or on cooling slowly in high oxygen partial pressures. Hence applying reducing atmosphere during sintering can facilitate the conductivity of donor-doped BaTiO3 and enhance the critical donor concentration significantly.107,108

The room-temperature resistivity of donor-doped BaTiO3 increases with sintering temperature and dwell time which is attributed to an increase in the amount of acceptor-states along grain boundaries.109, 110 Kahn111 and Zubair112, 113 found that the resistivity of donor-doped BaTiO3 increases as the rate of cooling is reduced as seen in Figure 7. The authors claimed that this is due to an increase of the activated surface state density in grain boundaries caused by the oxidation during the cooling cycle. However, LaCourse106 observed that when quenched the Y-doped BT from the sintering temperature, the resistivity below Tc was analogous with that of the sample subjected normal cooling rate as 5°C/min in comparison with the significant lower resistivity exhibited from the sample quenched from 200 °C below the sintering temperature. This is due to the immediately solidified liquid phase staying in the grain boundary increases the thickness of insulating grain boundary layer and hence increases the room-temperature resistivity. The heating rate can also have an influence but has a minor impact on the PTCR characteristics.114 Liu115 also observed that an improvement of room-temperature conductivity of lightly donor-doped BaTiO3 can be occurred when a secondary thermal treatment is subjected by reheated the sample to 400~650 °C for 20~40 minutes after firing processing. This is resulted from the relief of internal stress in the crystal lattice through more directional domain alignment thereby reducing the electrical potential barrier. Furthermore, lower room-temperature resistivity of Nb-doped BaTiO3 is obtained by employing a microwave heating technique comparing with conventional sintering in an electric furnace.116 The mechanism of improvement of PTCR characteristics caused by microwave sintering is still under active investigation.

- Microstructure-PTCR Property Relationships in Donor-doped BaTiO3

The PTCR behaviour of donor-doped polycrystalline BaTiO3 ceramics is known to be dependent on microstructural aspects such as grain size, domain orientation, phase profile and porosity. It has been generally observed that the room-temperature resistivities (ρRT) are low for donor-doped BaTiO3 having large grains and the ρRT of a doped-BaTiO3 sample with fine grains is large (>105 Ω·cm).117 Furthermore, a donor-doped BaTiO3 sample sintered in a non-reducing environment with very fine grains (less than 1 μm) becomes an insulating material and exhibits no PTCR characteristics. The hypotheses that account for large grains in donor-doped BaTiO3 facilitating electric conductivity below Tc are:

  - As grain boundaries act as insulating layers compared with the internal region of grains, a system with large grains has a lower volume fraction of grain boundaries;118 this suggests that large grain systems contain relatively lower portions of insulating component on the conducting path in the presence of an applied electric field.

  - Based on Daniels’ model,27 the thickness of cation vacancy-rich insulating layers in as-sintered donor-doped BaTiO3 grains can be up to 3 μm. For BaTiO3 samples with fine grains, such cation-vacancy layers which act as acceptor-state dominate the electric structures in grains, resulting in overall insulating profile.

  - The high room-temperature resistivity of donor-doped BaTiO3 with small grains can be also accounted for by the strain effect at grain boundaries. The strain which is caused by interfacial segregation of dopants and formation of cation vacancies at grain boundaries increases the potential barrier and hence increases the resistivity.67 This strain effect becomes more significant for small grain systems and alters its electric properties significantly.

  - The mechanism that causes the electrical insulating behaviour of donor-doped BaTiO3 with nano-sized grains is more complex. There may be a shift of tetragonal-cubic phase transition temperature due to the size effect. Begg et al.119 reported that when the size of BaTiO3 particles is below about 190 nm, the cubic rather than the tetragonal phase is thermodynamically preferred at room temperature. Further investigation by Yashima et al.120 confirmed that the Tc of nano-grained BaTiO3 is suppressed with decreasing particle size and a ferroelectric-paraelectric transition occurs below room temperature leading to disappearance of the PTCR effect above room temperature. Park et al.121 also verified that the crystal phase of the nano-grained BaTiO3 ceramics is a mixed state of the tetragonal and cubic phases. This may well explain the insulating phenomenon at room temperature for donor-doped BaTiO3 made by thin-film processing122-124 or some sol-gel methods because the BaTiO3 grains are nano-size.

There is a common observation that the grain size of donor-doped BaTiO3 decreases rapidly with increasing donor concentration after exceeding the critical concentration and leading to a rapid increase of resistivity. Desu et al. believed, based on Auger electron spectroscopy (AES) results, that this phenomenon is due to the impediment of the boundary mobility caused by interfacial segregation of dopants, including donors and acceptors, at the grain boundaries.66, 68 As the average donor concentration increases, the excess local concentration of donor at the grain boundary resulting from interfacial segregation would not only retard grain growth but also shift from electronic to ionic compensation, resulting in the formation of highly resistive layers.

Within the same composition, higher PTCR jump (Rmax/Rmin ratio) is generally achieved in donor-doped BaTiO3 samples with a heterogeneous grain size distribution and having an optimum porosity, in comparison with materials with large dense grain structures. Kuwabara125 found that the magnitude of the PTCR jump reaches a maximum at an optimum sintered density (≈75-85% of theoretical density) and then decreases with increasing density. Those results were partially interpreted that the samples with very dense grain structures, i.e. low porosity, indicating containing higher level of conducting-grain to conducting-grain contacts, thus have poor PTCR resistivity jump at Tc.126 In addition, the enhancement of the PTCR jump by increase of porosity127, 128 from very dense structure may also be due to the assistance for oxygen transport into the ceramic bulk hence facilitating the oxidation of grain boundaries,129 which increases the potential barrier and hence the electrical resistivity. However, it is difficult to specify the optimum combination of the grain size and the porosity of as-sintered donor-doped BT sample in order to satisfy both the need for lowering the room-temperature resistivity and increasing PTCR jump.

The domain structure within grains of a donor-doped BaTiO3 can reveal the level of doping. Roseman126 claimed that an optimal amount of donor can produce unidirectional domain microstructure and domain randomness is only observed in the near grain boundary regions; nevertheless for under-doped and over-doped cases, the domain orientations and widths are random. This phenomenon is suggested to be associated with the Jahn-Teller effect. The spherically asymmetric defect field of optimally donor-doped BaTiO3 can be aligned spontaneously by internal stress generated from Jahn-Teller distortion and this type of defect can, therefore, act as nucleation sites for the ferroelectric phase upon cooling through the Curie point. However, for under-doped samples, the distorted defect field does not dominate the domain nucleation sources; in case of over-doped BaTiO3 samples, the defect compensation mechanism switches to cation vacancy compensation hence the Jahn-Teller distortion no longer exists. As the electron mobility is anisotropic in the tetragonal unit cell in donor-doped BaTiO3, the aligned domains can facilitate conducting electrons and thus enhance conduction. This can explain why optimal donor-doped BaTiO3 exhibits the lowest resistivity at room temperature.126

The PTCR properties are strongly controlled by the microstructural aspects of donor-doped BaTiO3 which is highly sensitive to the cation stoichiometry90, 117, 130, 131 and processing parameters.46 Understanding the relationship between microstructure and the PTCR effect and the ways in which microstructure can be changed by chemistry and processing conditions not only help to optimize the performance of PTCR materials but also master potentially the capability for tailoring the PTCR properties by targetedly adjusting composition and processing parameters.

- Emerging Trend and Conclusion

After half a century’s development, the technologies for fabrication of advanced PTCR thermistors have vastly expanded and improved. The requirements for new PTCR sensors are miniaturization, environmental acceptability and optimizing the PTCR effect by reducing Rmin, increasing the PTCR jump, decreasing the response time near Tc, increasing Tc and obtaining voltage independence. The single-donor doping system may be inadequate to satisfy all these needs. Multiple-donor systems are considered as potential solutions. Currently double-donor doping systems including Y2O3+Nb2O5132 and Sb2O3+Nb2O5133 have been investigated leading to lower room-temperature resistivity. However, the co-influence of the multiple-donor system still remains poorly understood.

Fabrication of multilayer structures of semiconducting BaTiO3 ceramics provides another way to decrease the room-temperature resistivity.134 This method has the advantage in substantially reducing the room-temperature resistivity over those that rely on change of compositions or heat-treatment parameters because it creates a parallel electric system. However, it is very difficult to co-fire BaTiO3 having PTCR characteristics with an internal electrode system because the need for an oxidizing atmosphere oxidizes base metal electrodes causing severe deterioration to the ohmic contact with the n-type semiconducting BaTiO3.135 On the other hand, if sintered in a reduced atmosphere, the PTCR effect would be substantially compromised.38 Therefore, a procedure that prevents oxidation of the internal electrodes without sacrificing the PTCR characteristics during firing is required.

So far, commercially available PTCR thermistors with Tc > 130(C are mainly based on Pb-doped BaTiO3 ceramics. Because of the toxicity of lead oxide and detrimental influence on the environment during the preparation of Pb-contained products, considerately effort is devoted to compositional developments of lead-free PTCR ceramics. Recently, an excellent PTCR effect at 170(C has been reported in the La-doped 95BaTiO3-5(Bi0.5Na0.5)TiO3 (BT-BNT) ceramics.136 Furthermore, without adding any foreign donor dopant, a PTCR effect was found in pure BT-BNT solid solution ceramics with low BNT contents.5, 137 The BT-BNT system shows PTCR properties comparable to those of lead-containing BT ceramics. However the noncompetitive PTCR jump and strong sensitivity to the oxygen atmosphere during sintering lag its applications. Research is ongoing to tackle those disadvantages.138, 139 In addition, similar system like BaTiO3-(Bi0.5K0.5)TiO3 also attracts many interests most recently.140-142 Other new systems of lead-free high Curie temperature PTCR ceramics are also demanded.

The PTCR effect in nanograined BaTiO3 ceramics is hardly realized regardless of the compositions or processing parameters. This barrier has limited the application of modern nanotechnologies such as using nanoparticles or thin-film fabrications. Most recently, a few articles have reported that PTCR characteristics could be found in nanograined BaTiO3 ceramics synthesized from surface-coated nanopowders.121, 143 More work is needed to explore new methods that are able to make very fine grained (≈1 μm) BaTiO3 ceramics exhibiting good PTCR effects which would be a significant step towards creating the next generation miniaturized PTCR devices.

The conventional fabrication methods of PTCR materials are time consuming especially for making different batches having different compositions. Hence high-throughput fabrication of PTCR products in applications to both industrial and research is desire. Currently, a freeforming method of making thick-film PTC thermistor by paste extrusion technology combined with laser sintering is reported.144 This technique does not require any high temperature post processing as oven-fired is required for PTC ceramics produced by all other methods. This can inspire the new applications of PTCR products in rapid-prototyping which has never been reported before. The development of PTCR materials is still very often a kind of empirical (“trial and error”) science; therefore the high-throughput combinatorial method is a key to the speed-up of production of optimized materials. The London University Search Instrument (LUSI) has been proved the working of the automation system on producing and measuring combinatorial libraries of microwave dielectric ceramics including Ba1-xSrxTiO3 (BST)145 and Ba1-xCaxTiO3 (BCT)146 families. The new study of using such technique on BaTiO3-based PTCR ceramics will be reported and discussed.

In this paper, the state of art in the field of positive temperature coefficient resistivity in BaTiO3-based ceramics is described. Several models to elucidate the PTCR effect in donor-doped BaTiO3 are reviewed. The origin of the room-temperature conductivity of doped-BaTiO3 with PTCR behaviour is due to a combination of multiple mechanisms including the charge compensation scheme and the oxygen-loss theory because neither of them can explain the entire phenomenon individually. The PTCR property of donor-doped BaTiO3 is very sensitive to the chemical composition including the donor’s type and concentration, the acceptor’s type and concentration, cation stoichiometry and other sintering aid additives. Changing the processing parameters can substantially influence the microstructure and therefore the PTCR performance of donor-doped BaTiO3. There is general agreement that the PTCR behaviour is caused by the grain boundary effect. An understanding of the microstructural aspects of donor-doped BaTiO3 is of fundamental importance for correct interpretation of the PTCR effect. These are materials for which understanding the complex interrelationship between composition and microstructure is necessary to predict and improve PTCR properties.

References

1.	D. Y. Wang and K. Umeya: 'Electrical properties of PTCR barium titanate', J. Am. Ceram. Soc., 1990, 73(3), 669-677.

2.	J. Qi, Z. Gui, Y. Wang, Q. Zhu, Y. Wu, and L. Li: 'The PTCR effect in BaTiO3 ceramics modified by donor dopant', Ceram. Int., 2002, 28(2), 141-143.

3.	C. K. Liang and C. C. Tsai: 'Evaluation of a novel PTC thermistor for telecom overcurrent protection', Sens. Actuator A-Phys., 2005, 121(2), 443-449.

4.	S. Jayanthi and T. R. N. Kutty: 'Effect of segregative additives on the positive temperature coefficient in resistance characteristics of n-BaTiO3 ceramics', J. Mater. Sci. - Mater. Electron., 2006, 17(11), 883-897.

5.	T. Shimada, K. Touji, Y. Katsuyama, H. Takeda, and T. Shiosaki: 'Lead free PTCR ceramics and its electrical properties', J. Eur. Ceram. Soc., 2007, 27(13-15), 3877-3882.

6.	B. Huybrechts, K. Ishizaki, and M. Takata: 'The positive temperature-coefficient of resistivity in barium titanate', J. Mater. Sci., 1995, 30(10), 2463-2474.

7.	J. Nowotny and M. Rekas: 'Positive temperature-coefficient of resistivity for BaTiO3-based materials', Ceram. Int., 1991, 17(4), 227-241.

8.	E. Brzozowski and M. S. Castro: 'Conduction mechanism of barium titanate ceramics', Ceram. Int., 2000, 26(3), 265-269.

9.	O. Saburi: 'Semiconducting bodies in the family of barium titanates', Journal of the American Ceramic Society, 1961, 44(2), 54-63.

10.	T. Ota and I. Yamai: 'Positive-temperature-coefficient effect in graphite cristobalite composites', J. Am. Ceram. Soc., 1992, 75(7), 1772-1776.

11.	D. Lisjak, M. Drofenik, and D. Kolar: 'Composite ceramics with a positive temperature coefficient of electrical resistivity effect', Journal of Materials Research, 2000, 15(2), 417-428.

12.	S. Hirano and A. Kishimoto: 'Effect of heating rate on positive-temperature-coefficient-of-resistivity behaviour of conductive composite thin films', Appl. Phys. Lett., 1998, 73(25), 3742-3744.

13.	S. Bhadrakumari and P. Predeep: 'YBa2Cu3O7-x/Thermoplastic polymer composite thermistors', Eur. Polym. J., 2009, 45(1), 226-229.

14.	B. C. Hendrix, X. Wang, W. Chen, and W. Q. Cui: 'Understanding doped V2O3 as a functional positive temperature-coefficient material', J. Mater. Sci. - Mater. Electron., 1992, 3(2), 113-119.

15.	H. R. Kokabi, M. Rapeaux, J. A. Aymami, and G. Desgardin: 'Electrical characterization of PTC thermistor based on chromium doped vanadium sesquioxide', Mater. Sci. Eng., B, 1996, 38(1-2), 80-89.

16.	A. J. Moulson and J. M. Herbert: 'Electroceramics: materials, properties, applications. 2nd Edition ', pp.167-173; 2003, Chichester, John Wiley & Sons, Ltd.

17.	B. M. Kulwicki: 'Advances in ceramics', pp.138-139; 1981, Colombus, OH, American Ceramic Society

18.	L. A. Xue, Y. Chen, and R. J. Brook: 'The influence of ionic-radii on the incorporation of trivalent dopants into BaTiO3', Mater. Sci. Eng., B-solid state mater., 1988, 1(2), 193-201.

19.	Y. S. Jung, E. S. Na, U. Paik, J. Lee, and J. Kim: 'A study on the phase transition and characteristics of rare earth elements doped BaTiO3', Mater. Res. Bull., 2002, 37(9), 1633-1640.

20.	M. D. Glinchuk, I. P. Bykov, S. M. Kornienko, V. V. Laguta, A. M. Slipenyuk, A. G. Bilous, O. I. V'Yunov, and O. Z. Yanchevskii: 'Influence of impurities on the properties of rare-earth-doped barium-titanate ceramics', J. Mater. Chem., 2000, 10(4), 941-947.

21.	O. Saburi: 'Properties of semiconductive barium titanates', Journal of the Physical Society of Japan, J. Phy. Soc. Jpn., 1959, 14, 1159-1174.

22.	W. Heywang: 'Resistivity anomaly in doped barium titanate', J. Am. Ceram. Soc., 1964, 47(10), 484-490.

23.	W. T. Peria, W. R. Bratschun, and R. D. Fenity: 'Possible explanation of positive temperature coefficient in resistivity of semiconducting ferroelectrics', J. Am. Ceram. Soc., 1961, 44(5), 249-250.

24.	G. H. Jonker: 'Some aspects of semiconducting barium titanate', Solid-State Electron., 1964, 7(12), 895-903.

25.	H. D. Megaw: 'Crystal structure of barium titanium oxide and other double oxides of perovskite type', Trans. Faraday Soc., 1946, 42A, 224-231.

26.	O. Saburi and K. Wakino: 'Processing techniques and applications of positive temperature coefficient thermistors', IEEE Transactions on Component Parts, 1963, 10(2), 53-67.

27.	J. Daniels, K. H. Hardtl, and R. Wernicke: 'PTC effect of barium titanate', Philips Technical Review, 1979, 38(3), 73-82.

28.	L. Hozer: 'Semiconductor ceramics : grain boundary effects ', pp.109-141; 1994, London, Ellis Horwood.

29.	G. Goodman: 'Electrical conduction anomaly in samarium doped barium titanate', J. Am. Ceram. Soc., 1963, 46(1), 48-54.

30.	D. C. Sinclair and A. R. West: 'Impedance and modulus spectroscopy of semiconducting BaTiO3 showing positive temperature-coefficient of resistance', J. Appl. Phys., 1989, 66(8), 3850-3856.

31.	H. M. Alallak, A. W. Brinkman, G. J. Russell, A. W. Roberts, and J. Woods: 'The effect of donor dopant concentration on the room temperature resistivity of BaTiO3 ceramics with positive temperature coefficients of resistance', J. Phys. D-Appl. Phys., 1988, 21(7), 1226-1233.

32.	W. Preis, A. Burgermeister, W. Sitte, and P. Supancic: 'Bulk and grain boundary resistivities of donor-doped barium titanate ceramics', Solid State Ion., 2004, 173(1-4), 69-75.

33.	B. Huybrechts, K. Ishizaki, and M. Takata: 'Experimental evaluation of the acceptor-states compensation in positive-temperature-coefficient-type barium titanate', J. Am. Ceram. Soc., 1992, 75(3), 722-724.

34.	M. A. Zubair and C. Leach: 'Modeling the resistance-temperature characteristic of a positive temperature coefficient thermistor, using experimentally determined permittivity data', Appl. Phys. Lett., 2007, 91(8), Article Number: 082105.

35.	T. Miki, A. Fujimoto, and S. Jida: 'An evidence of trap activation for positive temperature coefficient of resistivity in BaTiO3 ceramics with substitutional Nb and Mn as impurities', J. Appl. Phys., 1998, 83(3), 1592-1603.

36.	A. B. Alles, V. R. W. Amarakoon, and V. L. Burdick: 'Positive temperature-coefficient of resistivity effect in undoped, atmospherically reduced barium titanate', J. Am. Ceram. Soc., 1989, 72(1), 148-151.

37.	S. Jiang, D. Zhou, S. Gong, and X. Guan: 'Effect of heat-treatment under oxygen atmosphere on the electrical properties of BaTiO3 thermistor', Microelectron. Eng., 2003, 66(1-4), 896-903.

38.	N. Hideaki, M. Kenjiro, S. Yukio, and K. Makoto: 'Influence of Ba/Ti ratio on the positive temperature coefficient of resistivity characteristics of Ca-doped semiconducting BaTiO3 fired in reducing atmosphere and reoxidized in air', J. Am. Ceram. Soc., 2007, 90(6), 1817-1821.

39.	J. Daniels, K. H. Hardtl, D. Hennings, and R. Wernicke: 'Defect chemistry and electrical-conductivity of doped barium titanate ceramics', Philips Research Reports, 1976, 31(6), 487-488.

40.	G. H. Jonker and E. E. Havinga: 'The influence of foreign ions on the crystal lattice of barium titanate', Mater. Res. Bull., 1982, 17(3), 345-350.

41.	H. M. Chan, M. P. Harmer, and D. M. Smyth: 'Compensating defects in highly donor-doped BaTiO3', J. Am. Ceram. Soc., 1986, 69(6), 507-510.

42.	M. T. Buscaglia, V. Buscaglia, M. Viviani, and P. Nanni: 'Atomistic simulation of dopant incorporation in barium titanate', J. Am. Ceram. Soc., 2001, 84(2), 376-384.

43.	D. M. Smyth: 'The defect chemistry of donor-doped BaTiO3: A rebuttal', J. Electroceram., 2002, 9(3), 179-186.

44.	H. T. Langhammer, M. Drofenik, K. H. Felgner, and H. P. Abicht: 'Investigation of semiconducting barium titanate ceramics by oxygen coulometry', J. Electroceram., 2004, 13(1-3), 793-797.

45.	H. T. Langhammer, Q. M. Song, K. H. Felgner, and H. P. Abicht: 'Investigations on the defect chemistry and the sintering of barium titanate ceramics by oxygen coulometry', Solid State Sci., 2002, 4(2), 197-203.

46.	D. Makovec and M. Drofenik: 'Microstructural changes during the reduction/reoxidation process in donor-doped BaTiO3 ceramics', Journal of the American Ceramic Society, J. Am. Ceram. Soc., 2000, 83(10), 2593-2599.

47.	O. I. V'Yunov, L. L. Kovalenko, A. G. Belous, and V. N. Belyakov: 'Oxidation of reduced Y-doped semiconducting barium titanate ceramics', Inorg. Mater., 2005, 41(1), 87-93.

48.	F. D. Morrison, A. M. Coats, D. C. Sinclair, and A. R. West: 'Charge compensation mechanisms in La-doped BaTiO3', J. Electroceram., 2001, 6(3), 219-232.

49.	F. D. Morrison, D. C. Sinclair, and A. R. West: 'Doping mechanisms and electrical properties of La-doped BaTiO3 ceramics', International Journal of Inorganic Materials, Inter. J. Inorg. Mater. 2001, 3(8), 1205-1210.

50.	F. D. Morrison, D. C. Sinclair, and A. R. West: 'An alternative explanation for the origin of the resistivity anomaly in La-doped BaTiO3', J. Am. Ceram. Soc., 2001, 84(2), 474-476.

51.	H. Beltran, E. Cordoncillo, P. Escribano, D. C. Sinclair, and A. R. West: 'Oxygen loss, semiconductivity, and positive temperature coefficient of resistance behavior in undoped cation-stoichiometric BaTiO3 ceramics', J. Appl. Phys., 2005, 98(9), Article Number: 094102.

52.	W. Hayes and A. M. Stoneham: 'Defects and defect processes in nonmetallic solids'; 1985, London, John Wiley & Sons, Inc.

53.	M. A. Zubair and C. Leach: 'The effect of SiO2 addition on the development of low-Σ grain boundaries in PTC thermistors', J. Eur. Ceram. Soc., 2010, 30(1), 107-112.

54.	D. Makovec, N. Ule, and M. Drofenik: 'Positive temperature coefficient of resistivity effect in highly donor-doped barium titanate', J. Am. Ceram. Soc., 2001, 84(6), 1273-1280.

55.	F. D. Morrison, D. C. Sinclair, and A. R. West: 'Characterization of lanthanum-doped barium titanate ceramics using impedance spectroscopy', J. Am. Ceram. Soc., 2001, 84(3), 531-538.

56.	L. Affleck, J. Seaton, and C. Leach: 'Characterisation of the R-T response of BaTiO3 thermistors on three different length scales', J. Eur. Ceram. Soc., 2007, 27(12), 3439-3444.

57.	P. Fiorenza, R. Lo Nigro, P. Delugas, V. Raineri, A. G. Mould, and D. C. Sinclair: 'Direct imaging of the core-shell effect in positive temperature coefficient of resistance-BaTiO3 ceramics', Appl. Phys. Lett., 2009, 95(14), article No. 142904.

58.	D. Makovec, Z. Samardzija, and M. Drofenik: 'Solid solubility of holmium, yttrium, and dysprosium in BaTiO3', J. Am. Ceram. Soc., 2004, 87(7), 1324-1329.

59.	H. Ueoka: 'Doping effects of transition-elements on PTC anomaly of semiconductive ferroelectric ceramics', Ferroelectrics, 1974, 7(1-4), 351-353.

60.	T. Murakami, T. Miyashita, M. Nakahara, and E. Sekine: 'Effect of rare-earth ions on electrical conductivity of BaTiO3 ceramics', J. Am. Ceram. Soc., 1973, 56(6), 294-297.

61.	V. J. Tennery and R. L. Cook: 'Investigation of rare-earth doped barium titanate', J. Am. Ceram. Soc., 1961, 44(4), 187-193.

62.	Y. Tsur, T. D. Dunbar, and C. A. Randall: 'Crystal and defect chemistry of rare earth cations in BaTiO3', J. Electroceram., 2001, 7(1), 25-34.

63.	T. D. Dunbar, W. L. Warren, B. A. Tuttle, C. A. Randall, and Y. Tsur: 'Electron paramagnetic resonance investigations of lanthanide-doped barium titanate: dopant site occupancy', J. Phys. Chem. B, 2004, 108(3), 908-917.

64.	J. Zhi, A. Chen, Y. Zhi, P. M. Vilarinho, and J. L. Baptista: 'Incorporation of yttrium in barium titanate ceramics', J. Am. Ceram. Soc., 1999, 82(5), 1345-1348.

65.	D. Makovec, Z. Samardzija, and M. Drofenik: 'The solid solubility of holmium in BaTiO3 under reducing conditions', J. Am. Ceram. Soc., 2006, 89(10), 3281-3284.

66.	S. B. Desu and D. A. Payne: 'Interfacial segregation in perovskites: 2. experimental evidence', J. Am. Ceram. Soc., 1990, 73(11), 3398-3406.

67.	S. B. Desu and D. A. Payne: 'Interfacial segregation in perovskites: 4. internal boundary layer devices', J. Am. Ceram. Soc., 1990, 73(11), 3416-3421.

68.	S. B. Desu and D. A. Payne: 'Interfacial segregation in perovskites: 3. microstructure and electrical properties', J. Am. Ceram. Soc., 1990, 73(11), 3407-3415.

69.	C. J. Peng and H. Y. Lu: 'Compensation effect in semiconducting barium titanate', J. Am. Ceram. Soc., 1988, 71(1), C44-C46.

70.	C. J. Ting, C. J. Peng, H. Y. Lu, and S. T. Wu: 'Lanthanum-magnesium and lanthanum-manganese donor-acceptor-codoped semiconducting barium titanate', J. Am. Ceram. Soc., 1990, 73(2), 329-334.

71.	S. H. Yoon, K. H. Lee, and H. Kim: 'Effect of acceptors on the segregation of donors in niobium-doped barium titanate positive temperature coefficient resistors', J. Am. Ceram. Soc., 2000, 83(10), 2463-2472.

72.	J. Seaton and C. Leach: 'Local property measurement in PTC thermistors', Acta Mater., 2003, 51(20), 6027-6034.

73.	P.-J. Wang, Z.-Q. Zeng, Z.-L. Gui, and L.-T. Li: 'Strontium-lead titanate ceramics with positive temperature coefficient of resistance', Mater. Lett., 1997, 30(4), 275-277.

74.	J. Zhao, L. Li, and Z. Gui: 'A study of V-shaped PTC behaviour of Sr0.4Pb0.6TiO3 ceramics', J. Eur. Ceram. Soc., 2002, 22(7), 1171-1175.

75.	J. Zhao, L. Li, and Z. Gui: 'Influence of lithium modification on the properties of Y-doped Sr0.5Pb0.5TiO3 thermistors', Sens. Actuators, A, 2001, 95(1), 46-50.

76.	C. Chou, H. Chang, I. Lin, and B. Shaw: 'Microscopic examination of the microwave sintered (Pb0.6Sr0.4)TiO3 positive-temperature-coefficient resistor materials', Jpn. J. Appl. Phys., 1998, 37, 5269-5272.

77.	D. Völtzke, H. P. Abicht, E. Pippel, and J. Woltersdorf: 'Ca-containing additives in PTC-BaTiO3 ceramics: effects on the microstructural evolution', J. Eur. Ceram. Soc., 2000, 20(11), 1663-1669.

78.	S. Anwar, P. R. Sagdeo, and N. P. Lalla: 'Ferroelectric relaxor behavior in hafnium doped barium-titanate ceramic', Solid State Commun., 2006, 138(7), 331-336.

79.	M. Kumar, A. Garg, R. Kumar, and M. C. Bhatnagar: 'Structural, dielectric and ferroelectric study of Ba0.9Sr0.1ZrxTi1-xO3 ceramics prepared by the sol-gel method', Physica B, 2008, 403(10-11), 1819-1823.

80.	S. G. Lu, Z. K. Xu, and H. Chen: 'Tunability and relaxor properties of ferroelectric barium stannate titanate ceramics', Appl. Phys. Lett., 2004, 85(22), 5319-5321.

81.	Z. Yu, C. Ang, R. Y. Guo, and A. S. Bhalla: 'Ferroelectric-relaxor behavior of Ba(Ti0.7Zr0.3)O3 ceramics', J. Appl. Phys., 2002, 92(5), 2655-2657.

82.	V. V. Shvartsman, W. Kleemann, J. Dec, Z. K. Xu, and S. G. Lu: 'Diffuse phase transition in BaTi1-xSnxO3 ceramics: An intermediate state between ferroelectric and relaxor behavior', J. Appl. Phys., 2006, 99(12), Article Number: 124111.

83.	N. H. Chan and D. M. Smyth: 'Defect chemistry of donor-doped BaTiO3', J. Am. Ceram. Soc., 1984, 67(4), 285-288.

84.	F. A. Selmi and V. R. W. Amarakoon: 'Sol-gel coating of powders for processing electronic ceramics', J. Am. Ceram. Soc., 1988, 71(11), 934-937.

85.	M. Viviani, P. Nanni, M. T. Buscaglia, M. Leoni, V. Buscaglia, and L. Centurioni: 'Impedance spectroscopy of n-doped (Ba,Sr)TiO3 ceramics prepared by modified low temperature aqueous synthesis', J. Eur. Ceram. Soc., 1999, 19(6-7), 781-785.

86.	H. Yaseen, S. Baltianski, and Y. Tsur: 'Effect of incorporating method of niobium on the properties of doped barium titanate ceramics', J. Am. Ceram. Soc., 2006, 89(5), 1584-1589.

87.	B. Cui, P. Yu, J. Tian, H. Guo, and Z. Chang: 'Preparation and characterization of niobium-doped barium titanate nanocrystalline powders and ceramics', Mater. Sci. Eng., A, 2007, 454-455, 667-672.

88.	V. N. Shut, S. V. Kostomarov, and A. V. Gavrilov: 'PTCR ceramics produced from oxalate-derived barium titanate', Inorg. Mater., 2008, 44(8), 905-910.

89.	E. Brzozowski, A. C. Caballero, M. Villegas, M. S. Castro, and J. F. Fernandez: 'Effect of doping method on microstructural and defect profile of Sb-BaTiO3', J. Eur. Ceram. Soc., 2006, 26(12), 2327-2336.

90.	N. Mukherjee, R. D. Roseman, and Q. Zhang: 'Sintering behavior and PTCR properties of stoichiometric blend BaTiO3', J. Phys. Chem. Solids, 2002, 63(4), 631-638.

91.	B. K. Park, J. H. Lee, D. Y. Kim, and N. M. Hwang: 'Positive temperature coefficient of resistance effect in heavily niobium-doped barium titanate by the growth of the double-twinned seeds', J. Am. Ceram. Soc., 2001, 84(11), 2707-2709.

92.	J. Qi, Z. Gui, Y. Wu, and L. Li: 'Positive temperature coefficient resistance effect in Ba1-xSrxTiO3 ceramics modified with Bi2O3 and PbO by vapour doping method', J. Mater. Res., 1999, 14(8), 3328-3329.

93.	S. Chatterjee and H. S. Maiti: 'A novel method of doping PTC thermistor sensor elements during sintering through diffusion by vapour phase', Mater. Chem. Phys., 2001, 67(1-3), 294-297.

94.	J. Qi, Z. Gui, Q. Zhu, Y. Wang, Y. Wu, and L. Li: 'Doping behavior of CdO in BaTiO3-based PTCR ceramics', Sens. Actuators, A, 2002, 100(2-3), 244-246.

95.	J. Qi, Z. Gui, Y. Wu, and L. Li: 'Influence of manganese on PTCR effect in BaTiO3-based ceramics doped with Bi2O3 vapour', Mater. Chem. Phys., 2002, 73(1), 97-100.

96.	S. R. Syrtsov, V. N. Shut, and I. F. Kashevich: 'Positive temperature coefficient of resistivity in thin films of barium titanate', Mater. Sci. Semicond. Process., 2003, 5, 223-225.

97.	L. Yan, H. B. Lu, Z. H. Chen, S. Y. Dai, Y. L. Zhou, and G. Z. Yang: 'Characteristics of BaNbxTi1-xO3 thin films grown by laser molecular beam epitaxy', J. Cryst. Growth, 2002, 244(3-4), 225-228.

98.	N. Lemee, C. Dubourdieu, G. Delabouglise, J. P. Senateur, and F. Laroudie: 'Semiconductive Nb-doped BaTiO3 films grown by pulsed injection metalorganic chemical vapor deposition', J. Cryst. Growth, 2002, 235(1-4), 347-351.

99.	D. Nagano, H. Funakubo, K. Shinozaki, and N. Mizutani: 'Electrical properties of semiconductive Nb-doped BaTiO3 thin films prepared by metal-organic chemical-vapor deposition', Appl. Phys. Lett., 1998, 72(16), 2017-2019.

100.	Y. Shao, R. A. Hughes, A. Dabkowski, G. Radtke, W. H. Gong, J. S. Preston, and G. A. Botton: 'Structural and transport properties of epitaxial niobium-doped BaTiO3 films', Appl. Phys. Lett., 2008, 93(19), 3.

101.	E. Arveux, S. Payan, M. Maglione, and A. Klein: 'Surface segregation in Nb-doped BaTiO3 films', Appl. Surf. Sci., 2010, 256(21), 6228-6232.

102.	S. Chatterjee, K. Sengupta, and H. S. Maiti: 'A miniature PTC thermistor based sensor element fabricated by tape casting technique', Sens. Actuators, B, 1999, 60(2-3), 155-160.

103.	D. Zhou, Z. Zheng, S. Gong, G. Huang, and Y. Hu: 'The influence of shaping process on microstructure and properties of BaTiO3-based chip thermistors', Ceram. Int., 2006, 32(7), 839-842.

104.	H. A. Sauer and J. R. Fisher: 'Processing of positive temperature coefficient thermistors', J. Am. Ceram. Soc., 1960, 43(6), 297-301.

105.	J. B. MacChesney and J. F. Potter: 'Factors and Mechanisms Affecting the Positive Temperature Coefficient of Resistivity of Barium Titanate', J. Am. Ceram. Soc., 1965, 48(2), 81-88.

106.	B. C. LaCourse and V. R. W. Amarakoon: 'Characterization of the firing schedule for positive temperature coefficient of resistance BaTiO3', J. Am. Ceram. Soc., 1995, 78(12), 3352-3356.

107.	D. C. Sinclair and A. R. West: 'Effect of atmosphere on the PTCR properties of BaTiO3 ceramics', J. Mater. Sci., 1994, 29(23), 6061-6068.

108.	M. Ozawa and S. Suzuki: 'Influence of heat treatment with nitrogen in positive-temperature-coefficient-type BaTiO3', J. Mater. Sci. Lett., 1997, 16(7), 545-546.

109.	M. Kuwabara, H. Matsuda, N. Kurata, and E. Matsuyama: 'Shift of the curie point of barium titanate ceramics with sintering temperature', J. Am. Ceram. Soc., 1997, 80(10), 2590-2596.

110.	R. N. Basu and H. S. Maiti: 'Effect of sintering time on the resistivity of semiconducting BaTiO3 ceramics', Mater. Lett., 1987, 5(3), 99-102.

111.	M. Kahn: 'Effect of heat-treatment on PTCR anomaly in semiconductinig barium titanate', Am. Ceram. Soc. Bull., 1971, 50(8), 676-677.

112.	M. A. Zubair and C. Leach: 'The influence of cooling rate and SiO2 additions on the grain boundary structure of Mn-doped PTC thermistors', J. Eur. Ceram. Soc., 2008, 28(9), 1845-1855.

113.	M. A. Zubair and C. Leach: 'Modeling the effect of SiO2 additions and cooling rate on the electrical behavior of donor-acceptor codoped positive temperature coefficient thermistors', J. Appl. Phys., 2008, 103(12), Article Number:123713.

114.	P. Bomlai, N. Sirikulrat, and T. Tunkasiri: 'Effect of heating rate on the properties of Sb and Mn-doped barium strontium titanate PTCR ceramics', Mater. Lett., 2005, 59(1), 118-122.

115.	G. S. Liu and R. D. Roseman: 'Secondary thermal treatment effect on PTCR BaTiO3', J. Mater. Sci. Lett., 1999, 18(22), 1875-1878.

116.	S. Jida, T. Suemasu, and T. Miki: 'Effect of microwave heating on BaTiO3 : Nb ceramics with positive temperature coefficient of resistivity', J. Appl. Phys., 1999, 86(4), 2089-2094.

117.	T.-F. Lin, C.-T. Hu, and I. N. Lin: 'Influence of stoichiometry on the microstructure and positive temperature coefficient of resistivity of semiconducting barium titanate ceramics', J. Am. Ceram. Soc., 1990, 73(3), 531-536.

118.	P. Knauth: 'Ionic and electronic conduction in nanostructured solids: Concepts and concerns, consensus and controversies', Solid State Ionics, 2006, 177, 2495-2502.

119.	B. D. Begg, E. R. Vance, and J. Nowotny: 'Effect of particle size on the room-temperature crystal structure of barium titanate', J. Am. Ceram. Soc., 1994, 77(12), 3186-3192.

120.	M. Yashima, T. Hoshina, D. Ishimura, S. Kobayashi, W. Nakamura, T. Tsurumi, and S. Wada: 'Size effect on the crystal structure of barium titanate nanoparticles', J. Appl. Phys., 2005, 98(1), Article Number: 014313.

121.	M. B. Park, N. H. Cho, C. D. Kim, and S. K. Lee: 'Phase transition and physical characteristics of nanograined BaTiO3 ceramics synthesized from surface-coated nanopowders', J. Am. Ceram. Soc., 2004, 87(3), 510-512.

122.	C. S. Hwang, B. T. Lee, H. J. Cho, K. H. Lee, C. S. Kang, H. Hideki, S. I. Lee, and M. Y. Lee: 'A positive temperature coefficient of resistivity effect from a paraelectric Pt/(Ba0.5,Sr0.5)TiO3/IrO2 thin-film capacitor', Appl. Phys. Lett., 1997, 71(3), 371-373.

123.	W. F. Qin, J. Zhu, J. Xiong, J. L. Tang, W. J. Jie, X. H. Wei, Y. Zhang, and Y. R. Li: 'Electrical behavior of Y-doped Ba0.6Sr0.4TiO3 thin films', J. Mater. Sci. - Mater. Electron., 2007, 18(12), 1217-1220.

124.	M. Okano, Y. Watanabe, and S. W. Cheong: 'Nonlinear positive temperature coefficient of resistance of BaTiO3 film', Appl. Phys. Lett., 2003, 82(12), 1923-1925.

125.	M. Kuwabara: 'Effect of microstructure on the PTCR effect in semiconducting barium titanate ceramics', J. Am. Ceram. Soc., 1981, 64(11), 639-644.

126.	R. D. Roseman and N. Mukherjee: 'PTCR effect in BaTiO3: Structural aspects and grain boundary potentials', J. Electroceram., 2003, 10(2), 117-135.

127.	D. L. Zhang, D. X. Zhou, S. L. Jiang, X. Wang, and S. P. Gong: 'Effects of porosity on the electrical characteristics of current-limiting BaTiO3-based positive-temperature-coefficient (PTC) ceramic thermistors coated with electroless nickel-phosphorous electrode', Sens. Actuator A-Phys., 2004, 112(1), 94-100.

128.	J.-G. Kim: 'Synthesis of porous (Ba,Sr)TiO3 ceramics and PTCR characteristics', Mater. Chem. Phys., 2002, 78(1), 154-159.

129.	A. Hasegawa, S. Fujitsu, K. Koumoto, and H. Yanagida: 'The enhanced penetration of oxygen along the grain-boundary in semiconducting barium titanate', Jpn. J. Appl. Phys., 1991, 30(6), 1252-1255.

130.	G. S. Liu and R. D. Roseman: 'Effect of BaO and SiO2 addition on PTCR BaTiO3 ceramics', Journal of Materials Science, J. Mater. Sci. 1999, 34(18), 4439-4445.

131.	M. Drofenik, D. Makovec, I. Zajc, and H. T. Langhammer: 'Anomalous grain growth in donor-doped barium titanate with excess barium oxide', Journal of the American Ceramic Society, J. Am. Ceram. Soc., 2002, 85(3), 653-660.

132.	Z. He, J. Ma, Y. Qu, and X. Feng: 'Effect of additives on the electrical properties of a (Ba0.92Sr0.08)TiO3-based positive temperature coefficient resistor', J. Eur. Ceram. Soc., 2002, 22(13), 2143-2148.

133.	Z. M. He, J. Ma, Y. F. Qu, and C. G. Wang: 'Compositional and processing effects on electrical properties of (Ba0.85Pb0.15)TiO3-based positive temperature coefficient resistors', J. Eur. Ceram. Soc., 2004, 24(14), 3617-3622.

134.	H. Mimi, K. Mihara, Y. Sakabe, and M. Kuwabara: 'Preparation of multilayer semiconducting BaTiO3 ceramics co-fired with Ni inner electrodes', Jpn. J. Appl. Phys. Part 1 - Regul. Pap. Brief Commun. Rev. Pap., 2007, 46(10A), 6715-6718.

135.	A. Kanda, S. Tashiro, and H. Igarashi: 'Effect of firing atmosphere on electrical properties of multilayer semiconducting ceramics having positive temperature coefficient of resistivity and Ni–Pd internal electrodes', Jpn. J. Appl. Phys., 1994, 33, 5431-5434.

136.	H. Takeda, W. Aoto, and T. Shiosaki: 'BaTiO3-(Bi1/2Na1/2)TiO3 solid-solution semiconducting ceramics with Tc > 130°C', Appl. Phys. Lett., 2005, 87(10), Article Number: 102104.

137.	B. J. Chu, D. R. Chen, G. R. Li, and Q. R. Yin: 'Electrical properties of Na1/2Bi1/2TiO3-BaTiO3 ceramics', J. Eur. Ceram. Soc., 2002, 22(13), 2115-2121.

138.	P. h. Xiang, H. Harinaka, H. Takeda, T. Nishida, K. Uchiyama, and T. Shiosaki: 'Annealing effects on the characteristics of high Tc lead-free barium titanate-based positive temperature coefficient of resistivity ceramics', J. Appl. Phys., 2008, 104(9), Article Number: 094108.

139.	P. H. Xiang, H. Takeda, and T. Shiosaki: 'Characterization of manganese-doped BaTiO3-(Bi1/2Na1/2)TiO3 positive temperature coefficient of resistivity ceramics using impedance spectroscopy', J. Appl. Phys., 2008, 103(6), Article Number: 064102.

140.	S. L. Leng, G. R. Li, L. Y. Zheng, T. B. Wang, and Q. R. Yin: 'Synthesis of Y-Doped BaTiO3-(Bi1/2K1/2)TiO3 Lead-Free Positive Temperature Coefficient of Resistivity Ceramics and Their PTC Effects', J. Am. Ceram. Soc., 2009, 92(11), 2772-2775.

141.	H. Takeda, H. Harinaka, T. Shiosaki, M. A. Zubair, C. Leach, R. Freer, T. Hoshina, and T. Tsurumi: 'Fabrication and positive temperature coefficient of resistivity properties of semiconducting ceramics based on the BaTiO3-(Bi1/2K1/2)TiO3 system', J. Eur. Ceram. Soc., 2010, 30(2), 555-559.

142.	J. F. Wei, Y. P. Pu, Y. Q. Mao, and J. F. Wang: 'Effect of the Reoxidation on Positive Temperature Coefficient Behavior of BaTiO3-Bi0.5Na0.5TiO3', J. Am. Ceram. Soc., 2010, 93(6), 1527-1529.

143.	R. L. Brutchey, G. S. Cheng, Q. Gu, and D. E. Morse: 'Positive temperature coefficient of resistivity in donor-doped BaTiO3 ceramics derived from nanocrystals synthesized at low temperature', Adv. Mater., 2008, 20(5), 1029-1032.

144.	Z. Cai, X. Li, Q. Hu, and X. Zeng: 'Laser sintering of thick-film PTC thermistor paste deposited by micro-pen direct-write technology', Microelectron. Eng., 2009, 86(1), 10-15.

145.	R. C. Pullar, Y. Zhang, L. F. Chen, S. F. Yang, J. R. G. Evans, P. K. Petrov, A. N. Salak, D. A. Kiselev, A. L. Kholkin, V. M. Ferreira, and N. M. Alford: 'Manufacture and measurement of combinatorial libraries of dielectric ceramics - Part II. Dielectric measurements of Ba1-xSrxTiO3 libraries', J. Eur. Ceram. Soc., 2007, 27(16), 4437-4443.

146.	R. C. Pullar, Y. Zhang, L. Chen, S. Yang, J. R. G. Evans, A. N. Salak, D. A. Kiselev, A. L. Kholkin, V. M. Ferreira, and N. M. Alford: 'Dielectric measurements on a novel Ba1-xCaxTiO3 (BCT) bulk ceramic combinatorial library', J. Electroceram., 2009, 22(1), 245-251.

147.	J. G. Stark: 'Chemistry Data book', pp.28-29; 1984, London, John Murray Ltd.

148.	J. G. Kim, W. P. Tai, and J. G. Ha: 'PTCR characteristics and fabrication of porous, Sb-doped BaTiO3 ceramics', J. Porous Mat., 2003, 10(1), 69-74.

149.	D. Zhou, M. Cao, and S. Gong: 'A novel method of preparing Ba0.96Ca0.04Ti1.02O3 ceramics with low room temperature resistivity', Mater. Sci. Eng., B, 2003, 99(1-3), 399-402.

150.	Z. C. Li and B. Bergman: 'Electrical properties and ageing characteristics of BaTiO3 ceramics doped by single dopants', J. Eur. Ceram. Soc., 2005, 25(4), 441-445.

151.	F. D. Morrison, D. C. Sinclair, and A. R. West: 'Electrical and structural characteristics of lanthanum-doped barium titanate ceramics', J. Appl. Phys., 1999, 86(11), 6355-6366.

152.	M. Cernea, O. Monnereau, P. Llewellyn, L. Tortet, and C. Galassi: 'Sol-gel synthesis and characterization of Ce doped-BaTiO3', J. Eur. Ceram. Soc., 2006, 26(15), 3241-3246.

153.	Z. A. Nemati, M. Tabibazar, and M. R. Deguire: 'The effects of cerium doping on the resistivity of PTCR barium lead titanate', Br. Ceram. Trans., 1993, 92(3), 109-113.

154.	Z. C. Li, H. Zhang, X. D. Zou, and B. Bergman: 'Synthesis of Sm-doped BaTiO3 ceramics and characterization of a secondary phase', Mater. Sci. Eng., B-solid state mater., 2005, 116(1), 34-39.

155.	N. Motohira, H. Okamoto, Y. Nakamura, A. Kishimoto, M. Miyayama, and H. Yanagida: 'Single crystal growth and electrical properties of lanthanum- and gadolinium-doped BaTiO3', J. Ceram. Soc. Jpn., 1996, 104(4), 273-276.

156.	H. Y. Miao, M. Dong, G. Q. Tan, and Y. P. Pu: 'Doping effects of Dy and Mg on BaTiO3 ceramics prepared by hydrothermal method', J. Electroceram., 2006, 16(4), 297-300.

157.	W. H. Lee, W. A. Groen, H. Schreinemacher, and D. Hennings: 'Dysprosium doped dielectric materials for sintering in reducing atmospheres', J. Electroceram., 2000, 5(1), 31-36.

158.	A. Al-Shahrani and S. Abboudy: 'Positive temperature coefficient in Ho-doped BaTiO3 ceramics', J. Phys. Chem. Solids, 2000, 61(6), 955-959.

159.	F. G. Chang, T. Li, Y. X. Ge, Z. P. Chen, Z. S. Liu, and X. P. Jing: 'Electrical properties and positron annihilation study of (Ba1-xHox)TiO3 ceramics', J. Mater. Sci., 2007, 42(17), 7109-7115.

160.	S. K. Jo, Y. H. Han, and K. H. Choi: 'Effects of oxygen partial pressure control on the microstructure and PTCR properties of Ho doped BaTiO3', J. Mater. Sci., 2007, 42(16), 6696-6700.

161.	Y. Liu and A. R. West: 'Ho-doped BaTiO3: Polymorphism, phase equilibria and dielectric properties of BaTi1-xHoxO3-x/2: 0 <= x <= 0.17', J. Eur. Ceram. Soc., 2009, 29(15), 3249-3257.

162.	M. Viviani, M. T. Buscaglia, V. Buscaglia, L. Mitoseriu, A. Testino, P. Nanni, and D. Vladikova: 'Analysis of conductivity and PTCR effect in Er-doped BaTiO3 ceramics', J. Eur. Ceram. Soc., 2004, 24(6), 1221-1225.

163.	M. T. Buscaglia, M. Viviani, V. Buscaglia, C. Bottino, and P. Nanni: 'Incorporation of Er3+ into BaTiO3', J. Am. Ceram. Soc., 2002, 85(6), 1569-1575.

164.	D. J. Wang, Z. L. Gui, and L. T. Li: 'Preparation and electrical properties of semiconducting strontium-lead titanate PTCR ceramics', J. Mater. Sci. - Mater. Electron., 1997, 8(4), 271-276.

165.	S. W. Ding, G. Jia, J. Wang, and Z. Y. He: 'Electrical properties of Y- and Mn-doped BaTiO3-based PTC ceramics', Ceram. Int., 2007, 321.

166.	Y. Wang, L. Li, J. Qi, and Z. Gui: 'Ferroelectric characteristics of ytterbium-doped barium zirconium titanate ceramics', Ceram. Int., 2002, 28(6), 657-661.

167.	W. H. Tzing and W. H. Tuan: 'Effect of NiO addition on the sintering and grain growth behaviour of BaTiO3', Ceram. Int., 1999, 25(1), 69-75.

168.	H. T. Langhammer, T. Müller, R. Böttcher, V. Mueller, and H. P. Abicht: 'Copper-doped hexagonal barium titanate ceramics', J. Eur. Ceram. Soc., 2004, 24(6), 1489-1492.

169.	G. Er, S. Ishida, and N. Takeuchi: 'Durability of Nb-(Fe,Mn)-codoped PTCR BaTiO3 ceramics to reducing atmosphere', J. Ceram. Soc. Jpn., 1998, 106(5), 470-476.

170.	B. Cui, P. Yu, J. Tian, and Z. Chang: 'Preparation and characterization of Co-doped BaTiO3 nanosized powders and ceramics', Mater. Sci. Eng., B, 2006, 133(1-3), 205-208.

171.	D. K. Lee, H. I. Yoo, and K. D. Becker: 'Nonstoichiometry and defect structure of Mn-doped BaTiO3-d', Solid State Ion., 2002, 154, 189-193.

172.	J. H. Lee, S. H. Kim, and S. H. Cho: 'Valence change of Mn ions in BaTiO3-based PTCR materials', J. Am. Ceram. Soc., 1995, 78(10), 2845-2848.

173.	O. I. V'Yunov, L. L. Kovalenko, and A. G. Belous: 'Electrical properties of BaTi1-xMxO3 (M= Nb, Ta, Mo, W) ceramics', Inorg. Mater., 2006, 42(12), 1363-1368.

174.	N. Maso, H. Beltran, E. Cordoncillo, A. A. Flores, P. Escribano, D. C. Sinclair, and A. R. West: 'Synthesis and electrical properties of Nb-doped BaTiO3', J. Mater. Chem., 2006, 16(30), 3114-3119.

175.	X. Wang, H. L. W. Chan, and C. Choy: 'Positive temperature coefficient of resistivity effect in niobium-doped barium titanate ceramics obtained at low sintering temperature', J. Eur. Ceram. Soc., 2004, 24(6), 1227-1231.

176.	N. Maso, H. Beltran, E. Cordoncillo, D. C. Sinclair, and A. R. West: 'Polymorphism and dielectric properties of Nb-doped BaTiO3', J. Am. Ceram. Soc., 2008, 91(1), 144-150.

Table Captions

Table 1. Summary of aliovalent dopants in BaTiO3 (ionic radii data from 147).

Table 1.

| Ions | Ionic radius (Å) | Main type of dopant when Ba/Ti=1 | Reference |
| --- | --- | --- | --- |
| Ba2+ | 1.35 |  |  |
| Ti4+ | 0.68 |  |  |
| Sb3+ | 2.45 | Donor | 89, 148, 149 |
| Bi3+ | 1.20 | Donor | 150 |
| La3+ | 1.15 | Donor | 50, 54, 151 |
| Ce3+ | 1.11 | Donor | 152, 153 |
| Nd3+ | 1.08 | Donor | 68 |
| Sm3+ | 1.04 | Donor | 154 |
| Gd3+ | 1.02 | Donor | 155 |
| Dy3+ | 0.99 | Donor | 156, 157 |
| Ho3+ | 0.97 | Amphoteric dopant | 158-161 |
| Er3+ | 0.96 | Amphoteric dopant | 162, 163 |
| Y3+ | 0.93 | Amphoteric dopant | 64, 164, 165 |
| Yb3+ | 0.86 | Acceptor | 2, 18, 166 |
| Ni2+ | 0.78 | Acceptor | 167 |
| Cu2+ | 0.69 | Acceptor | 168 |
| Cr3+ | 0.69 | Acceptor | 59 |
| Mg2+ | 0.65 | Acceptor | 71 |
| Fe3+ | 0.64 | Acceptor | 169 |
| Co3+ | 0.63 | Acceptor | 170 |
| Mn2+ | 0.80 | Acceptor | 35, 171, 172 |
| Ta5+ | 0.73 | Donor | 150, 173 |
| Nb5+ | 0.70 | Donor | 35, 71, 174-176 |
| W6+ | 0.67 | Donor | 173 |
| Sb5+ | 0.62 | Donor | 4 |
| Mo6+ | 0.62 | Donor | 173 |

Figure Captions.

1. Typical resistivity-temperature characteristic of a BaTiO3-based PTCR material.

2. Electrical double layer at a grain boundary. Es is the electron-trap energy, Ef the Fermi level, Ns the concentration of trapped electrons and b the width of electron depletion layer.

3. Ferroelectric domains at the grain boundaries. P is the vector of spontaneous polarization and PN the normal component of P.

4. Schematic model of the microstructure of the donor-doped BaTiO3 and its equivalent electric circuit. (replotted from 54)

5. Schematic representation of the room-temperature dc resistivity as a function of La-dopant concentration for BaTiO3 ceramics sintered in air. (replotted from 50)

6. The effect of isovalent dopant doping on Tc. (replotted from 151)

7. ρ(T) curves as a function of cooling rate for donor-doped BaTiO3 samples. (replotted from 112)

Figure 1.

Figure 2.

Figure 3.

Figure 4.

Figure 5.

Figure 6.

Figure 7.

# Footnotes

* Corresponding author. Tel: +44 23 8059 8697; Fax: +44 23 8059 3016

E-mail address: s.yang@soton.ac.uk

# Text boxes

ρc

ρmin

ρmax

Tc

Sn4+

Zr4+

Sr2+

Ca2+

Pb2+

Resistivity / (Ω·cm)

150 °C/hr

300 °C/hr

600 °C/hr

Temperature /°C

Resistivity / (Ω·cm)

Reoxidized part

of the grain

Grain

interior

Rg

Rgb

Qox

Rox

Qgb

Intrinsic

grain boundary

Rgb,Qgb

Rox, Rox

Rg