## Slide 1
Optical second harmonic generation from V-shaped chromium nanohole arrays Ngo Khoa Quang1, Yoshihiro Miyauchi1, Goro Mizutani1, Martin D.Charlton2, Ruiqi Chen2, Stuart Boden2, and Harvey Rutt2
1School of Materials Science, Japan Advanced Institute of Science and Technology, 1-1 Asahidai, Nomi, Ishikawa 923-1292, Japan 2School of Electronics and Computer Science, University of Southampton, SO17 1BJ, UK
Introduction
Nonlinear optics of metamaterial
Enhancement of SHG signal from the disordered circular gold nanoholes compared with the periodic one.
Enhancement of SHG signal from the disordered circular gold nanoholes compared with the periodic one.
M.Airola et al. J. Opt. A: Pure Appl. Opt. 7 118 (2005)
Plasmon resonance
Plasmon resonance depends on the orientation of the nanostructures.
Sensible observability
for a surface plasmon resonance of Cr < 0.1
Plasmon resonance of Cr from nonlinear optical standpoint?
Lesufﬂeur et al., Phys. Rev. B. 75, 045423 (2007)
Surface SHG is employed to probe plasmon excitation.
V-shaped holes exhibits a noncentrosymmetry structure
Centrosymetry is broken at the surface
B. K.Canﬁeld et al., J. Opt. A: Pure Appl. Opt. 8, 278 (2006)
Objective
Survey plasmon resonance of the V-shaped chromium nanohole arrays from second order optical standpoint
e-beam lithography & AFM observation
JBX-9300FS Electron Beam Lithography System
100 keV acceleration voltage
200 pA beam current
dose of 150 µC/cm²
V-shaped area of 100 µm²
e-beam exposure
Evaporation of Cr
40nm resist
e-beam resist
Dry etching
SHG signal from V-shaped subwavelength nanoholes
Mutual cancellation at the aperture edge surfaces
The appearance of χ313 proves that SHG signal actually reflects V-shaped nanoholes.
Insignificant contribution of plasmon resonance
Field enhancement at the sharp apex does not occur in terms of nonlinear optics as well.
Designed parameters
AFM observation
15nm Cr
r = 0.8
r = 0.3
r = 0.5
r = 0.4
Correlation coefficient
No field enhancement at the sharp apex
Cancelation
Enhancement
Image dipole effect
at the metal surface
Conclusion
Future plan
Reference
Contact
J. R. Sambles et al., Contemp. Phys. 32, 173 (1991)
  The appearance of χ 313 proves that SHG signal actually reflects V-shaped nanoholes.
  We have considered several competing contributions with respect to the behavior of χ313, which are bulk quadrupoles, lightning rod effect, plasmon exciation, and edge nonlinearity.
  implies an insignificant plasmon excitation.
The change of periodicity or designed parameters could hopefully support the grating coupler for plasmon resonance.
M. Omote et al., J. Phys.: Condens. Matter. 17, 175 (2005).
-Mail address: Mizutani Laboratory, School of Materials Science, 1-1 Asahidai, Nomi, Ishikawa 923-1292 Japan
-Phone: +81-761-51-1521
-E-mail: mizutani@jaist.ac.jp
nm
Remove remaining resist