## Slide 1: Carbon Nanotube Composite Surfaces for Electrical Contacts of MEMS Switches
Project members:
University of Southampton:
Dr Liudi Jiang
Prof Mark Spearing
Mr Michael P. Down
Dr Chamaporn Chianrabutra
USMC:
Prof John W. McBride
Dr Suan H. Pu
Dr Hong Liu
Micro | Nano | MEMS 2014
Dr Adam P. Lewis

## Slide 2: Outline
Introduction
  Motivation and Aims
  Electromechanical Switching Behaviour
Carbon Nanotube Composites
  Mechanical and Electro-mechanical Characterisation
Experimental Overview
  Initial Experiments
    Setup
    Results
  MEMS Experiments
    Fabrication of MEMS Devices
    Results
Summary

## Slide 3: Introduction: Motivation
MEMS relays have numerous advantages:
  Excellent frequency response
  Off-state: zero-low current leakage/high isolation
  On-state: low resistance/low insertion loss
  Small size
Alternative technologies:
  PIN diodes, FETs
  Electromechanical relays
  Reed relays
Source: G. M. Rebeiz – “RF MEMS – Theory, Design, and Technology” (2003)

## Slide 4: Introduction: Motivation
Two types of MEMS switch:
    Capacitive (AC signals only)
    Metal-contacting (DC – AC signals)
Problem:
  Electromechanical interaction between metal contacts
   degradation of contact  limits device lifetime
Lincoln Laboratories
Analog Devices
Raytheon
Source: G. M. Rebeiz & J. B. Muldavin – “RF MEMS Switches and Switch Circuits” – IEEE Microwave Magazine (2001)

## Slide 5: Introduction: Aims
Investigate benefit of Au/MWCNT composites for MEMS switches
Characterise electro-mechanical performance of Au/MWCNT composites
Demonstration of Au/MWCNT as electrical contact for MEMS switch
Further understanding of failure process of Au/MWCNT composites

## Slide 6: Introduction: Electromechanical Switching Behaviour
Every switching cycle:
  Mechanical damage
    Impact (contact) force caused because the contacts physically separate and come into contact – resulting in wear
  Electrical damage
    Hot-switching
    Cold-switching
    Dry-switching

## Slide 7: Introduction: Electromechanical Switching Behaviour
For hot-switching case: molten metal bridge (MMB)
Every cycle:
    Surface melts
    Molten metal bridge
    Breaks unevenly
    Material transfer
Contact 1
Contact 2

## Slide 8: Introduction: Electromechanical Switching Behaviour
Graph showing typical MMB
For gold:
  Melting voltage: 0.43 V
  Boiling voltage: 0.88 V

## Slide 9: Introduction: Electromechanical Switching Behaviour
Graph showing typical MMB
For gold:
  Melting voltage: 0.43 V
  Boiling voltage: 0.88 V

## Slide 10: Introduction: Electromechanical Switching Behaviour
Illustration showing variation of MMB phenomenon
  10 cycles – same switching conditions

## Slide 11: Carbon Nanotube Composites
Mechanical Characterisation
Electro-mechanical Characterisation

## Slide 12: Carbon Nanotube Composites
Mechanical properties of Multi-Walled Carbon Nanotube (MWCNT) forest reduces wear and improves lifetime

## Slide 13: Carbon Nanotube Composites
Buffer layer = Al₂O₃
Catalyst layer = Fe
Sputter
CVD
CVD
Sputter
Heat to growth temperature - anneal
Gas = Ar + H₂
Grow MWCNTs
Gas = Ar + C2H4
Sputter
Au layer: 500 nm

## Slide 14: Carbon Nanotube Composites: Mechanical Properties
Controllable by varying thickness of components
  Increasing gold thickness provides stiffer and harder surface
  Increasing MWCNT thickness increases indentation depth, and contact area

## Slide 15: Carbon Nanotube Composites: Mechanical Properties
Material properties can be defined by composition
Varying the components allows a control of the samples properties, and design for best results

## Slide 16: Carbon Nanotube Composites: Mechanical Properties
Characterising the samples in terms of the thickness ratio
Allows predictive models of various untested compositions
Sample of specific mechanical properties can then be developed

## Slide 17: Carbon Nanotube Composites: Mechanical Properties
Au thickness affects only the energy absorption of the composite and dynamic hardness
More Au provides a less absorbing surface, with more bounces

## Slide 18: Carbon Nanotube Composites: Mechanical Properties
The MWCNT layer affects the residual depth of the indents more than absorption
The long CNTs provide more compliance, increasing depth and contact area

## Slide 19: Carbon Nanotube Composites: Electro-mechanical Properties
Notes: Discuss: electro mechanical characterisation based on composition (thicker MWCNTs slightly increase resistance, thicker Au dramatically reduces the resistance); the evidence of a good electrical contact surface (low resistivity at low loads (below 1 Ohm at 1mN);

## Slide 20: Switching Experiments

## Slide 21: Experimental Overview
Number of experiments performed on range of rigs and devices
  Initial Experiments:
      PZT-based rig
      Limited frequency
      Long testing durations
  MEMS based rig
    Higher frequency
    Closer to MEMS device
      dimensions/actuation method/contact force/etc.
    Two stage development process:
      2.1 Device 1 – design, fabrication and results
      2.2 Device 2 – design and fabrication

## Slide 22: Initial Experiments: Setup
Au-coated ball
Charge amplifier
Au-MWCNT composite
PZT cantilever moves sample up and down
- simulating contact

## Slide 23: Initial Experiments: Setup
Constants:
  Load voltage: 4 V
  Contact force: 1 mN
  Contact pair: Cr/Au ball to Au/MWCNT forest [30 µm high forest with 500 nm Au]
Varied:
  Load current: 20, 30, 40, 50 and 200 mA

## Slide 24: Initial Experiments: Results
Fine transfer model
The number of cycle to failure for a given load current:
volume = k x I2
Nfail = 3x1011 x I-2
Au/MWCNT
Model

## Slide 25: Initial Experiments: Results
SEM images of failed Au/MWCNT composites tested with different load currents
20 mA
50 mA
40 mA
200 mA
30 mA

## Slide 26: MEMS Devices
Device 1

## Slide 27: MEMS Experiments: Fabrication of MEMS Device 1
From the fundamental equations and modelling with Coventor the following dimensions were chosen:
  Length: 10 mm
  Thickness: 20 µm
  Width: 2 mm
Predicted resonant frequency: 240 Hz
  70 mins for 106 cycles
  4.8 days for 108 cycles
Predicted pull-in voltage (for gap <25 µm): < 30 V

## Slide 28: MEMS Experiments: Fabrication of MEMS Device 1
Silicon wafer
Photolithography on top side
Etch top (~20 µm)
Wafer dicing
Photolithography on under side
Etch large part of underside
(~400 µm)
Finish underside etch

## Slide 29: MEMS Experiments: Fabrication of the MEMS Device 1
Sputter-coat cantilever beam with 10 nm and 500 nm of Cr and Au respectively
Measured 1st modal resonant frequency:
  235 Hz
2 mm
10 mm

## Slide 30: MEMS Experiments: Setup
Constants:
  Load voltage: 4 V
  Electrostatic actuation
    Contact force: ~5 – 10 µN
Varied:
  Load current: 10 and 50 mA

## Slide 31: MEMS Experiments: Device 1 Results

## Slide 32: MEMS Experiments: Device 1 Results
At 10 mA composite survived for >500 million hot-switched (4 V) cycles
At 50 mA composite failed after 44.4 million hot-switched (4 V) cycles

## Slide 33: MEMS Experiments: Device 1 Results
Outline illustrating cantilever beam overlap
Au/MWCNT
Au/MWCNT

## Slide 34: MEMS Experiments: Device 1 Results
Before experiment
After experiment
Cantilever Beam Tip
Cantilever Beam Tip

## Slide 35: MEMS Devices
Device 2

## Slide 36: MEMS Experiments: Fabrication of MEMS Device 2
From the fundamental equations and modelling with Coventor the following dimensions were chosen:
  Length: 1.7 mm
  Thickness: 10 µm
  Width: 100 µm
Predicted resonant frequency: 4.3 kHz
  At 4 kHz it would take 1.5 days to reach 500 million cycles
Predicted pull-in voltage (for gap <5 µm): < 12 V

## Slide 37: MEMS Experiments: Fabrication of MEMS Device 2
SOI wafer
Photolithography to define cantilevers
Wet etch large part of oxide layer
HF vapour etch to release beams
Etch device layer (10 µm)
Wafer dicing
Sputter with Cr/Au
500 µm

## Slide 38: MEMS Experiments: Planned Experiments
Investigate lifetime for range of load currents
  10 mA – 100 mA
Investigate failure mechanisms at low force and compare with initial results (1 mN)
Investigate effect of MWCNT forest parameters:
  forest height
  gold-thickness
  contact material

## Slide 39: Summary

## Slide 40: Summary
Understanding electrical and mechanical aspects of switching contacts
  Molten metal bridge phenomenon
  Electrical and mechanical failure mechanisms
Described Au/MWCNT composites
  Fabrication
  Mechanical
  Electro-mechanical performance
  Function as a electrical contact material

## Slide 41: Summary
Investigate failure mechanisms of Au/MWCNT composites when used as electrical contacts
Au/MWCNTs composites give large switching lifetimes even when tested under hot-switching conditions:
  44.4 million cycles at 50 mA (4 V)
  Over 500 million cycles at 10 mA (4V)
Discussed new experimental setup for testing Au/MWCNT contacts
  Enables acquisition of data for further analysis and investigation of failure mechanisms for Au/MWCNT composite contacts
  New setup more closely resembles end device
    Size, contact force, actuation method

## Slide 42: Questions?
This work was supported by the Innovative Electronics Manufacturing Research Centre (IeMRC), UK and Engineering and Physical Sciences Research Council (EPSRC), UK under grant number: EP/H03014X/1.