Electrochemical detection of cupric ions with boron-doped diamond electrode for corrosion monitoring

S. Neodoa, M. Niea,*, J.A. Whartona, A. Crannyb, N.R. Harrisb, R.J.K. Wooda, K.R. Stokesa,c

a National Centre for Advanced Tribology at Southampton (nCATS), Engineering Sciences, Faculty of Engineering and the Environmental, University of Southampton, Southampton,  SO17 1BJ, UK

b Electronic Systems and Devices Group, Electronics and Computer Science, Faculty of Physical Sciences and Engineering, University of Southampton, Southampton,  SO17 1BJ, UK

c Physical Sciences Department, Dstl, Porton Down, Salisbury, Wiltshire, SP4 0JQ, UK

* Corresponding Author

Tel: +44 23 8059 3761; Fax: +44 23 8059 3016; Email: m.nie@soton.ac.uk

Corrosion induced structural failures continue to be a costly problem in many industrial situations, and the development of robust corrosion sensing systems for structural health integrity monitoring is still a demanding challenge.  The applicability of corrosion monitoring of copper alloys using a boron-doped diamond electrode (BDD) has been performed based on determination of copper ions within localised corrosion microenvironments.  The electrochemical behaviour of copper ions on the BDD electrode surface were first reported in details in 0.6 M NaCl aqueous solution, and the results revealed that the electrochemical processes of copper ions on the BDD electrode proceed as two successive single electron transfer steps producing two well-separated pairs of peaks in cyclic voltammograms in the chloride ion containing electrolyte solutions.  Compared with perchlorate and sulphate ions, chloride ions were observed with a significant stabilization effect on copper ions via the formation of  complex, thus having two well-separated pairs of peaks in the obtained cyclic voltammograms on the BDD electrode in the chloride ion electrolyte solution.  The apparent rate constant for the redox couple of Cu(II)/Cu(I) in chloride ion electrolyte was determined as 0.94 × 10–6 cm s–1 by using quasi-steady polarisation technique, thus signifying a quasi-reversible electron transfer process of Cu(II)/Cu(I).  Moreover, the differential pulse voltammetric results exhibited the BDD electrode is promising for corrosion monitoring of copper alloys with an excellent relationship between peak current and concentration of copper ions without significant interference from the commonly presented metal ions within the simulated marine corrosion environments.

Keywords: Electrochemical sensing; boron-doped diamond; marine corrosion monitoring; differential pulse voltammetry