Effects of eutectic modifier and high-pressure torsion processing on microstructure and corrosion resistance of hypoeutectic Al-7Si alloy

Mengyan Nie1*, Xue Wang2,3, Chuan Ting Wang4, Shun Cai Wang1, Nong Gao2

1 National Centre for Advanced Tribology at Southampton (nCATS), Engineering Sciences, Faculty of Engineering and the Environment, University of Southampton, Southampton, SO17 1BJ, UK

2 Materials Research Group, Engineering Sciences, Faculty of Engineering and the Environment, University of Southampton, Southampton, SO17 1BJ, UK

3 School of Materials Science and Engineering, Hefei University of Technology, Hefei, 230009, China

4 School of Mechanical Engineering, Nanjing University of Science & Technology, Nanjing, 210094, China

*Author to whom correspondence should be addressed; E-mail: m.nie@soton.ac.uk; Tel: +44-23-80593761; Fax: +44-23-80593061

Abstract

High-pressure torsion (HPT) has recently been proven as an effective technique to produce bulk ultrafine-grained materials.  Both strontium-modified and unmodified Al-7Si alloys were processed by HPT under an applied pressure of 6.0 GPa for different numbers of torsional revolutions and then exposed to a 3.5 wt.% NaCl solution for open-circuit potential measurements followed by electrochemical impedance spectroscopy and potentiodynamic polarization curve tests.  The results exhibit that corrosion resistance of both Al-7Si and Al-7Si-Sr alloys in NaCl solution is enhanced upon high torsion strains of HPT processing compared with that of the as-received sample, but the improvement in corrosion resistance for Al-7Si alloy is more significantly than the Sr-modified alloy, which is possibly due to the increased HPT-induced active sites, the homogenous microstructure and the breakage of brittle coarse silicon particles and intermetallic phases demonstrated by microstructure and microhardness measurements. The corroded samples were further characterized with scanning electron microscopy and energy dispersive X-ray spectroscopy to examine the effect of grain refinement on corrosion mechanism of the Al-7Si alloy.

Keywords: Al-7Si alloys, high-pressure torsion, grain refinement, corrosion resistance, microstructure, electrochemical impedance spectroscopy