Photon tunneling into a single-mode planar silicon waveguide

Liping Fang,1,* Kian S Kiang,2 Nicholas P Alderman,3 Lefteris Danos,4 and Tom Markvart1

1Solar Energy Laboratory, University of Southampton, Southampton SO17 IBJ, UK.

2Electronics and Computer Sciences, University of Southampton, Southampton SO17 IBJ, UK.

3Department of Chemistry, University of Ottawa, Ottawa K1N 6N5, Canada.

4Department of Chemistry, University of Lancaster, Lancaster LA1 4YB, UK.

*liping.fang@outlook.com

Abstract: We demonstrate the direct excitation of a single TE mode in 25 nm thick planar crystalline silicon waveguide by photon tunneling from a layer of fluorescent dye molecules deposited by the Langmuir-Blodgett technique. The observed photon tunneling rate as a function of the dye-silicon separation is well fitted by a theoretical tunneling rate, which is obtained via a novel approach within the framework of quantum mechanics. We suggest that future ultrathin crystalline silicon solar cells can be made efficient by simple light trapping structures consisting of molecules on silicon.

(2015 Optical Society of America

OCIS codes: (240.7040) Tunneling; (260.2510) Fluorescence; (350.6050) Solar energy.

References and links

E. Yablonovitch, "Statistical ray optics," J. Opt. Soc. Am. 72(7), 899-907 (1982).

T. Markvart, and L. Castañer, Practical Handbook of Photovoltaics: Fundamentals and Applications (Elsevier, 2003).

H. R. Stuart, and D. G. Hall, "Thermodynamic limit to light trapping in thin planar structures," J. Opt. Soc. Am. A 14(11), 3001-3008 (1997).

T. Gao, E. Stevens, J. K. Lee, and P. W. Leu, "Designing metal hemispheres on silicon ultrathin film solar cells for plasmonic light trapping," Opt. Lett. 39(16), 4647-4650 (2014).

S. Zhu, A. W. Yu, D. Hawley, and R. Roy, "Frustrated total internal reflection: A demonstration and review," Am. J. Phys. 54(7), 601-607 (1986).

J. C. Bose, "On the influence of the thickness of air-space on total reflection of electric radiation," Proc. R. Soc. Lond. 62(379-387), 300-310 (1897).

R. Y. Chiao, P. G. Kwiat, and A. M. Steinberg, "Analogies between electron and photon tunneling: A proposed experiment to measure photon tunneling times," Physica B 175(1-3), 257-262 (1991).

H. B. Callen, Thermodynamics and An Introduction to Thermostatistics (Wiley, 1985).

R. R. Chance, A. Prock, and R. Silbey, “Molecular fluorescence and energy transfer near interfaces,” Adv. Chem. Phys. 37, 1–65 (1978).

H. Kuhn, D. Möbius, and H. Bücher, "Spectroscopy of Monolayer Assemblies," in Techniques of Chemistry, A. Weissberger, and B. W. Rossiter, eds. (Wiley, 1972), Chap. VII.

K. H. Drexhage, ‘‘Interaction of light with monomolecular dye layers,’’ in Progress in Optics, E. Wolf, ed. (NorthHolland, 1974), Vol. 12, Chap. 4.

L. Danos, R. Greef, and T. Markvart, "Efficient fluorescence quenching near crystalline silicon from Langmuir-Blodgett dye films," Thin Solid Films 516(20), 7251-7255 (2008).

L. Danos, and T. Markvart, "Excitation energy transfer rate from Langmuir Blodgett (LB) dye monolayers to silicon: Effect of aggregate formation," Chem. Phys. Lett. 490(4-6), 194-199 (2010).

L.Fang, N. Alderman, L. Danos, and T. Markvart, “Silicon sensitization using light harvesting layers,” Mater.  Res. Innov. 18(7), 494-499 (2014).

1. Introduction

Effective capture of sunlight by semiconductors - particularly silicon - represents one of the great challenges to photovoltaics today. Statistical light trapping techniques based on surface texturing [1] are now commonplace in commercial solar cells (see, for example, [2]). A detailed balance treatment of light trapping in thin films was given in [3] showing that significant enhancements in absorption are possible even when the thin film acceptor only supports a limited number of waveguide modes. Other techniques involve photoexcitation enhancement by exploiting the interaction of a semiconductor with a dipole near the surface. Much work is currently under way to implement such techniques with the use of plasmonics (see, for example, [4]).

Fig. 1. (a) Quantum tunneling through a potential barrier (b) Photon tunneling through an air gap between two prisms (c) Photon tunneling into thin silicon film.

In this paper we report efficient injection of photons directly into a single mode of a thin silicon waveguide via the interaction of molecules on the surface with the evanescent field. Due to the similarity with frustrated total internal reflection [5] (observed more than a century ago [6]) we have termed this effect photon tunneling, through the potential barrier which confines photons inside the high refractive index material by total internal reflection (Fig. 1) (see also [7]). In our system, we have simply replaced the exciting prism by fluorescent molecules.

2. Calculation of photon tunneling rate

The tunneling rate for photons emitted by the molecular dipole into a waveguide mode can be conveniently determined theoretically by the application of the Golden Rule:

(1)

where  is the reduced Planck’s constant,  and  are the wavenumber components in the  and  directions,  is the transition dipole moment,  is the electric field of the trapped mode labelled by the collection of quantum numbers , and normalized by:

(2)

where  is the permittivity of vacuum,  is the relative permittivity (a function of the  coordinate perpendicular to the waveguide) and  the frequency. The summation in Eq. (1) is carried out over the manifold of trapped modes related by cylindrical symmetry, on a shell defined by the characteristic equation for the waveguide mode:

(3)

where  is the “round trip” phase shift of the trapped wave,  is the waveguide thickness,  is the phase shift on reflection from the interface between media 1 and 2, and  is an integer. Here we have assumed, for simplicity, that the waveguide is symmetric.

Replacing the summation in Eq. (1) by an integral and transforming to polar coordinates  gives:

(4)

where ,  is the angle between  and ,  is the mode area, we inserted the density of states  in the  plane, and defined the orientation averaging factor:

(5)

where  is the angle between  and  and  denotes an element of the solid angle. The factor  in Eq. (4) can be taken outside the integral and bearing in mind that the integration is carried out on the shell of , the remaining integral (which effectively gives the density of states of the trapped mode) can be evaluated by standard rules for the delta function:

(6)

Equation (6) represents the main result for the tunneling rate into the trapped mode. In practical calculations it may be simpler to evaluate the partial derivative with the use of Euler’s cyclic relation (see, for example, [8]):

(7)

giving for the photon tunneling rate in Eq. (4):

(8)

where  is the spontaneous emission rate of a dipole in a homogeneous space with refractive index : , ,  is the speed of light, , , and  is the dipole-waveguide separation.

The analytical expression shown in Eq. (8) can also be obtained by complex variable analysis of the pure classical theory developed by Chance, Prock and Silbey (CPS) [9] in the complex wavenumber plane: the rate of photon tunneling to a waveguide mode can be calculated analytically from the contribution of the related pole (of the Fresnel reflection coefficients) to the integral in the CPS model.

3. Experiments for demonstation of photon tunneling

Photon tunneling can also be demonstrated experimentally by revisiting the early investigations of energy transfer between molecules and metal by Kuhn [10], Drexhage [11] and colleagues. The comprehensive classical theory developed by CPS can be used to fit the experimental results for the fluorescence lifetime of the Eu3+ ions doped in Langmuir-Blodgett (LB) monolayer at different distance to the surface of gold, silver and copper obtained by Drexhage.

In our experiments we have deposited different thicknesses of LB film onto a 25 nm (±5 nm) crystalline silicon layer (fabricated by a series of wet oxidation and HF etching cycles of a silicon-on-insulator wafer with buried oxide thickness of 1000 nm); the last LB bilayer is doped with a carbocyanine dye (1,1'-Dioctadecyl-3,3,3',3'-Tetramethylindocarbocyanine perchlorate). Dye-silicon separations were known to be controlled accurately by the LB technique, as confirmed also by ellipsometry measurements. The fluorescence lifetime of the dye as a function of distance from silicon was measured by time-resolved fluorescence.

For reference, we have also done similar experiments on glass, bulk silicon and copper (sputtered on silicon wafers) substrates. More detailed experimental procedures could be found in our previous publications [12-14], and we only show the results here.

4. Results and discussion

Figure 2 shows the measured fluorescence lifetime results (shown by symbols, and has been normalized to the lifetime measured from a glass substrate reference sample = 2.1±0.1 ns) and the related modelling results (shown by curves) by CPS for a horizontal electric dipole; an orientation established from a number of previous results [12-14]. It is seen from Fig. 2 that the modeling results fit well with the measured results.

Fig. 2. Fluorescence lifetime versus distance to related substrate.

The classical CPS model is comprehensive, but it hides the key physical process of fluorescence near thin silicon films such as photon tunneling. We demonstrate this process by the comparison of the observed and modeled photon tunneling rates in Fig. 3. The observed photon tunneling rate (yellow dots in Fig. 3) was obtained by subtracting the emission rate into the classically allowed photon states (which can be obtained simply by accounting interference of the source wave of the molecular dipole and its reflected wave from the interface [10] , shown by dashed blue curve in Fig. 3) from the measured total damping rate (inverse fluorescence lifetime), while the modeled photon tunneling rate (solid red curve in Fig. 3) was calculated from Eq. (8). Here we set  since, in the case of a horizontal electric dipole, both  and  lie in the  plane. It is seen from Fig. 3 that the modeled results show good agreement with the measured results.

Fig. 3. Comparison of observed and modeled photon tunneling rates.

5. Conclusion

In this paper we have demonstrated that fluorescent molecules can couple incident light into the underlying thin silicon film as trapped modes via photon tunneling. This can be perceived as the first step towards the fabrication of efficient ultrathin crystalline silicon solar cells, made possible by simple light trapping structures consisting of molecules on silicon.

Acknowledgements

This work has been funded by the UK EPSRC SUPERGEN program “Photovoltaic materials for the 21st century” (Reference: EP/F029624/1 and EP/F029624/2). Liping Fang thanks for financial support from the Faculty of Engineering and the Environment, University of Southampton and China Scholarship Council.