## Slide 1
Packaged silica and chalcogenide microspheres and their applications for telecommunications
Pengfei Wang*1,2, Ming Ding3, Ganapathy Senthil Murugan2, Timothy Lee2, Dan Hewak2, Gerald Farrell1 and Gilberto Brambilla2
1Photonics Research Centre, Dublin Institute of Technology, Kevin Street, Dublin, Ireland
2Optoelectronics Research Centre, University of Southampton, Southampton SO17 1BJ, United Kingdom
3School of Instrumentation Science and Opto-electronics, Beihang University, Beijing China
Photonics Research Centre
School of Electrical and Electronics Engineering
Dublin Institute of Technology, Ireland
*Email: pengfei.wang@dit.ie & p.wang@soton.ac.uk
@ T H E D U B L I N I N S T I T U T E O F T E C H N O L O G Y
www.prc.dit.ie
Objective
To investigate, both theoretically and experimentally, packaged silica and chalcogenide microsphere and their potential applications in telecommunication.
Silica and soft glass microspheres fabricated to date
Conclusion
A compact packaged silica microsphere based add-drop filter with a Q-factor of 0.9 X 105 has been presented .
The transmission spectral responses of the add and drop channels demonstrate the add–drop potential of the filter for very closely spaced DWDM channels.
The photosensitivity of the packaged chalcogenide microsphere device with a Q-factor of 1.8 X 105 to a 405 nm laser radiation has been presented.
These two packaged devices are promising candidates for ideal photonic building-blocks for several telecommunication applications including add-drop filters, highly integrated optical switches, modulators, ultra small optical tunable filters and integrated microlasers.
Simulated electric field distribution for a silica microsphere coupled with two tapered fibers in air and polymer
Fabrication process
Output spectra from the through
and the drop ports
Temperature dependence
~15.1 pm/oC
Packaged chalcogenide microsphere
Transmission spectra over the wavelength ranges 1540-1560 nm
Peak shift as a function of exposure time
ONNA 2015
Packaged silica microsphere
Packaged chalcogenide microsphere
Tapered fibre