# Appendix  D

# Comparison of GHG emission factor data from the literature

An overview of material recycling GHG emission factors reported in the literature is presented in Table D1.

Table D1

Overview of material recycling GHG emissions literature data.

| Waste material group | Waste material type | Reference | Geographic coverage | Reference year | Substituted production | GHG emissions (net) kg CO2-eq. |
| --- | --- | --- | --- | --- | --- | --- |
| Glass | Green glass | Pratt (2014) | Scotland | 2012 | 56% primary glass; 44% primary aggregates | -201 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -392 |
|  |  | Larsen et al. (2009) | Northern Europe | 2009 | Primary glass | -506 to -445 |
|  |  | Fisher (2006) | UK | 2006 | Primary glass | -762 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary glass | -253 |
|  |  | US EPA (2015) | USA | 2015 | Primary glass | -309 |
|  | Brown glass | Pratt (2014) | Scotland | 2012 | 56% primary glass; 44% primary aggregates | -201 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -392 |
|  |  | Larsen et al. (2009) | Northern Europe | 2009 | Primary glass | -506 to -445 |
|  |  | Fisher (2006) | UK | 2006 | Primary glass | -762 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary glass | -253 |
|  |  | US EPA (2015) | USA | 2015 | Primary glass | -309 |
|  | Clear glass | Pratt (2014) | Scotland | 2012 | 56% primary glass; 44% primary aggregates | -201 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -392 |
|  |  | Larsen et al. (2009) | Northern Europe | 2009 | Primary glass | -506 to -445 |
|  |  | Fisher (2006) | UK | 2006 | Primary glass | -762 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary glass | -253 |
|  |  | US EPA (2015) | USA | 2015 | Primary glass | -309 |
|  | Mixed glass | Pratt (2014) | Scotland | 2012 | 56% primary glass; 44% primary aggregates | -201 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -233 |
|  |  | Larsen et al. (2009) | Northern Europe | 2009 | Primary glass | -506 to -445 |
|  |  | Fisher (2006) | UK | 2006 | Primary glass | -762 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary glass | -253 |
|  |  | US EPA (2015) | USA | 2015 | Primary glass | -309 |
| Paper & card | Paper | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary paper and card | -888 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -811 |
|  |  | Merrild et al. (2009) | Northern Europe | 2009 | Virgin paper | -1269 to 390 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin paper | -620 to -280 |
|  |  | Fisher (2006) | UK | 2006 | Virgin thermo-mechanical pulp | -496 |
|  |  | Smith et al. (2001) | Europe | 2001 | Virgin newsprint | -600 |
|  |  | US EPA (2015) | USA | 2015 | Virgin newspaper | -3031 |
|  |  | US EPA (2015) | USA | 2015 | Virgin office paper | -3153 |
|  |  | US EPA (2015) | USA | 2015 | 48% virgin fibre corrugated containers; 8% primary magazines, 24% primary newspaper; 20% primary office paper | -3891 |
|  | Card | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary paper and card | -888 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin paper | -620 to -280 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -894 |
|  |  | Fisher (2006) | UK | 2006 | Virgin thermo-mechanical pulp | -496 |
|  |  | US EPA (2015) | USA | 2015 | Virgin corrugated containers | -3439 |
|  | Books | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary paper and card | -888 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -811 |
|  |  | US EPA (2015) | USA | 2015 | Virgin fibre textbooks | -3428 |
|  | Mixed paper & card | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary paper and card | -888 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -873 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin paper | -620 to -280 |
|  |  | Fisher (2006) | UK | 2006 | Virgin thermo-mechanical pulp | -496 |
|  | Yellow pages | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary paper and card | -888 |
|  |  | US EPA (2015) | USA | 2015 | Virgin fibre phone books | -2910 |
| Metal | Steel cans | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary ferrous metals | -1806 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1799 |
|  |  | Damgaard et al. (2009) | Northern Europe | 2009 | Primary steel | -2360 to -560 |
|  |  | Fisher et al. (2006) | UK | 2006 | Pig iron (max) Primary steel (min) | -830 to -580 |
|  |  | Fisher (2006) | UK | 2006 | Pig iron | -496 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary tin plate | -1487 |
|  |  | US EPA (2015) | USA | 2015 | Primary steel | -1995 |
|  | Aluminium cans | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary non-ferrous metals | -9985 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -9267 |
|  |  | Damgaard et al. (2009) | Northern Europe | 2009 | Primary aluminium | -19340 to -5040 |
|  |  | Fisher et al. (2006) | UK | 2006 | Primary aluminium | -13100 to -12300 |
|  |  | Fisher (2006) | UK | 2006 | Primary aluminium | -11634 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary aluminium | -9074 |
|  |  | US EPA (2015) | USA | 2015 | Primary aluminium | -10042 |
|  | Mixed cans | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary ferrous and non-ferrous metals | -2573 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -3965 |
|  |  | US EPA (2015) | USA | 2015 | Primary steel and aluminium (unknown proportion) | -4828 |
|  | Other scrap metal | Pratt (2014) | Scotland | 2012 | Unknown – assumed primary ferrous and non-ferrous metals | -2573 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -2239 |
|  |  | US EPA (2015) | USA | 2015 | Primary steel and aluminium (unknown proportion) | -4828 |
|  | Aluminium foil | WRAP (2012) | England | 2011 | Unknown | -9267 |
| Plastic | Mixed plastics | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1215 |
|  |  | Astrup et al. (2009) | Northern Europe | 2009 | Virgin plastic | -1574 to -838 |
|  |  | Astrup et al. (2009) | Northern Europe | 2009 | Virgin wood lumber | -108 to -58 |
|  |  | Fisher et al. (2006) | UK | 2006 | Primary PET (max) Primary plastic (LDPE) lumber (min) | -1820 to 1470 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  |  | US EPA (2015) | USA | 2015 | Primary HDPE (35%) and PET (65%) | -1135 |
|  | Mixed plastic bottles | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1156 |
|  |  | Fisher et al. (2006) | UK | 2006 | Primary PET (max) Primary Plastic (LDPE) lumber (min) | -1820 to 1470 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  |  | US EPA (2015) | USA | 2015 | Primary HDPE (35%) and PET (65%) | -1135 |
|  | PET | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1705 |
|  |  | Fisher et al. (2006) | UK | 2006 | Primary PET | -1820 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary PET granules | -1761 |
|  |  | US EPA (2015) | USA | 2015 | Primary PET | -1246 |
|  | HDPE | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1161 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary HDPE granules | -253 |
|  |  | US EPA (2015) | USA | 2015 | Primary HDPE | -970 |
|  | PVC | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -888 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  | LDPE | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -948 |
|  |  | Fisher et al. (2006) | UK | 2006 | Primary LDPE (max) Virgin timber (min) | -1470 to 850 |
|  |  | Fisher (2006) | UK | 2006 | Primary polyethylene | -1586 |
|  | PP | Pratt (2014) | Scotland | 2012 | Unknown | -566 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -948 |
|  |  | Fisher (2006) | UK | 2006 | Primary PET | -2324 |
|  | PS | WRAP (2012) | England | 2011 | Unknown | -1240 |
|  | Other plastics | WRAP (2012) | England | 2011 | Unknown | -688 |
| Wood | Wood | Pratt (2014) | Scotland | 2012 | N, P, and K fertilisers (unknown proportions) | -265 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1276 |
|  |  | Merrild and Christensen (2009) | Northern Europe | 2009 | Virgin wood chips | -665 to -125 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin timber | -90 to 1.2 |
|  |  | US EPA (2015) | USA | 2015 | Virgin timber | -2712 |
|  | Chipboard & MDF | Pratt (2014) | Scotland | 2012 | N, P, and K fertilisers (unknown proportions) | -265 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1276 |
|  |  | Merrild and Christensen (2009) | Northern Europe | 2009 | Virgin wood chips | -665 to -125 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin timber | -90 to 1.2 |
|  |  | US EPA (2015) | USA | 2015 | Virgin MDF | -2723 |
|  | Composite wood materials | Pratt (2014) | Scotland | 2012 | N, P, and K fertilisers (unknown proportions) | -265 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1276 |
|  |  | Merrild and Christensen (2009) | Northern Europe | 2009 | Virgin wood chips | -665 to -125 |
|  |  | Fisher et al. (2006) | UK | 2006 | Virgin timber | -90 to 1.2 |
| WEEE | WEEE – LDAs | Pratt (2014) | Scotland | 2012 | Primary ferrous and non-ferrous metals (unknown proportions) | -181 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -1266 |
|  | WEEE – SDAs | WRAP (2012) | England | 2011 | Unknown | -1482 |
|  | WEEE – CRTs | US EPA (2015) | USA | 2015 | Primary asphalt (38%), steel sheet (27%, lead bullion (10%), CRT glass (2%), copper wire (5%), and aluminium sheet (18%) | -2767 |
|  | WEEE – fridges & freezers | Pratt (2014) | Scotland | 2012 | Primary ferrous and non-ferrous metals (unknown proportions) | -181 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -656 |
|  |  | Smith et al. (2001) | Europe | 2001 | Primary tin plate; primary aluminium, primary copper; marginal heat and electricity (plastics incineration) (unknown proportions) | -1042 |
| Batteries | Automotive batteries | Pratt (2014) | Scotland | 2012 | Unknown | -487 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -563 |
|  | Post-consumer, non-automotive batteries | Pratt (2014) | Scotland | 2012 | Unknown | -487 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -563 |
| Tyres | Car tyres | WRAP (2012) | England | 2011 | Unknown | -1910 |
|  |  | US EPA (2015) | USA | 2015 | Sand (42%) and synthetic rubber (58%) | -430 |
|  | Van tyres | WRAP (2012) | England | 2011 | Unknown | -1910 |
|  |  | US EPA (2015) | USA | 2015 | Sand (42%) and synthetic rubber (58%) | -430 |
|  | Large vehicle tyres | WRAP (2012) | England | 2011 | Unknown | -1910 |
|  |  | US EPA (2015) | USA | 2015 | Sand (42%) and synthetic rubber (58%) | -430 |
|  | Mixed tyres | WRAP (2012) | England | 2011 | Unknown | -1910 |
|  |  | US EPA (2015) | USA | 2015 | Sand (42%) and synthetic rubber (58%) | -430 |
| Furniture | Furniture | WRAP (2012) | England | 2011 | Unknown | -921 |
| Rubble | Rubble | Pratt (2014) | Scotland | 2012 | Unknown | 2 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -9 |
|  |  | Fisher et al. (2006) | UK | 2006 | Gravel (max) No substitution (min) | -2.3 to 2.1 |
|  |  | Fisher (2006) | UK | 2006 | Gravel | -2.7 |
| Soil | Soil | Pratt (2014) | Scotland | 2012 | Unknown | 1 |
|  |  | Fisher et al. (2006) | UK | 2006 | Gravel (max) No substitution (min) | -2.3 to 2.1 |
| Plasterboard | Plasterboard | WRAP (2012) | England | 2011 | Unknown | -139 |
|  |  | US EPA (2015) | USA | 2015 | Virgin gypsum drywall | 33 |
| Oil | Vegetable oil | Pratt (2014) | Scotland | 2012 | Unknown | -725 |
|  | Mineral oil | Pratt (2014) | Scotland | 2012 | Unknown | -725 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -725 |
| Composite | Composite food & beverage cartons | WRAP (2012) | England | 2011 | Unknown | -1730 |
| Mattresses | Mattresses |  |  |  |  |  |
| Paint | Paint | WRAP (2012) | England | 2011 | Unknown | -2840 |
| Textiles | Textiles & footwear | Pratt (2014) | Scotland | 2012 | 46% primary textiles; 32% virgin paper; 22% primary shoes | -5891 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -2028 |
|  |  | Fisher et al. (2006) | UK | 2006 | 50% cotton cloth; 50% primary PET (max) Kraft paper (min) | -1750 to -930 |
|  |  | Fisher (2006) | UK | 2006 | 50% cotton cloth; 50% primary PET | -7869 |
|  |  | Smith et al. (2001) | Europe | 2001 | Woollen rags | -3169 |
|  | Textiles only | Pratt (2014) | Scotland | 2012 | 46% primary textiles; 32% virgin paper; 22% primary shoes | -5891 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -5987 |
|  |  | Fisher et al. (2006) | UK | 2006 | 50% cotton cloth; 50% primary PET (max) Kraft paper (min) | -1750 to -930 |
|  |  | Fisher (2006) | UK | 2006 | 50% cotton cloth; 50% primary PET | -7869 |
|  |  | Smith et al. (2001) | Europe | 2001 | Woollen rags | -3169 |
|  | Footwear only | Pratt (2014) | Scotland | 2012 | 46% primary textiles; 32% virgin paper; 22% primary shoes | -5891 |
|  |  | WRAP (2012) | England | 2011 | Unknown | -4385 |
|  | Carpets | US EPA (2015) | USA | 2015 | Primary Nylon 6, Nylon 6-6, PET, and PP plastic resins | -2601 |

GHG, greenhouse gas; PET, polyethylene terephthalate; LDPE, low-density polyethylene; HDPE, high-density polyethylene; PVC, polyvinyl chloride; PP, polypropylene; PS, polystyrene; MDF, medium-density fibreboard; WEEE, waste electrical and electronic equipment; LDA, large domestic appliance; SDA, small domestic appliance; CRT, cathode ray tube

## References

Astrup, T., Fruergaard, T. and Christensen, T.H. (2009) Recycling of plastic: Accounting of greenhouse gases and global warming contributions. Waste Management & Research, 27 (8), 763-772.

Damgaard, A., Larsen, A.W. and Christensen, T.H. (2009) Recycling of metals: Accounting of greenhouse gases and global warming contributions. Waste Management & Research, 27 (8), 773-780.

Fisher, J.I. (2006) Impact of Energy from Waste and Recycling Policy on UK Greenhouse Gas Emissions. London, UK: Department for Environment, Food & Rural Affairs.

Fisher, K., Collins, M., Aumônier, S. and Gregory, B. (2006) Carbon balances and energy impacts of the management of UK wastes. London, UK: Department for Environment, Food & Rural Affairs.

Larsen, A.W., Merrild, H. and Christensen, T.H. (2009) Recycling of glass: Accounting of greenhouse gases and global warming contributions. Waste Management & Research, 27 (8), 754-762.

Merrild, H. and Christensen, T.H. (2009) Recycling of wood for particle board production: Accounting of greenhouse gases and global warming contributions. Waste Management & Research, 27 (8), 781-788.

Merrild, H., Damgaard, A. and Christensen, T.H. (2009) Recycling of paper: Accounting of greenhouse gases and global warming contributions. Waste Management & Research, 27 (8), 746-753.

Pratt, K. (2014) The Scottish carbon metric. A national carbon indicator for waste. 2012 updates to the Carbon Metric Technical Report. Stirling, UK: Zero Waste Scotland.

Smith, A., Brown, K., Ogilvie, S., Rushton, K. and Bates, J. (2001) Waste management options and climate change. Final report to the European Commission, DG Environment. Luxembourg: European Commission.

US EPA (2015) WARM Version 13. Recycling. Washington, DC, USA: United States Environmental Protection Agency.

Waste & Resource Action Programme (WRAP) (2012) England carbon metric report - detailed breakdown. London, UK: Department for Environment, Food & Rural Affairs.