# Appendix E

Perturbation analysis – detailed results

Detailed results of the perturbation analysis undertaken to test the sensitivity of calculated results to the market substitution ratio parameter are presented in Table E1.

Table E1

Market substitution parameter sensitivity ratios (SR) of the material recycling systems investigated – detailed results.

| Material type | Secondary material | Avoided primary material | Initial market substitution rate | Initial result | Parameter contribution | Test market substitution rate | ∆Parameter | Test result | Test parameter contribution | ∆Result | SR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | kg CO2-eq. | kg CO2-eq. |  |  | kg CO2-eq. | kg CO2-eq. | kg CO2-eq. |  |
| Green glass | Glass | Glass | 1 | -314 | -709 | 0.9 | 0.10 | -243 | -638 | 71 | -2.26 |
| Brown glass | Glass | Glass | 1 | -314 | -709 | 0.9 | 0.10 | -243 | -638 | 71 | -2.26 |
| Clear glass | Glass | Glass | 1 | -314 | -709 | 0.9 | 0.10 | -243 | -638 | 71 | -2.26 |
| Mixed glass | Glass | Glass | 1 | -314 | -709 | 0.9 | 0.10 | -243 | -638 | 71 | -2.26 |
| Paper | Newsprint | Newsprint | 1 | -459 | -2033 | 0.9 | 0.10 | -255 | -1830 | 203 | -4.43 |
| Card | Testliner | Kraftliner | 1 | -120 | -320 | 0.9 | 0.10 | -88 | -288 | 32 | -2.66 |
|  | Wellenstoff | SCF | 1 | -120 | -358 | 0.9 | 0.10 | -85 | -322 | 36 | -2.97 |
|  | Total avoided production |  | 1 | -120 | -678 | 0.9 | 0.10 | -53 | -610 | 68 | -5.63 |
| Books | Testliner | Kraftliner | 1 | -117 | -320 | 0.9 | 0.10 | -85 | -288 | 32 | -2.72 |
|  | Wellenstoff | SCF | 1 | -117 | -358 | 0.9 | 0.10 | -82 | -322 | 36 | -3.04 |
|  | Total avoided production |  | 1 | -117 | -678 | 0.9 | 0.10 | -50 | -610 | 68 | -5.77 |
| Mixed paper & card | Testliner | Kraftliner | 1 | -123 | -320 | 0.9 | 0.10 | -91 | -288 | 32 | -2.61 |
|  | Wellenstoff | SCF | 1 | -123 | -358 | 0.9 | 0.10 | -87 | -322 | 36 | -2.92 |
|  | Total avoided production |  | 1 | -123 | -678 | 0.9 | 0.10 | -55 | -610 | 68 | -5.52 |
| Yellow Pages | Testliner | Kraftliner | 1 | -117 | -320 | 0.9 | 0.10 | -85 | -288 | 32 | -2.72 |
|  | Wellenstoff | SCF | 1 | -117 | -358 | 0.9 | 0.10 | -82 | -322 | 36 | -3.04 |
|  | Total avoided production |  | 1 | -117 | -678 | 0.9 | 0.10 | -50 | -610 | 68 | -5.77 |
| Steel cans | Steel | Steel | 1 | -862 | -1391 | 0.9 | 0.10 | -723 | -1252 | 139 | -1.61 |
| Aluminium cans | Aluminium | Aluminium | 1 | -8143 | -9256 | 0.9 | 0.10 | -7218 | -8330 | 926 | -1.14 |
| Mixed cans | Steel | Steel | 1 | -3577 | -766 | 0.9 | 0.10 | -3500 | -690 | 77 | -0.21 |
|  | Aluminium | Aluminium | 1 | -3577 | -3693 | 0.9 | 0.10 | -3208 | -3324 | 369 | -1.03 |
|  | Total avoided production |  | 1 | -3577 | -4460 | 0.9 | 0.10 | -3131 | -4014 | 446 | -1.25 |
| Other scrap metal | Steel | Steel | 1 | -3577 | -766 | 0.9 | 0.10 | -3500 | -690 | 77 | -0.21 |
|  | Aluminium | Aluminium | 1 | -3577 | -3693 | 0.9 | 0.10 | -3208 | -3324 | 369 | -1.03 |
|  | Total avoided production |  | 1 | -3577 | -4460 | 0.9 | 0.10 | -3131 | -4014 | 446 | -1.25 |
| Aluminium foil | Aluminium | Aluminium | 1 | -8143 | -9256 | 0.9 | 0.10 | -7218 | -8330 | 926 | -1.14 |
| Aerosols | Steel | Steel | 1 | -3577 | -766 | 0.9 | 0.10 | -3500 | -690 | 77 | -0.21 |
|  | Aluminium | Aluminium | 1 | -3577 | -3693 | 0.9 | 0.10 | -3208 | -3324 | 369 | -1.03 |
|  | Total avoided production |  | 1 | -3577 | -4460 | 0.9 | 0.10 | -3131 | -4014 | 446 | -1.25 |
| Fire extinguishers | Steel | Steel | 1 | -673 | -1324 | 0.9 | 0.10 | -541 | -1192 | 132 | -1.97 |
| Gas bottles | Steel | Steel | 1 | -673 | -1324 | 0.9 | 0.10 | -541 | -1192 | 132 | -1.97 |
| Bicycles | Steel | Steel | 1 | -3577 | -766 | 0.9 | 0.10 | -3500 | -690 | 77 | -0.21 |
|  | Aluminium | Aluminium | 1 | -3577 | -3693 | 0.9 | 0.10 | -3208 | -3324 | 369 | -1.03 |
|  | Total avoided production |  | 1 | -3577 | -4460 | 0.9 | 0.10 | -3131 | -4014 | 446 | -1.25 |
| Mixed plastics | HDPE | HDPE | 1 | -1024 | -339 | 0.9 | 0.10 | -990 | -305 | 34 | -0.33 |
|  | PVC | PVC | 1 | -1024 | -62 | 0.9 | 0.10 | -1018 | -56 | 6 | -0.06 |
|  | PP | PP | 1 | -1024 | -114 | 0.9 | 0.10 | -1012 | -103 | 11 | -0.11 |
|  | Total avoided production |  | 1 | -1024 | -1363 | 0.9 | 0.10 | -888 | -1227 | 136 | -1.33 |
| Mixed plastic bottles | PET | PET | 1 | -1084 | -814 | 0.9 | 0.10 | -1003 | -732 | 81 | -0.75 |
|  | HDPE | HDPE | 1 | -1084 | -574 | 0.9 | 0.10 | -1027 | -516 | 57 | -0.53 |
|  | PVC | PVC | 1 | -1084 | -15 | 0.9 | 0.10 | -1083 | -13 | 1 | -0.01 |
|  | PP | PP | 1 | -1084 | -18 | 0.9 | 0.10 | -1083 | -16 | 2 | -0.02 |
|  | Total avoided production |  | 1 | -1084 | -1420 | 0.9 | 0.10 | -942 | -1278 | 142 | -1.31 |
| PET | PET | PET | 1 | -2192 | -2347 | 0.9 | 0.10 | -1957 | -2112 | 235 | -1.07 |
| HDPE | HDPE | HDPE | 1 | -1149 | -1528 | 0.9 | 0.10 | -996 | -1375 | 153 | -1.33 |
| PVC | PVC | PVC | 1 | -1549 | -1928 | 0.9 | 0.10 | -1356 | -1735 | 193 | -1.24 |
| LDPE | LDPE | LDPE | 1 | -972 | -1001 | 0.9 | 0.10 | -872 | -901 | 100 | -1.03 |
| PP | PP | PP | 1 | -1184 | -1563 | 0.9 | 0.10 | -1027 | -1407 | 156 | -1.32 |
| Wood | rMDF | vMDF | 1 | -351 | -981 | 0.9 | 0.10 | -253 | -883 | 98 | -2.79 |
| Chipboard and MDF | rMDF | vMDF | 1 | -351 | -981 | 0.9 | 0.10 | -253 | -883 | 98 | -2.79 |
| Composite wood materials | rMDF | vMDF | 1 | -177 | -785 | 0.9 | 0.10 | -98 | -706 | 78 | -4.44 |
| WEEE - large domestic appliances | Steel | Steel | 1 | -866 | -716 | 0.9 | 0.10 | -795 | -645 | 72 | -0.83 |
|  | Aluminium | Aluminium | 1 | -866 | -566 | 0.9 | 0.10 | -810 | -509 | 57 | -0.65 |
|  | PP | PP | 1 | -866 | -12 | 0.9 | 0.10 | -865 | -11 | 1 | -0.01 |
|  | Total avoided production |  | 1 | -866 | -1294 | 0.9 | 0.10 | -737 | -1165 | 129 | -1.49 |
| WEEE - small domestic appliances | Steel | Steel | 1 | -1350 | -542 | 0.9 | 0.10 | -1295 | -488 | 54 | -0.40 |
|  | Aluminium | Aluminium | 1 | -1350 | -1223 | 0.9 | 0.10 | -1227 | -1101 | 122 | -0.91 |
|  | PP | PP | 1 | -1350 | -34 | 0.9 | 0.10 | -1346 | -31 | 3 | -0.03 |
|  | Zinc (from batteries) | Zinc | 1 | -1350 | -7 | 0.9 | 0.10 | -1349 | -6 | 1 | -0.01 |
|  | Manganese (from batteries) | Manganese | 1 | -1350 | -3 | 0.9 | 0.10 | -1349 | -3 | 0 | 0.00 |
|  | Mercury (from batteries) | Mercury | 1 | -1350 | 0 | 0.9 | 0.10 | -1350 | 0 | 0 | 0.00 |
|  | Mercury (from batteries) | Ferromanganese | 1 | -1350 | -1 | 0.9 | 0.10 | -1349 | -1 | 0 | 0.00 |
|  | Steel (from batteries) | Steel | 1 | -1350 | -3 | 0.9 | 0.10 | -1349 | -2 | 0 | 0.00 |
|  | Total avoided production |  | 1 | -1350 | -1812 | 0.9 | 0.10 | -1168 | -1631 | 181 | -1.34 |
| WEEE - CRTs | Steel | Steel | 1 | -228 | -133 | 0.9 | 0.10 | -214 | -120 | 13 | -0.59 |
|  | Aluminium | Aluminium | 1 | -228 | -151 | 0.9 | 0.10 | -213 | -136 | 15 | -0.66 |
|  | Copper | Copper | 1 | -228 | -13 | 0.9 | 0.10 | -226 | -12 | 1 | -0.06 |
|  | Lead | Lead | 1 | -228 | -198 | 0.9 | 0.10 | -208 | -178 | 20 | -0.87 |
|  | Copper (from cables) | Copper | 1 | -228 | -3 | 0.9 | 0.10 | -227 | -2 | 0 | -0.01 |
|  | Total avoided production |  | 1 | -228 | -499 | 0.9 | 0.10 | -178 | -449 | 50 | -2.19 |
| WEEE - fluorescent tubes & other light bulbs | Steel | Steel | 1 | -779 | -33 | 0.9 | 0.10 | -776 | -30 | 3 | -0.04 |
|  | Aluminium | Aluminium | 1 | -779 | -518 | 0.9 | 0.10 | -728 | -467 | 52 | -0.66 |
|  | Glass | Glass | 1 | -779 | -745 | 0.9 | 0.10 | -705 | -671 | 75 | -0.96 |
|  | Total avoided production |  | 1 | -779 | -1297 | 0.9 | 0.10 | -650 | -1167 | 130 | -1.66 |
| WEEE - fridges & freezers | Steel | Steel | 1 | -853 | -851 | 0.9 | 0.10 | -768 | -766 | 85 | -1.00 |
|  | Aluminium | Aluminium | 1 | -853 | -459 | 0.9 | 0.10 | -807 | -413 | 46 | -0.54 |
|  | PP | PP | 1 | -853 | -13 | 0.9 | 0.10 | -852 | -11 | 1 | -0.01 |
|  | Total avoided production |  | 1 | -853 | -1322 | 0.9 | 0.10 | -721 | -1190 | 132 | -1.55 |
| Automotive batteries | Lead | Lead | 1 | -435 | -1373 | 0.9 | 0.10 | -298 | -1236 | 137 | -3.15 |
| Post-consumer, non-automotive batteries | Zinc | Zinc | 1 | -204 | -682 | 0.9 | 0.10 | -136 | -614 | 68 | -3.35 |
|  | Manganese | Manganese | 1 | -204 | -294 | 0.9 | 0.10 | -174 | -265 | 29 | -1.45 |
|  | Mercury | Mercury | 1 | -204 | -2 | 0.9 | 0.10 | -204 | -2 | 0 | -0.01 |
|  | Ferromanganese | Ferromanganese | 1 | -204 | -104 | 0.9 | 0.10 | -193 | -94 | 10 | -0.51 |
|  | Steel | Steel | 1 | -204 | -250 | 0.9 | 0.10 | -179 | -225 | 25 | -1.23 |
|  | Total avoided production |  | 1 | -204 | -1333 | 0.9 | 0.10 | -70 | -1199 | 133 | -6.54 |
| Car tyres | Steel | Steel | 1 | -636 | -213 | 0.9 | 0.10 | -614 | -192 | 21 | -0.33 |
|  | Rubber crumb | Synthetic rubber | 1 | -636 | -419 | 0.9 | 0.10 | -594 | -377 | 42 | -0.66 |
|  | Rubber granulate | Bitumen | 1 | -636 | -209 | 0.9 | 0.10 | -615 | -188 | 21 | -0.33 |
|  | Total avoided production |  | 1 | -636 | -841 | 0.9 | 0.10 | -551 | -757 | 84 | -1.32 |
| Van tyres | Steel | Steel | 1 | -671 | -188 | 0.9 | 0.10 | -653 | -169 | 19 | -0.28 |
|  | Rubber crumb | Synthetic rubber | 1 | -671 | -453 | 0.9 | 0.10 | -626 | -408 | 45 | -0.68 |
|  | Rubber granulate | Bitumen | 1 | -671 | -227 | 0.9 | 0.10 | -649 | -205 | 23 | -0.34 |
|  | Total avoided production |  | 1 | -671 | -868 | 0.9 | 0.10 | -584 | -782 | 87 | -1.29 |
| Large vehicle tyres | Steel | Steel | 1 | -671 | -188 | 0.9 | 0.10 | -653 | -169 | 19 | -0.28 |
|  | Rubber crumb | Synthetic rubber | 1 | -671 | -453 | 0.9 | 0.10 | -626 | -408 | 45 | -0.68 |
|  | Rubber granulate | Bitumen | 1 | -671 | -227 | 0.9 | 0.10 | -649 | -205 | 23 | -0.34 |
|  | Total avoided production |  | 1 | -671 | -868 | 0.9 | 0.10 | -584 | -782 | 87 | -1.29 |
| Mixed tyres | Steel | Steel | 1 | -640 | -210 | 0.9 | 0.10 | -619 | -189 | 21 | -0.33 |
|  | Rubber crumb | Synthetic rubber | 1 | -640 | -423 | 0.9 | 0.10 | -598 | -381 | 42 | -0.66 |
|  | Rubber granulate | Bitumen | 1 | -640 | -211 | 0.9 | 0.10 | -619 | -190 | 21 | -0.33 |
|  | Total avoided production |  | 1 | -640 | -845 | 0.9 | 0.10 | -555 | -760 | 84 | -1.32 |
| Furniture | rMDF | vMDF | 1 | -177 | -785 | 0.9 | 0.10 | -98 | -706 | 78 | -4.44 |
| Rubble | Aggregate | Gravel | 1 | -2 | -3 | 0.9 | 0.10 | -1 | -2 | 0 | -1.65 |
|  | Steel | Steel | 1 | -2 | -14 | 0.9 | 0.10 | 0 | -13 | 1 | -8.81 |
|  | Total avoided production |  | 1 | -2 | -17 | 0.9 | 0.10 | 0 | -15 | 2 | -10.45 |
| Soil | - | - | - | - | - | - | - | - | - | - | - |
| Plasterboard | Gypsum | Gypsum | 1 | 4 | -35 | 0.9 | 0.10 | 7 | -32 | 4 | 9.95 |
|  | Testliner | Kraftliner | 1 | 4 | -7 | 0.9 | 0.10 | 4 | -6 | 1 | 1.99 |
|  | Wellenstoff | SCF | 1 | 4 | -8 | 0.9 | 0.10 | 4 | -7 | 1 | 2.22 |
|  | Total avoided production |  | 1 | 4 | -50 | 0.9 | 0.10 | 9 | -45 | 5 | 14.16 |
| Vegetable oil | Biodiesel | Fossil diesel | 1 | -2759 | -3406 | 0.9 | 0.10 | -2418 | -3065 | 341 | -1.23 |
| Mineral oil | Biodiesel | Fossil diesel | 1 | -2759 | -3406 | 0.9 | 0.10 | -2418 | -3065 | 341 | -1.23 |
| Composite food & beverage cartons | Testliner | Kraftliner | 1 | -242 | -189 | 0.9 | 0.10 | -223 | -170 | 19 | -0.78 |
|  | Wellenstoff | SCF | 1 | -242 | -212 | 0.9 | 0.10 | -220 | -191 | 21 | -0.88 |
|  | HDPE | HDPE | 1 | -242 | -199 | 0.9 | 0.10 | -222 | -179 | 20 | -0.82 |
|  | Aluminium | Aluminium | 1 | -242 | -454 | 0.9 | 0.10 | -196 | -408 | 45 | -1.88 |
|  | Total avoided production |  | 1 | -242 | -1054 | 0.9 | 0.10 | -136 | -948 | 105 | -4.36 |
| Mattresses | Steel | Steel | 1 | -1241 | -661 | 0.9 | 0.10 | -1175 | -595 | 66 | -0.53 |
|  | Mattress filling fibre | PE foam | 1 | -1241 | -410 | 0.9 | 0.10 | -1200 | -369 | 41 | -0.33 |
|  | Synthetic cloths | Polyester cloths | 1 | -1241 | -551 | 0.9 | 0.10 | -1186 | -496 | 55 | -0.44 |
|  | Natural fibre cloths | Kraft paper | 1 | -1241 | -97 | 0.9 | 0.10 | -1231 | -87 | 10 | -0.08 |
|  | Total avoided production |  | 1 | -1241 | -1718 | 0.9 | 0.10 | -1069 | -1546 | 172 | -1.38 |
| Paint | Steel | Steel | 1 | 86 | -278 | 0.9 | 0.10 | 114 | -250 | 28 | 3.24 |
| Textiles & footwear | Mattress filling fibre | PE foam | 1 | -3376 | -1463 | 0.9 | 0.10 | -3230 | -1317 | 146 | -0.43 |
|  | Synthetic cloths | Polyester cloths | 1 | -3376 | -1969 | 0.9 | 0.10 | -3179 | -1772 | 197 | -0.58 |
|  | Natural fibre cloths | Kraft paper | 1 | -3376 | -345 | 0.9 | 0.10 | -3342 | -311 | 35 | -0.10 |
|  | Total avoided production |  | 1 | -3376 | -3777 | 0.9 | 0.10 | -2999 | -3399 | 378 | -1.12 |
| Textiles only | Mattress filling fibre | PE foam | 1 | -3376 | -1463 | 0.9 | 0.10 | -3230 | -1317 | 146 | -0.43 |
|  | Synthetic cloths | Polyester cloths | 1 | -3376 | -1969 | 0.9 | 0.10 | -3179 | -1772 | 197 | -0.58 |
|  | Natural fibre cloths | Kraft paper | 1 | -3376 | -345 | 0.9 | 0.10 | -3342 | -311 | 35 | -0.10 |
|  | Total avoided production |  | 1 | -3376 | -3777 | 0.9 | 0.10 | -2999 | -3399 | 378 | -1.12 |
| Footwear only | Mattress filling fibre | PE foam | 1 | -3376 | -1463 | 0.9 | 0.10 | -3230 | -1317 | 146 | -0.43 |
|  | Synthetic cloths | Polyester cloths | 1 | -3376 | -1969 | 0.9 | 0.10 | -3179 | -1772 | 197 | -0.58 |
|  | Natural fibre cloths | Kraft paper | 1 | -3376 | -345 | 0.9 | 0.10 | -3342 | -311 | 35 | -0.10 |
|  | Total avoided production |  | 1 | -3376 | -3777 | 0.9 | 0.10 | -2999 | -3399 | 378 | -1.12 |
| Carpets | PP | PP | 1 | -9 | -152 | 0.9 | 0.10 | 6 | -137 | 15 | -17.15 |
| AHPs | Testliner | Kraftliner | 1 | 14 | -13 | 0.9 | 0.10 | 15 | -11 | 1 | 0.93 |
|  | Wellenstoff | SCF | 1 | 14 | -14 | 0.9 | 0.10 | 15 | -13 | 1 | 1.04 |
|  | PET | PET | 1 | 14 | -9 | 0.9 | 0.10 | 14 | -8 | 1 | 0.65 |
|  | PP | PP | 1 | 14 | -14 | 0.9 | 0.10 | 15 | -13 | 1 | 1.06 |
|  | Total avoided production |  | 1 | 14 | -50 | 0.9 | 0.10 | 19 | -45 | 5 | 3.68 |

PET, polyethylene terephthalate; HDPE, high-density polyethylene; PVC, polyvinyl chloride; LDPE, low-density polyethylene; PP, polypropylene; MDF, medium-density fibreboard; WEEE, waste electrical and electronic equipment; CRT, cathode-ray tube; AHP, absorbent hygiene product.