Supporting Information

Structural and magnetic properties of novel dinuclear Cu(II) complexes featuring triazolyl-naphthalimide ligands

Jonathan A. Kitchen†*, Ningjin Zhang†, Anthony B. Carter†, Anthony J. Fitzpatrick‡ and Grace G. Morgan‡

† Chemistry, Faculty of Natural and Environmental Sciences, Highfield Campus, University of Southampton, Southampton, SO17 1BJ, UK
‡ School of Chemistry, University College Dublin, Belfield, Dublin 4, Ireland.

Contents

1. High Resolution Mass Spectra

Figure S1: HRMS (ESI+) spectrum of L1	2

Figure S2: HRMS (ESI+) spectrum of L2	2

2. Infrared Spectra

Figure S3: IR(neat) spectrum of L1	3

Figure S4: IR(neat) spectrum of L2	3

Figure S5: IR(neat) spectrum of [Cu2(L1)4(NO3)4]	4

Figure S6: IR(neat) spectrum of [Cu2(L1)2(OAc)4]	4

3. NMR Spectra

Figure S7: 1H NMR (DMSO-d6, 400 MHz) spectrum of L1	5

Figure S8: 1H NMR (DMSO-d6, 400 MHz) spectrum of L1 – aromatic region	5

Figure S9: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L1	6

Figure S10: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L1 (110 – 165 ppm)	6

Figure S11: 1H NMR (DMSO-d6, 400 MHz) spectrum of L2	7

Figure S12: 1H NMR (DMSO-d6, 400 MHz) spectrum of L2 – aromatic region	7

Figure S13: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L2	8

Figure S14: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L2 (100 – 170 ppm)	8

4. Variable temperature magnetic susceptibility

Table S1: χmT v T data for [Cu2(L1)4(NO3)4]	9

Table S2: χmT v T data for [Cu2(L1)2(OAc)4]	10

1. High Resolution Mass Spectra

Figure S1: HRMS (ESI+) spectrum of L1

Figure S2: HRMS (ESI+) spectrum of L2

2. Infrared spectra

Figure S3: IR(neat) spectrum of L1

Figure S4: IR(neat) spectrum of L2

Figure S5: IR(neat) spectrum of [Cu2(L1)4(NO3)4]

Figure S6: IR(neat) spectrum of [Cu2(L1)2(OAc)4]

3. NMR spectra

Figure S7: 1H NMR (DMSO-d6, 400 MHz) spectrum of L1

Figure S8: 1H NMR (DMSO-d6, 400 MHz) spectrum of L1 – aromatic region

Figure S9: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L1

Figure S10: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L1 (110 – 165 ppm)

Figure S11: 1H NMR (DMSO-d6, 400 MHz) spectrum of L2

Figure S12: 1H NMR (DMSO-d6, 400 MHz) spectrum of L2 – aromatic region

Figure S13: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L2

Figure S14: 13C{1H} NMR (DMSO-d6, 101 MHz) spectrum of L2 (100 – 170 ppm)

4. Variable temperature magnetic susceptibility

Variable temperature magnetic susceptibility for poly-crystalline powder samples were recorded on a Quantum Design MPMS® XL-7 SQUID magnetometer at 0.1 T. Magnetic susceptibility was recorded in the range of 300-4 K cooling at 3 K/min. Diamagnetism of the sample and sample holder were accounted for using pascals constants and by measurement, respectively. Data for [Cu2(L1)4(NO3)4] and [Cu2(L1)2(OAc)4] presented in Table S1 and S2.

Table S1: χmT v T data for [Cu2(L1)4(NO3)4]

| Temperature (K) |  | χmT (cm3mol-1K) |  |
| --- | --- | --- | --- |
| 300.0019 | 0.75702 |  |
| 289.8316 | 0.77741 |  |
| 279.5016 | 0.77593 |  |
| 269.2881 | 0.77416 |  |
| 259.0646 | 0.77234 |  |
| 248.8808 | 0.77052 |  |
| 238.6562 | 0.76951 |  |
| 228.629 | 0.76749 |  |
| 218.2655 | 0.76863 |  |
| 208.0807 | 0.77042 |  |
| 197.8687 | 0.77277 |  |
| 187.6833 | 0.77581 |  |
| 177.4646 | 0.77647 |  |
| 167.3067 | 0.77656 |  |
| 157.1044 | 0.77675 |  |
| 146.8847 | 0.7781 |  |
| 136.6957 | 0.77862 |  |
| 126.4884 | 0.77907 |  |
| 116.3026 | 0.78095 |  |
| 106.0944 | 0.78066 |  |
| 95.88165 | 0.78008 |  |
| 85.6864 | 0.78135 |  |
| 75.47318 | 0.78104 |  |
| 65.24604 | 0.78394 |  |
| 55.06224 | 0.78608 |  |
| 44.83253 | 0.79685 |  |
| 34.62006 | 0.78948 |  |
| 24.41437 | 0.78906 |  |
| 14.20805 | 0.78795 |  |
| 3.99839 | 0.77531 |  |

| Table S2: χmT v T data for [Cu2(L1)2(OAc)4] Temperature (K); χmT (cm3mol-1K). 299.989; 0.76804. 289.928; 0.74346. 279.862; 0.71746. 269.685; 0.68963. 259.777; 0.66099. 249.648; 0.63004. 239.671; 0.59785. 229.666; 0.56384. 219.638; 0.52799. 209.676; 0.49065. 200.1; 0.45320. 189.801; 0.41136. 179.802; 0.36940. 169.887; 0.32685. 159.908; 0.28352. 149.958; 0.24043. 139.977; 0.19808. 129.979; 0.15750. 119.994; 0.11987. 110.012; 0.08628. 100.006; 0.05771. 90.0128; 0.03509. 79.9987; 0.01870. 70.0326; 0.00831. 60.0311; 0.00280. 50.0327; 0.00061. 39.9973; 0.00006. 30.0007; 0.00000. 19.9978; 0.00000. 17.4371; 0.00000. 10.0138; 0.00000. 4.01032; 0.00000. |  |
| --- | --- |