Read me file:

University of Southampton – ECS - Suvi Virtanen - s.virtanen@soton.ac.uk

The excel file contains experimental data for the paper. In particular:

Fig.1 FTIR spectra of a) triethoxy(octyl)silane b) silica c) triethoxy(octyl)silane functionalised silica.

Fig.2 The derivative mass as function of temperature for a) unwashed functionalised (+1 off set) b) washed functionalised c) untreated silica nanoparticles (+2.5 offset).

Fig.3 Estimates and two-sided 90 % confidence intervals for distribution percentiles used in Weibul plot of breakdown data.

Fig. 4 Weibull breakdown parameters for composites containing functionalized (PEx/C8Si/13) and un-functionalized (PEx/Si/7) silica: alpha value at start and after drying are normalised to PE sample; the numerical beta-value for each data set.

Fig.5 The electric field calculated from applied voltage and corresponding DC-conductivity of different materials when 10 V/s ramp rate was used at 30 °C

Fig.6 The electric field and corresponding DC-conductivity using SCLC model and the experimental values for electric field calculated from applied voltage and corresponding DC-conductivity when 10 V/s ramp rate was used at 30 °C for xylene processed LDPE (PEx)

Fig.7 The electric field and corresponding DC-conductivity using SCLC model and the experimental values for electric field calculated from applied voltage and corresponding DC-conductivity when 10 V/s ramp rate was used at 30 °C for xylene processed LDPE composite containing 13wt% of octyl-functionalized nanosilica (PEx/C8Si/13).

Date of data collection: from December 2015 to April 2016.

Information about geographic location of data collection: University of Southampton, U.K.

Date that the file was created: September 2016