Read me file:

University of Southampton – ECS - Suvi Virtanen   s.virtanen@soton.ac.uk

The excel file contains experimental data for the paper. In particular:

Fig.2 The averaged water uptake capability from 4 samples of: PE/C8Si/8, PE/Si/7, and PE as reference. The error bars show standard deviation.

Fig. 3 DC-conductivity of PE and PE/C8Si/8 composite in ambient and dry conditions.

Fig.4 DC-conductivity of untreated silica composite PE/Si/7 and treated nanosilica PE/C8Si/8 composite in different humidities.

Fig.5 Real relative permittivity of nanocomposites containing a) 8 wt% of octylsilane treated nanosilica, b) 7 wt% of untreated nanosilica, c) 4 wt% of octylsilane treated nanosilica, d) 4 wt% of untreated nanosilica, and dielectric loss tangent of nanocomposites containing e) 8 wt% of octylsilane treated nanosilica f) 7 wt% of untreated nanosilica g) 4 wt% of octylsilane treated nanosilica h) 4 wt% untreated nanosilica upon water immersion at different time intervals. The spectra for 30 day immersed pure system (PE) is also plotted for reference in Figs. 5a and 5e.

Date of data collection: from March 2016 to March 2017.

Information about geographic location of data collection: University of Southampton, UK

Date that the file was created: May 2017