Data sets support:
Luis F. Arenas, Carlos Ponce de León, Frank C. Walsh, Pressure drop through platinized titanium porous electrodes for cerium-based redox flow batteries, AIChE Journal, 2017.

Data derived from hydraulic pressure drop through platinized titanium porous electrodes for cerium-based redox flow batteries and the industrial processes involving cerium ion conversion.

Data for Figure 4: Pressure drop vs. mean linear flow velocity, Pressure drop vs. Re
Data for Figure 5: Log-log plot for pressure drop vs. Re
Data for Figure 6: Darcy’s friction factor vs. mean linear flow velocity, Darcy’s friction factor vs. Re
Data for Figure 7: Darcy’s permeability vs. mean linear flow velocity, Darcy’s permeability vs. Re
Data for Figure 8: Ergun plot calculated from pressure drop
Data for Figure 9a: Electrode limiting current vs. mean linear flow velocity
Data for Figure 9a and 10: kmAe vs. mean linear flow velocity, kmAe vs. pressure drop

Assigned DOI: 10.5258/SOTON/D0229