READ ME File For 'Accompanying data to: The characteristics and performance of hybrid redox flow batteries with zinc negative electrodes for energy storage'
Dataset DOI: 10.5258/SOTON/D0394
ReadMe Author: Luis Fernando Arenas Martinez, University of Southampton

Data sets supporting the review paper:

Luis F. Arenas, Adeline Loh, David P. Trudgeon, Xiaohong Li, Carlos Ponce de León, Frank C. Walsh, The characteristics and performance of hybrid redox flow batteries with zinc negative electrodes for energy storage, Renewable and Sustainable Energy Reviews, 2018.

Data for Figure 9: Cyclic voltammogram at a glassy carbon electrode for 10 mmol dm–3 Zn(II) in 0.5 mol dm–3 sodium methanesulfonate. Potential sweep rate: 20 mV s–1 at 298 K.

Data for Figure 11: Charge-discharge cell potential of a Zn-Ce RFB unit cell using a Pt/Ti felt electrode in constant charge regime at 20 mA cm–2 and a mean linear flow rate of 4 cm s–1, operating at 50 °C and starting at 50% SOC. Positive electrolyte composition: 0.4 mol dm–3 Ce(IV) in 4.0 mol dm–3 MSA; Negative electrolyte composition: 1.5 mol dm–3 Ce(IV) in 1.0 mol dm–3 MSA.

Geographic location of data collection: University of Southampton, U.K.
Dataset available under a CC BY 4.0 licence
Publisher: University of Southampton, U.K.
Date: March 2018