READ ME File For 'X-ray computed micro-tomography of reticulated vitreous carbon'
Dataset DOI: 10.5258/SOTON/
ReadMe Author: Luis Fernando Arenas Martinez, University of Southampton

Data sets supporting the review paper:

Luis F. Arenas, Richard P. Boardman, Carlos Ponce de León, Frank C. Walsh, X-ray computed micro-tomography of reticulated vitreous carbon, Carbon, 2018.

Data for Figure 8: Surface area per unit volume of different RVC grades. μCT data for all specimens obtained at a resolution of 9.6 μm per voxel, and additionally for RVC 100 ppi at 1.3 μm per voxel. Comparative data from SEM measurements [1,22] and pressure drop via the Ergun equation [3]. Linear fit for Friedrich’s A_e SEM data: y = 0.66x – 0.53 (R2 = 0.99). Linear fit for (underestimated) A_e by μCT at low resolution: y = 0.11x + 5.44 (R2 = 0.78).

Data for Figure 10: Distribution of the open-foam cell properties in 100 ppi RVC at a resampled resolution of 6 μm per voxel from a μ-CT scan: a) cell volume b) cell surface area. Both approximate to gamma distributions.

Geographic location of data collection: University of Southampton, U.K.
Dataset available under a CC BY 4.0 licence
Publisher: University of Southampton, U.K.
Date: March 2018