ESI for:

Low temperature CVD of thermoelectric SnTe thin films from the single source precursor [nBu3Sn(TenBu)]

Fred Robinson, Daniel W. Newbrook, Peter Curran, C. H. (Kees) de Groot, Duncan Hardie, Andrew L. Hector, Ruomeng Huang and Gillian Reid

Contents:

Figure S1 NMR spectra for [nBu3Sn(TenBu)] in CDCl3 at 295 K.

Figure S2 Isothermal step TGA experiment of Bu4Sn used for vapour pressure calculation.

Figure S3  Grazing incidence XRD data for SnTe samples FR148T8 (black), FR148T7 (red), FR146T5 (green), FR173T4 (blue) and ICSD-188457 (bottom red).1

Table S1 Lattice parameters calculated from decomposition analysis of XRD patterns of thin films of SnTe, crystallite sizes acquired using the Halder-Wagner method and literature values.

Figure S4 Lower magnification SEM images of films deposited by CVD onto fused SiO2 substrates showing uniform film deposition and the corresponding EDX spectra for; tile (a) deposition 1 tile 2, (b) deposition 2 tile 1, (c) deposition 2 tile 2 and (d) deposition 3 tile 1.

Figure S5 Halder-Wagner plots with trend lines obtained by linear regression analysis.

Figure S1 NMR spectra for [nBu3Sn(TenBu)] in CDCl3 at 295 K.

Figure S1.1 The 1H NMR spectrum.

Figure S1.2 The 13C{1H} NMR spectrum.

Figure S1.3 The 2D HSQC NMR spectrum.

Figure S1.4 The 119Sn{1H} NMR spectrum.

Figure S1.5 The 125Te{1H} NMR spectrum.

Figure S2 Isothermal step TGA experiment of Bu4Sn used for vapour pressure calculation.

Figure S3  Grazing incidence XRD data for SnTe samples deposition 2 tile 2 (black), deposition 2 tile 1 (green), deposition 1 tile 1 (purple), deposition 3 tile 1 (blue) and ICSD-188457 (bottom red).1

Table S1 Lattice parameters calculated from decomposition analysis of XRD patterns of thin films of SnTe, crystallite sizes acquired using the Halder-Wagner method and literature values. *Lanthanum hexaboride standard used and matched to a literature pattern.2

| Data | Deposition Temperature (◦C) | a (Å) | Rwp% | Rp% | Crystallite size (nm) with standard* |
| --- | --- | --- | --- | --- | --- |
| Deposition 1 Tile 1 | 404 | 6.3881(3) | 14.30 | 9.82 | 110(30) |
| Deposition 2 Tile 1 | 410 | 6.35250(18) | 15.50 | 10.82 | 100(10) |
| Deposition 2 Tile 2 | 355 | 6.3304(4) | 12.59 | 9.29 | 210(110) |
| Deposition 3 Tile 1 | 434 | 6.30301(19) | 12.73 | 9.75 | - |
| Bulk SnTe1 | - | 6.318(3) | 13.70 | 13.60 | - |

Figure S4 Lower magnification SEM images of films deposited by CVD onto fused SiO2 substrates showing uniform film deposition and the corresponding EDX spectra for; tile (a) deposition 1 tile 2, (b) deposition 2 tile 1, (c) deposition 2 tile 2 and (d) deposition 3 tile 1.

aaaaa

(b)

(c)

(d)

Figure S5 Halder-Wagner plots with trend lines obtained by linear regression analysis and compared to a lanthanum hexaboride standard to account for instrumental peak broadening.

Figure S5.1 Plot for Deposition 1 tile 1.

Figure S5.2 Plot for Deposition 2 tile 1.

Figure S5.3 Plot for Deposition 2 tile 2.

Figure S5.4 Plot for Deposition 3 tile 1.

References

1	P. Bauer Pereira, I. Sergueev, S. Gorsse, J. Dadda, E. Müller and R. P. Hermann, Phys. status. Solidi B, 2013, 250, 1300.

2	A. A. Eliseev, G. M. Efremmov, V A Kuz’micheva, E. S. Konovalova, V. I. Lazorenko, Y. B. Paderno and S. Y. Khlyustova, Kristallografiya, 1986, 31, 803.