## Slide 1: Modelling and Optimising Femtosecond Laser Machining using Deep Learning
Ben Mills, James A Grant-Jacob, Michael McDonnell,
and Robert W Eason
b.mills@soton.ac.uk
Optoelectronics Research Centre, University of Southampton, UK
Notes: Please use the dd month yyyy format for the date for example 11 January 2008. The main title can be one or two lines long.

## Slide 2: Outline
Motivation
Introduction to neural networks
Using a digital micromirror device (DMD), as an intensity spatial light modulator, for laser machining
Training a neural network to predict the outcome of laser machining
Conclusions
Notes: If using a school logo, make sure that if you have a long page title, it does not encroach on the logo. Allow about 2cm around the logo. Run the page title onto two lines if necessary.

## Slide 3: What is a Neural Network?
A network of nonlinear functions, with an input layer and an output layer
Transforms data from one domain to another domain
Notes: If using a school logo, make sure that if you have a long page title, it does not encroach on the logo. Allow about 2cm around the logo. Run the page title onto two lines if necessary.

## Slide 4: What is a Neural Network?
We actually use variants of convolutional neural networks
As used in self-driving cars and medical diagnostics
The neurons in the network learn to recognise objects
Perfect for image data
Notes: If using a school logo, make sure that if you have a long page title, it does not encroach on the logo. Allow about 2cm around the logo. Run the page title onto two lines if necessary.

## Slide 5: Key Technology –Beam Shaping
Change the spatial intensity profile of every laser pulse
Using a digital micromirror device (DMD), which is a spatial light modulator

## Slide 6: Key Technology –Beam Shaping
6

## Slide 7: The Research Objective
In order to achieve this, the NN needs to learn the complex interaction of light and matter

## Slide 8: Training Data Collection
Objective is to train a NN to convert DMD pattern into depth profile
INPUT data = DMD pattern
OUTPUT data = depth profile

## Slide 9: Experimental or Predicted?
The NN has never seen this beam shape

## Slide 10: Experimental or Predicted?
The NN has never seen this beam shape
Experimental
Predicted

## Slide 11: Experimental or Predicted?
The NN has never seen this beam shape

## Slide 12: Experimental or Predicted?
The NN has never seen this beam shape
Experimental
Predicted

## Slide 13: Predictive Capabilities
The trained NN can then be used to predict almost any beam profile
Showing here, prediction for laser machining with a circular beam profile with diameter a) 1 µm, b), 3 µm, c) 5 µm and d) 7 µm

## Slide 14: Predictive Capabilities
A neural network can be trained to predict the appearance of the sample, for different beam shapes, if it was imaged using an scanning electron microscope (SEM)

## Slide 15: Predictive Capabilities
All these images were created via a neural network

## Slide 16: Predictive Capabilities
The neural network has “discovered” a property that we refer to as the diffraction limit

## Slide 17: Extension to 3-pulse prediction
DMD Stack
Experimental Profile
Generated Profile

## Slide 18: Extension to 3-pulse prediction
DMD Stack
Experimental Profile
Generated Profile

## Slide 19: Extension to 3-pulse prediction
DMD Stack
Experimental Profile
Generated Profile

## Slide 20: Extension to 3-pulse prediction
The network has never seen this experimental data.
However, the profiles generated by the neural network match the experimental results.
Neural network confirmed to correctly simulate multiple pulse femtosecond ablation
DMD Stack
Experimental Profile
Generated Profile

## Slide 21: Extension to 3-pulse prediction
The neural network can then used to simulate femtosecond ablation using any set of DMD patterns.
Here, showing machining with a single pulse, with ring patterns

## Slide 22: Extension to 3-pulse prediction
The prediction from
one pulse with three rings
and
three pulses with one ring each
are identical.

## Slide 23: The “reverse” is also possible
We can also train a neural network to perform the “reverse” calculation:
i.e. for a desired sample profile, what beam shape do we need?
McDonnell et al. "Identification of spatial intensity profiles from femtosecond", accepted Optics Express (2021)

## Slide 24: Conclusions
A CNN was trained in order to predict the outcome of laser machining.
Importantly, there was no need for any information regarding the underlying physical processes.
Each prediction took ~10 milliseconds.
Industrial applications, e.g. for immediate optimisation of machining parameters for product design, via the “reverse” neural network approach.
This work was supported via EPSRC: grant numbers EP/N03368X/1, EP/N509747/1 and EP/T026197/1