Using severe plastic deformation to produce nanostructured materials with superior properties

Ruslan Z. Valiev1,* , Boris Straumal2-4 and Terence G. Langdon5

1Institute of Physics of Advanced Materials, Ufa State Aviation Technical University, 12 K. Marx str., Ufa, 450000, Russia

2Ossipyan Institute of Solid State Physics, Russian Academy of Sciences, Ac. Ossipyan str. 2, 142432 Chernogolovka, Russia

3Karlsruhe Institute of Technology (KIT), Institute of Nanotechnology, Hermann-von-Helmholtz-Platz 1, 76344 Eggenstein-Leopoldshafen, Germany

4National University of Science and Technology «MISIS», Leninskii prosp. 4, 119049 Moscow, Russia

5Materials Research Group, Department of Mechanical Engineering,

University of Southampton, Southampton SO17 1BJ, U.K.

*Corresponding author ruslan.valiev@ugatu.su

Abstract

The recent decade was marked by significant advances in the development of severe plastic deformation (SPD) techniques to achieve new and superior properties in various materials. This review examines the achievements in these areas of study and explores promising trends in further research and development. SPD processing provides strong grain refinement at the nanoscale, produces very high dislocation and point defect densities as well as unusual phase transformations associated with particle dissolution, precipitation or amorphization. Such SPD-induced nanostructural features strongly influence the deformation and transport mechanisms and can produce a substantial enhancement in the performance of advanced materials. Exploiting this knowledge, we discuss the concept of nanostructural design of metals and alloys for multifunctional properties such as high strength and electrical conductivity, superplasticity, increased radiation and corrosion tolerance. Special emphasis is placed on advanced metallic biomaterials that promote innovative applications in medicine.

Keywords: bulk nanostructured materials, severe plastic deformation, ultrafine-grained biomaterials, functional properties, mechanical properties, nanostructural design

- Introduction

Processing by severe plastic deformation (SPD) is one of the most efficient means for fabricating bulk ultrafine-grained (UFG) metals and alloys. Pioneering research in this area has been conducted for over 25 years (, ). Fig. 1 illustrates the recent growth in research activity on SPD (). Most of the trends in SPD research are thoroughly described in several recently published review articles and books covering different aspects of the nano SPD topic, such as simulation and development [1, , , , ] of SPD techniques; grain refinement and its mechanisms in various materials – pure metals, model and commercial alloys [2, 3, 6, , , ], intermetallic compounds and also some ceramics and polymers [10, , ,]; fundamentals of superior properties and the innovative potential of nanoSPD materials [1, 2, 12, ,,,, ].

Recent studies demonstrated that SPD processing allows not only the introduction of effective grain refinement but also nontypical phase transformations (3, 14). These processes result in the formation of peculiar, non-equilibrium structural features at the nanoscale level, such as high dislocation densities located mainly at grain boundaries [1, 18]; nanotwins [13]; solid solution decomposition in alloys leading to the formation of nanoprecipitates [14, 16], and the re-distribution of alloying elements segregating at grain boundary areas (8, ). Especially remarkable is the unusual combination of SPD-induced diffusive and displacive (martensitic) phase transformations (, ).

Figure 1. Numbers of papers published on research in SPD and high pressure torsion (HPT) (reproduced from (3)

These SPD-induced nanostructural features influence deformation mechanisms in SPD materials and lead to substantial enhancement of their performance which cannot be attained by conventional processing. Exploiting this knowledge opens a new way of formulating the concept of nanostructural design by SPD processing and for evolving superior multifunctional properties in UFG materials.

The last decade has been marked by significant progress in developing and optimizing SPD processing techniques to achieve superior properties. These developments are associated either with modifications of the conventional SPD techniques to promote their commercialization (such as an improvement in the efficiency of processing techniques and a reduction of material wastage) (4, 7,  ) or with the optimization of SPD regimes and the development of complex SPD processing routes when two or more SPD processing techniques are combined (, ). It has been demonstrated that complex SPD processing routes applied to metallic materials provide further microstructural refinement and therefore higher reductions in grain size, resulting in drastic improvements in performance. A combination of several processing techniques provides an extra tool for texture design in UFG metallic materials to further control the anisotropy of microstructure and the resulting properties.

The present manuscript aims at providing a critical review of the latest achievements in advanced SPD processing, focusing on developments that have not received appropriate attention in the earlier reviews. Historical developments and a short overview of the most popular (classical) SPD processing techniques are presented briefly in the beginning of Section 2. Then modified SPD processing techniques and regimes are described in Section 2.1, followed by a presentation of complex SPD processing routes applied for nanostructuring of various metals and alloys (Section 2.2). Microstructural features of UFG materials produced by advanced SPD processing as well as the main principles of nanostructural design via SPD to achieve superior mechanical and functional properties are presented and discussed in sections 3 and 4. The existing and potential applications of UFG metals via advanced SPD processing are outlined and also discussed in Section 4.

- Recent trends in the development of SPD techniques

The processing of nanomaterials by SPD techniques has become of major importance in research laboratories around the world.

From a historical point of view, SPD processing is relatively ‘young’, but its basic idea goes back to the work of ancient artisans who used repetitive forging and folding technique (2). This process was first developed for steel manufacturing in China for use in swords about 2000 years ago. The processing approach was also employed for manufacturing of Wootz steel in Japan, later in India, then this processing concept spread further to the Middle East where the famous Damascus steel was developed. Impressively all of these processing techniques were developed without metallurgical knowledge and without any fundamental understanding of the basis for the processing procedures.

A detailed analysis of the research activities related to SPD in the period from 1935 to 1988 has been carried out recently by Edalati and Horita (). The first date of year 1935 is key as Prof. P.W. Bridgman from Harvard University (), introduced a die set for compression and torsion straining and conducted the first studies of the effects of high hydrostatic pressure combined with high shear stress on phase transformations in minerals and metals [26]. The principles of Bridgman’s fundamental work were further extended using die sets combining shear (torsion) and compression straining to introduce high shear strain without changing the sample shape. Such experimental die sets were developed by Polish and British scientists and by Russian scientists from Yekaterinburg (formerly Sverdlovsk, Soviet Union) (see 25) in the 1980s. Very large strains, with true strains exceeding 6–8, were achieved using these facilities, leading to significant microstructural refinement in several metals.

The year 1988 is another milestone. A pioneering study on SPD processing was performed in Ufa (), resulting in the production of metals and alloys with submicrometer grain sizes and high-angle grain boundaries which showed outstanding superplastic properties. This was further studied in the works by Valiev et al, using the combination of torsion and compression, later termed «high pressure torsion (HPT)» [] using the Bridgman type of die set. A short time later, this research was extended to equal-channel angular pressing (ECAP) []. The results of these early studies were summarized in a review (1).

HPT and ECAP have become the most popular SPD processing techniques since about 1988, although these processes continuously undergo modifications, as will be demonstrated below. Furthermore, several other SPD processing techniques are now also available, including accumulative roll bonding (ARB), twist extrusion, multi-axis forging. A number of recent reviews and books (7, 24, , ) are focused on the different SPD techniques and provide detailed information about their main principles and recent developments.

However, these SPD techniques have been used primarily for laboratory-scale research. The requirement of an economically-feasible production of UFG metals and alloys raises several new problems in the development of SPD processing. The key challenges are to reduce material waste, obtain a uniform UFG structure and enhanced properties in bulk billets and products, and to increase the productivity. Strategies for solving these problems are examined in the following section.

2.1. Continuous SPD processing techniques

Continuous ECAP

The conventional ECAP process is very labor-intensive since it requires significant manual effort related to inserting and removing the relatively short billets (typically having lengths of ~100…200 mm) from conventional dies. Therefore, the conventional ECAP technique was modified into continuous forms which can be used for efficient production of material in relatively large volumes with a lower wastage [citation]. Several early research activities focused on the development of continuous ECAP procedures combined with a rolling mill or drawing with the aim of processing long metal strips and rods (see 7). However, further modification of these techniques is required for processing materials with UFG structures.

Another modification of the ECAP technique for processing of long samples was proposed by Rosochowski and Olejnik (). This incremental ECAP (I-ECAP) is a cyclic process consisting of delivering of the billet into the deformation zone, when a small volume of material is deformed by simple shear in each cycle by a reciprocating punch. This technique was further modified into a double-billet I-ECAP process ().

Continuous pressing was first proposed by Segal et al as a continuous simple shear process of long rods () based on the famous Conform process. ECAP with a Conform (ECAP-C) procedure was first developed and used for grain refinement in commercially pure aluminum down to 650 nm (). Today, this technique is termed the ECAP-Conform process (Fig. 2) and it has been utilized in several laboratories around the world (4, 22, 23, , , ).

(a)   (b)

Figure 2 A schematic illustration of ECAP-C device (a): 1 – billet; 2 – running wheel die; 3 – pressure working surface; 4 – gauge; ψ – angle of intersection with wheel die; L – arc of billet grip; and (b) Al billets after six ECAP-C passes (35).

Similar to the conventional ECAP technique, the samples may be subjected to various processing routes and regimes, as described in detail in (4). Computer modeling of ECAP-C is widely applied for selection of load-bearing elements and materials (23,). It has been demonstrated that ECAP-Conform can be applied not only to easily deformable materials, such as commercially pure Al, but also to various alloys, commercially pure titanium and steels (22, 23, 38, 39).

A combination of ECAP-Conform with other deformation processing techniques (such as drawing, rolling, etc.) can achieve superior mechanical and functional properties in metallic materials and this topic is considered in detail in Section 5. The ECAP-Conform process can be used to process metallic rods with UFG microstructure, showing much higher mechanical and functional properties than conventional coarse-grained counterparts.

Continuous HPT

The HPT process is another SPD technique, though it has three main limitations (5, 21):

- Small disks produced by HPT are not suitable for most industrial applications;

- The high degree of applied pressure which must be maintained through straining introduces a limit on the installation construction;

- An inhomogeneous degree of strain in induced across the diameters of the disks resulting in microstructural and property gradients.

A modified HPT technique for the processing of rings introduced in () helps to overcome some of these limitations. The replacement of a disk by a ring permits not only the avoidance of the less-processed central part of the disk but also to a further scaling–up of the HPT technique to 100 mm in diameter (). The sample shape can be improved by high-pressure sliding (HPS) which is another attempt that was developed for fabrication of sheet metallic materials having 100 mm in length, 5 mm in width and 0.8 mm in  thickness ().

The HPS technique is shown in Fig. 3. Rectangular sheets can be processed using HPS and, there is also a possibility for scale-up of the process once an equal strain is introduced throughout the sample under the same load.

Continuous high-pressure torsion (CHPT), developed with the aim of microstructural refinement and subsequent enhancement of properties, was the next step in the improvement of HPT (). CHPT was successfully applied for manufacturing of ultrafine-grained wires having a diameter of 2 mm from pure Al and Cu.

- b)

Figure 3 Schematic illustration of HPS. (a) assembly of two anvils with guiding pins, one plunger and two thin sheet samples. (b) cross sectional view of assembly (42).

A new incremental HPT technique (IHPT) was also proposed recently which allows the processing of cylinders (). This technique offers new possibilities for processing UFG metallic materials and appears attractive from the viewpoint of industrial applications as it allows HPT processing of cylinders instead of disks. The method is worthy of further development as well as investigations of its effect on the microstructure and properties of various materials.

2.2. Complex SPD processing routes

Processing by combinations of several deformation processing techniques including at least one SPD technique is often referred to as complex SPD processing routes. For example, two-step SPD processing, such as ECAP followed by HPT, was reported to induce additional refinement in the grain size and a consequent increase in mechanical strength and ductility []. In the section below the main features of complex SPD processing are considered as well as its influence on the microstructure and properties of a number of metals and alloys.

Combinations of two and more SPD techniques

Different combinations of SPD techniques used for processing of metallic materials can be found in the literature: ECAP and HPT (5, , , ), ECAP and hydrostatic extrusion (), ECAP and ARB (),applied to various metallic materials. Typically, a combination of SPD processing techniques leads to microstructures which are quite different from those obtained if the material is processed by an individual SPD technique. This includes extreme grain refinement, variations of morphology, size and fractions of second phase precipitates, dislocation structure and density, crystallographic (micro)texture, grain boundary misorientations.

Grain refinement and further nanostructural modification in metallic materials processed using complex SPD routes generally results in improved mechanical properties (47, 49). However, it should be noted that the microstructure evolution during processing using combined SPD techniques also depends on the processing regimes (homologous temperature, strain) and chemical composition of the material (i.e. its thermal stability). This was clearly seen for pure Ti processed by ECAP and then subjected to HPT at 450 oC and at room temperature (45). The latter processing resulted in a much finer grain size and higher mechanical strength.

A combination of SPD techniques was also used for grain refinement in a commercial ZK60 magnesium alloy to improve its functional properties. In a recent report [50], the hydrogen storage properties were investigated after ECAP processing for 6 passes and ARB processing for 25 passes. The average grain size was ~0.8 μm after ECAP and was further reduced to around 0.3 μm after ARB processing. The latter also resulted in the formation of basal texture with (002) planes parallel to the rolling surface. The hydrogen absorption and desorption kinetics were also measured. Processing only by ECAP resulted in a very low hydrogen storage capacity of 0.5 wt. %. Additional processing by ARB refined the microstructure and improved the hydrogen absorption. The sample from the ECAP material absorbed 4.77 wt.% of hydrogen in 24 h while the capacity of the sample processed by ECAP and ARB was 6.4 wt.%. The enhanced kinetics of hydrogen absorption and desorption in the alloy after additional ARB processing were related to the finer grain size, since hydrogen diffusion is generally faster along grain boundaries and  the grain boundaries and triple junctions can act as nucleation sites for the hydride phase.

SPD processing with traditional metal forming techniques

Samples after simple SPD processing can be subjected also to deformation by a conventional metal forming technique (such as rolling, drawing, extrusion) or by their combination. This may be conducted with the aim to change the shape of the sample and/or to further modify the microstructure and properties. For example, the application of rolling allows the fabrication of UFG sheets from SPD-processed billets or rods. Several combinations of SPD techniques with deformation processing methods are reported in the literature. For example, ECAP was combined with rolling at various temperatures (, ), ECAP with extrusion (), ECAP with swaging and drawing (), ECAP with forging and drawing () and ECAP-Conform with drawing (23). Analysis of these results shows that the final microstructure, properties and shape of the processed material are determined both by microstructure and texture of the SPD-processed material before the metal forming operation(s) and also the parameters of the metal forming operation (temperature, strain, strain rate, strain path).

The microstructure and mechanical properties of commercially pure Cu after 1–10 ECAP passes using route BC were compared with those of samples further cold-rolled to a total reduction ratio of 90% (). Cold rolling caused a transformation of the relatively equiaxed UFG structure developed in Cu during ECAP processing into a lamellar structure with even finer boundary spacing (Fig. 4). For example, a boundary spacing approaching ~180 nm after 10 ECAP passes decreased to ~110 nm after rolling (Fig. 4g,h). A negligible grain refinement in terms of the formation of new boundaries takes place during rolling of ECAP-processed copper. Cold rolling after ECAP with a corresponding number of passes also led to a significant increase (~20%) in the average fraction of high angle grain boundaries.

There is also a significant effect of the metal forming parameters on the microstructure, texture and mechanical properties of SPD-processed material. This was clearly demonstrated for commercially pure Ti (, ) subjected to a two-step process consisting of ECAP (at 300 oC  and cold rolling with a reduction ratio of 70-76 % (at room temperature or at liquid nitrogen temperature). Such processing served to activate two strengthening mechanisms in the pure metal: grain boundary strengthening due to the grain size reduction from the ECAP processing and dislocation strengthening from deformation by rolling. A reduction of rolling temperature from 20 oC to cryogenic temperature improved the yield strength of the two-step processed pure Ti (ECAP for 6 passes followed by rolling) from ~785 MPa to ~915 MPa due to an increased dislocation density in the cryorolled material (57).

Figure 4 EBSD orientation maps of copper after ECAP (a, c, e, g) and ECAP with subsequent rolling (b, d, f, h); a, b - 1 pass; c, d – 2 passes; e, f – 4 passes; g, h – 10 passes.

Clear advantages of combining ECAP with further thermo-mechanical treatment (TMT) have been demonstrated in the development of Ti-based materials for biomedical applications (23, ), including shaping semi-products in the form of sheets or rods and enhancement of properties introduced by ECAP in UFG materials (see also Section 4.3 on nanostructured metallic biomaterials).

It should be noted that the development of complex SPD processing routes for fabrication of UFG materials is usually based on numerous experimental trials and appears as a very time consuming and expensive process requiring a significant amount of material and a precise analysis of microstructure, thermal stability and mechanical properties. Thermo-mechanical simulation of the metal forming processes helps to minimize the amount of expensive SPD-processed material for such experimental work as well as to increase the efficiency of the experimental work and thus reduce the cost []. The results may be used directly in the laboratory as well as in full-scale production.

A physical simulation of hot rolling of ECAP-processed UFG pure Ti was carried out (60) using samples having a size of 20 x 15 x 5 mm3 to predict microstructure and texture evolution, as well as the microhardness, during hot rolling. It was demonstrated that hot rolling leads to a breakup of the as-ECAP crystallographic texture, a further refinement of grain size and an improvement in microhardness with increasing total reduction ratio.

Recently, a modified HPT method, High Pressure Torsion Extrusion (HPTE) was proposed (). This technique represents to a combination of HPT and cyclic extrusion. Several advantages are characteristic of HPTE used for processing bulk nanostructured materials in quantities suitable for industrial applications: simple shear conditions, high hydrostatic pressure in a rod-shaped specimen, and the accumulation of a large strain in a single pass. Furthermore, hybrid materials with helical architecture, gradient materials and “hybrid” materials can be produced in a rather simple way using this newly developed process.

3. Nanostructural architecture of SPD processed materials

Studies performed during the last decade, using techniques including 3D-atom probe, TEM/HREM and X-ray diffraction, reveal that SPD processing can not only form UFGs but may also be used to engineer grain boundary structures and generate nanoparticles, segregation or nanoclusters and other structural elements at the nano-scale. The nature of these phenomena is related to the fact that, together with grain refinement, processing by SPD may also lead to unusual phase transformations as a dissolution of second phases, precipitation, amorphization, allotropic phase transformations, and other nanostructural features (see, for example, 12, 14, 16, 18). Also the unusual combinations of SPD-induced diffusive and displacive (martensitic) phase transformations (i.e. transitions with or without mass transfer) can take place during SPD (19, 20, ). On the other hand, the type and morphology of such nanostructural elements, as well as their number density, control deformation and transport mechanisms responsible for improvements of the mechanical, chemical and physical properties of bulk nanostructured materials through SPD techniques and the optimization of processing regimes. Nanostructuring via SPD processing is considered in this section.

3.1. Grain boundaries in nanostructured materials

The density of (GBs) and interphase boundaries (IBs) in UFG materials with submicron (100–1000 nm) or nanocrystalline (<100 nm) sizes is very high and can significantly impact properties. UFG materials can thus be considered as interface-controlled materials (, ).

Gleiter and colleagues suggested that the atomic structure of grain boundaries in UFG materials may be characterized by a number of special features in contrast to grain boundaries in conventional polycrystalline materials (64). This is especially important for materials in which UFG microstructures are produced by SPD techniques (1, 12, 18).

Although the physical mechanisms of microstructure evolution during SPD processing call for further investigation, numerous studies demonstrate that the formation of a UFG structure is determined by the evolution of cells or dislocation substructures formed in the early deformation stages into ultrafine grains with high-angle boundaries during subsequent deformation. At the same time, and depending on the regimes of SPD processing, different types of grain boundaries can be formed in the UFG materials, such as high and low-angle, special and random, equilibrium and so-called “non-equilibrium” grain boundaries with strain-distorted structures containing extrinsic dislocations, as well as boundaries with GB segregation of alloying elements  (16, 18).

As discussed in Section 2, the fabrication of UFG metals and alloys with predominantly high-angle grain boundaries by SPD techniques was first revealed by Valiev et al. (1, 2, 25). In the past decade, active development and application of electron back scattering diffraction (EBSD) has provided quantitative data on the low- to high-angle GB ratio and the presence of special and random boundaries in various metals and alloys subjected to SPD.

For example, EBSD analysis has been used to plot misorientation histograms (). A Mackenzie plot has been added to each histogram for an ECAP-processed Al 6016 alloy. The boundary misorientation angle histogram in Fig. 5 shows that after the first ECAP pass the microstructure is characterized by ~93% of the boundaries with misorientation angles of less than 15° (i.e., low-angle boundaries).

Figure 5 Relative frequency of dislocation cell/subgrain boundaries as a function of misorientation angle for Al 6016 samples processed by ECAP. (a) 1 Pass, (b) 2 passes, (c) 4 passes, and (d) 8 passes with a Mackenzie plot superimposed onto each histogram (71).

After the second pass (Fig. 5b), the average dislocation cell size is reduced considerably but the inhomogeneous structure remains characteristic for most cells orientated parallel with the Y- (or transverse) direction. Simultaneously the boundary misorientation distribution shifts upward, with ~67% of boundaries comprising misorientation angles less than 15°. After four ECAP passes some equiaxed dislocation cells/subgrains appear together with some shape irregularities and alignment of the microstructure off-axis to the Y- (or transverse) direction. The distribution histogram with ~34% of boundaries having a misorientation of less than 15° reflects a more gradual upward shift in the corresponding misorientation angle (Fig. 5c). Further processing to 8 passes resulted in an evident reduction of the dislocation cell/subgrain size, upward shifts in the misorientation distributions (Fig. 5d) and a near random distribution after 12 ECAP passes was observed in (65).

The results of this work, as well as another recent study by EBSD analysis (), provide convincing support for earlier conclusions that the formation of a UFG structure with mostly high-angle boundaries takes place during ECAP when the number of passes is over 4-6 (true strain > 4-6). Such very large strains cannot be achieved with the use of conventional processing techniques, such as rolling, extrusion or drawing, and therefore their application provides no opportunity for the formation of a real UFG microstructure with mostly high-angle grain boundaries. Moreover, SPD techniques involve simple shear, which makes it possible to form the ultrafine grains as equiaxial or at least close to it in shape.

A variety of characterization methods was used in different studies to investigate features of grain boundaries in UFG materials produced by SPD techniques. Among them were methods of high resolution transmission electron microscopy (HRTEM), X-ray diffraction, Mossbauer spectroscopy, dilatometry, differential calorimetry and others (see, for example, 1, 10, 16). It was clearly demonstrated that optimization of the SPD processing regimes results in the formation of mostly high-angle grain boundaries with specific non-equilibrium structures. The application of grain boundary diffusion measurements (, , ) and high resolution transmission electron microscopy (HRTEM) analyses (18, , ), helped to identify and characterize the effect of the severe deformation processing on transformations of the grain boundary structures.

For example, it was revealed that HPT may result in the formation of a very high density of dislocations, facets and steps at grain boundaries of an Al-3% Mg UFG alloy (). There are numerous reports which confirm the appearance of such non-equilibrium grain boundaries in different materials processed by SPD (1, 18, 69,  ).

The term “non-equilibrium grain boundaries” has been accepted and utilized by the entire SPD materials science community and it is also used here to describe grain boundaries which are defined formally as boundaries with strain-distorted structures and containing high densities of extrinsic dislocations (1, 18).

Thus, recent studies of the grain boundary structure in SPD-processed UFG materials suggest that specific non-equilibrium grain boundaries with strain-distorted structures associated with a correspondingly large residual microstrain is a typical feature in these nanomaterials.

3.2. Nanotwins in metallic nanomaterials

Decreasing grain size usually impedes twinning in coarse-grained face-centered-cubic (fcc) metals. In nanocrystalline metals, twinning becomes easier with decreasing grain size up to a certain grain size, reaching a maximum twinning probability, and then twinning becomes more difficult when the grain size decreases even further ().  The difference between twinning mechanisms in nanocrystalline and coarse-grained materials has been revealed by molecular dynamics simulations and experimental observations. Consequently, deformation twins are only observed in nanocrystalline materials. The formation of nanotwins can be promoted if certain properties intrinsic to the material and  external deformation conditions are satisfied. Among these properties are (74) 1) a relatively low stacking fault energy, 2) a low deformation temperature, 3) a high strain rate. It seems that there is a range of grain sizes which is optimal for deformation twinning for different materials and testing conditions.

In particular, lower temperatures and/or additional cold rolling (CR), extrusion, or drawing promote the formation of nanotwins. Fig. 6 shows a high resolution TEM image of UFG Cu after ECAP and CR at liquid nitrogen temperature. It is possible to clearly observe 10–20 nm twins (). It has been also observed that an enhanced strength and ductility can be obtained in nanocrystalline materials due to deformation twinning (75, ).

Figure 6 TEM images at (a) low and (b) high magnifications of a typical grain with a high density of deformation twins in UFG Cu processed by ECAP with subsequent cold rolling.

Twin GBs (even in nanotwins) typically contain the high-energy facets in addition to the “main” low-energy Σ3 {111}1//{111}2 facet. The observation of such high-energy facets in materials after SPD is an evidence of non-equilibrium GBs processed by SPD ().

3.3. Segregation in SPD-processed nanostructured alloys

Investigations of the thermal stability as a function of the impurity level in metals as reported in a few cases supply indirect evidence of grain boundary segregation in UFG materials. However, grain boundary segregation has recently been observed in UFG materials processed by SPD directly (18, 73, , , ). Atom probe tomography (APT) is the main technique used for atomic scale characterization in most of these reports. At the same time, crystallographic information provided by this technique is very limited and usually the grain boundary misorientation cannot be determined. Moreover, there is almost no possibility of statistical analysis because of the very small grain boundary areas that are analyzed. Nevertheless, the demonstration of grain boundary segregation in various SPD-processed metallic materials  confirms that this is not a marginal feature.

SPD processing resulted in the formation in a UFG AA6061 alloy having a microstructure characterized by Mg, Cu and Si segregation along planar defects attributed to grain boundaries (78). The thickness of the layer enriched by solute elements was about 2 nm. The local enrichment was less than 2 at.%. Segregation at grain boundaries was also observed in several Al alloys processed by both ECAP and HPT (79, 80). The achievement of a mean grain size of about 100 nm and a large fraction of high-angle grain boundaries after 20 turns of HPT processing was reported in AA7075. The data in Fig. 7 () show that clusters ~3-5 nm wide are made of  grain boundary segregants. Local concentrations up to 25 at.% of Mg in layers of ~6–8 nm thick were also observed by APT (80). It appears, therefore, that non-equilibrium grain boundaries with strain-distorted structure have higher amounts of segregating atoms with respect to relaxed interfaces, and the thickness of the segregated layer may be determined by the distorted layer near the non-equilibrium GB. It follows from APT observations that the distributions of the solute elements may be influenced by the local configurations of the GB, and especially dislocations lying at or near the boundaries.

Figure 7 Atom-probe elemental maps of polycrystalline region of an Al–Zn–Mg–Cu alloy after 8 passes of ECAP. (a) Mg, (b) Cu, and (c) Zn maps (81)

3.4 Nanosized particles and secondary phase precipitates

Solution quenching promotes the formation of particles in many alloys subjected to SPD (17,, and others). Examples of such nano-particles as large as ~10–20 nm precipitated in the UFG Al alloys after ECAP processing is presented in these studies. Nano-particles appeared due to dynamic ageing and caused additional precipitation hardening of the alloys. Parameters of SPD processing usually determine the size and morphology of precipitates. In recent years, the subject of dynamic ageing originating from SPD has attracted greater attention because the morphology of precipitates and their formation kinetics differ considerably from the processes of conventional ageing and provide for new possibilities in the production of advanced age-hardenable alloys (, ).

It was recently observed that dynamic ageing during high-pressure torsion competes with dynamic dissolution of precipitates in copper-based alloys (). As a result of this competition a certain steady-state forms between dynamic ageing and dynamic dissolution (). This is controlled by an accelerated diffusion-like mass transfer between matrix solid-solution and precipitates. As a result of this dynamic equilibrium, a certain steady-state solute concentration css is established.

4 Nanostructural design of UFG materials through SPD processing

As was shown in the previous section, there are unique structural characteristics which result from nanostructuring of bulk materials by SPD. Among them are ultrafine grain sizes and shapes, high density of interfaces and lattice defects in the grain interior, as well as the complex structure of grain boundaries, nanotwins, segregation and second-phase nanoparticles. These nanostructural features can strongly influence the transport and deformation mechanisms, therefore changing the properties of not only metallic materials, but also some polymers and ceramics (3, 12, 13).

Deformation mechanisms in nanometals are significantly influenced by grain boundaries, which constitute a large volume fraction in UFG metals. In general, GB-mediated deformation mechanisms can be divided into two basic categories: (1) ‘‘pure” GB mechanisms by the motion of GBs themselves, and (2) GB-mediated mechanisms associated with twinning and dislocation emission from GBs (12, 13, 69). The ‘‘pure” GB mechanisms include GB sliding, stress-driven GB migration, grain rotations mediated by GB dislocations, and GB and triple junction diffusional creep. These mechanisms can significantly contribute to plastic deformation in metallic nanograined materials. Both deformation mechanisms depend on the crystallography of grain boundaries and their defect structure related to the presence of GB dislocations and vacancies. In turn, as discussed in Section 3, the GB structure is determined by SPD processing conditions and regimes.

A recent discovery of the influence of GB segregation on GB sliding and diffusion in aluminum alloys has been substantiated by computer simulation () and experimental studies (, ).  Zn segregations at grain boundaries significantly accelerates the diffusion kinetics and sliding, while Mg segregation inhibits this process. This opens the path to control the mechanical properties of nanomaterials and their thermal stability through GB engineering (16, 70, 73, 90).

We now consider some examples of nanostructural design of metals and alloys for mechanical and functional property combinations in metal biomaterials. These problems refer specifically to simultaneously improving properties of multifunctional materials which are usually mutually exclusive (12, 17).

4.1. Superior strength and ductility

Earlier work on SPD processing (1, 2) focused mainly on grain refinement to improve the mechanical strength of metallic materials according to the well-known Hall–Petch relation

, 		(1)

where σy is the yield stress, d the grain size, and σ0 and KHP are constants for a given material. Later, it was revealed that this relationship may break down for nanomaterials with a grain size less than 20-50 nm [13]. Nevertheless, the Hall-Petch law is usually valid for the UFG materials produced by SPD as they generally have grain sizes in the submicrometer range. The mechanical strength of pure metals can be enhanced by a factor of ~3–6 due to extreme grain refinement via SPD (, ). However, as noted above, the SPD-processed materials often have various nanoscale features and this provides additional strengthening. The contribution of other strengthening mechanisms (dislocation hardening, precipitation hardening, etc.) can provide further enhancement of mechanical strength resulting in values which are much higher than those predicted by the standard Hall–Petch relationship (91, ). Such observations of superstrength were demonstrated for several Al alloys (such as Al 1570, Al 7475), Ti-6Al-4V and steels, and have already been considered in detail in the literature (12, 91).

Grain boundary segregation can provide additional strengthening. In experimental studies of a high strength UFG Al 1570 alloy using a 3D-APT technique, a clear relation between Mg segregation at grain boundaries and strength was demonstrated (80). Similar observations were also recently reported for several UFG Al alloys and stainless steels (79, , ).  A physical explanation for such segregation strengthening is related to dislocations generated at grain boundaries (80). The emitted dislocation glides through the grain interior and is trapped by the opposite grain boundary so that a “dislocation-grain boundary” interaction plays the role of the rate-controlling mechanism. GB segregation can suppress the emission of dislocations due to a solute drag effect which, in turn, results in higher values of stress required for the dislocation emission. Thus, a new strengthening mechanism related to GB segregation can be observed in SPD-processed UFG – referred to as GB segregation hardening (16). A model of this process has been recently considered in (). Figure 8 illustrates the expansion of a dislocation loop in the presence of segregation.

dislocation loop

segregation

l

b

A

B

x1

x3

x1

x2’

A

B

2a1

23>0

23>0

23= –<0

e

(b)

A

B

x1

x3

(d)

x1

A

B

x3

23<0

(a)

(c)

Figure 8 Expansion of a dislocation loop in the presence of segregation. The blue and red ovals denote the segregations that hinder and promote loop expansion, respectively. (a,b) The ends, A and B, of the dislocation loop, which nucleates and expands under the action of the applied load, are pinned by segregation. (a) Projection on the dislocation glide plane illustrates segregation-induced pinning. (b) Projection on the grain boundary plane illustrates the fact that segregation can either promote or hinder dislocation loop expansion, depending on the sign of the x2 -coordinate of its center. (c) By increasing the applied load, dislocation loop expansion is realized via its bow-out, if segregation-induced pinning is strong. (d) If pinning is weak, loop expansion is realized via the unpinning and lateral motion of points A and B (96).

Ductility is required to enable metal-forming operations as well as to avoid catastrophic failure during service. The maximum strain of homogeneous plastic flow before the onset of necking represents the uniform elongation, which is determined by the resistance of the material to macro-localization of plastic flow (13, 92). This parameter can be useful to determine the ability of material to undergo stretch-metal-forming operations. Another parameter determining ductility is the elongation to failure. This parameter takes into account the necking elongation, which is controlled by a competition between localized plastic flow and fracture. Typically, the total elongation of coarse-grained materials is slightly higher than their uniform elongation. For UFG metallic materials, the difference between these two parameters may become very significant. Thus, it is important when analyzing the ductility of UFG metals to unambiguously indicate the precise measure of ductility.

Strength and ductility are the key mechanical properties of any material but these properties are typically mutually exclusive such that materials may be strong or ductile but they are rarely both. Earlier works focusing on mechanical properties of SPD-processed materials demonstrated that grain refinement down to the nanoscale leads to very high mechanical strength, but that these materials invariably exhibit low tensile ductility (, ). This problem was well known in metals subjected to heavy straining by processes such as rolling, extrusion or drawing. The reason for this is that the plastic deformation mechanisms associated with the generation and storage of dislocations may not be active in heavily-deformed materials during their further tensile straining. Such situation is typical for SPD-processed materials as well.

Due to the significance of the problem of mechanical behavior of nanomaterials, the so called “paradox of strength and ductility” was introduced in literature (,). Early reports on combinations of extraordinary strength and ductility in some bulk SPD-processed materials attracted significant attention from the research community, promoting investigations on the development of novel approaches to improve tensile ductility of bulk nanostructured materials. Recent overviews of these research activities are now available (13, 91, , ). Various strategies to improve the low tensile ductility of nanostructured metals and alloys have been proposed. These approaches can be classified into two separate groups: (1) “mechanical” strategies and (2) “microstructural” strategies. The “mechanical” strategies are based on manipulating some mechanical characteristics of the UFG materials, such as strain rate sensitivity and/or work hardening ability, which can be controlled via testing parameters (temperature and/or strain rate). The “microstructural” strategies are based on the concept of microstructural design at the nanoscale level.

Among the strategies for ductility enhancement in UFG metals (see for example (13, 101)) are the development of bimodal microstructures consisting of micro and nano grains, developing graded nanograined metals or nanotwinned structures, and tailoring of the stacking fault energy (SFE) via alloying. These strategies are focused on increasing the strain hardening rate and this leads to an improvement of the uniform elongation during tensile tests. By contrast, a number of recent GB engineering strategies are intended to increase the strain rate sensitivity by accelerating grain boundary sliding, significantly enhancing the ductility (total elongation). For example, the presence of Zn segregation at grain boundaries in Al alloys with UFG structure sharply accelerates sliding, which leads to a considerable increase in ductility and even superplasticity at room temperature (89). At the same time by managing the deformation conditions (temperature, strain rate, etc.) it is possible to successfully combine high strength and ductility.

4.2. High strength and electrical conductivity

A new strategy for nanostructural design in Al and Cu alloys for advanced conductors was recently developed (84, , ). In this strategy, the strengthening mechanisms and mechanisms of electrical resistivity are manipulated by grain refinement (down to the submicrometer scale) and dynamic aging during SPD processing. This resulted in decomposition of the supersaturated solid solution and the formation of nanosized second-phase precipitates in the alloys with UFG structure (Fig. 9). Boundary strengthening and precipitation hardening resulting in superior mechanical strength are characteristic of these ultrafine-grained microstructures with second-phase nanoprecipitates. At the same time, significantly enhanced electrical conductivity results from the very low content of solute atoms and the absence of GP zones in the Al matrix. Theoretical evaluations [104] and experimental studies [84, 103] confirm this approach.

The dependence is well described by the ratio for strength (eq. 2) and electrical resistance (eq. 3) that were applied to assess the properties of UFG alloys in (84, 103, 104):

σtotal=σo+σgs+σss+σdis+σp,                                (2)

where σo is Peierls stress, σgs grain size strengthening, σss solid solution strengthening, σdis dislocation strengthening and σp represents precipitation strengthening.

The effective resistivity of an alloy, ρ, following Matthiessen rule, is normally written as

ρ=ρT+ρD,                                                                      (3),

where ρT is a temperature-dependent phonon contribution and ρD is a contribution from the lattice defects and solutes, which is independent of temperature. The temperature independent part describes resistivity from various defects and thus can be split up into several contributions as

ρtotal=ρss+ρp+ρdis+ρv+ρgbs,                                (4)

where ρss is the resistivity due to scattering by solute atoms dissolved in the matrix, ρp the resistivity added by second phase particles, ρdis and ρv resistivity due to dislocations

and vacancies, respectively, and ρgsb is the resistivity due to scattering on grain boundaries.

Figure 9 Nanostructure with nanoparticles to realize the combination of high strength, good electrical conductivity, and enhanced thermal stability in Cu and Al alloys (84). Red arrows indecate average grain size D and nanosized particles.

For example (84) AA6201, an alloy widely used for electroconductors, was chosen for experimental confirmation. Disks with diameters of 20 mm and thicknesses of 1.5 mm were solution heat treated at 530°C for 2 h and water quenched. Then HPT was used for SPD processing of the disks.

A strong decomposition of the supersaturated solid solution, confirmed by a significant decrease in the lattice parameter of the Al matrix, was revealed by X-ray diffraction. A good match of the X-ray results with recent 3D APT was revealed (104). Dynamic aging leads to a near-complete purification of the matrix from the solute atoms and formation of 10 to 30 nm spherical nanoprecipitates. The strength and electrical conductivity calculations based on the obtained structural data are in good agreement with the experimental values (104).

4.3. Metallic biomaterials with superior strength and functionality

Nanostructuring of biocompatible metallic materials by SPD opens up new avenues for their applications in biomedical engineering (38, ). The most impressive results in this area were achieved for commercially pure Ti. Ti is recognized as one of the most bioinert metals, which makes it attractive for producing medical implants (, ). Unlike many Ti alloys, it does not contain any toxic elements. In terms of biocorrosion resistance, Ti is superior to most surgical metals due to the formation of a very stable passive layer of TiO2 on its surface. Another favorable property of Ti is its low elastic modulus (half that of stainless steel and Co–Cr alloys), which results in less stress shielding and associated bone resorption around titanium orthopedic and dental implants. Furthermore, titanium is lighter than other surgical metals and produces fewer artifacts during computed tomography and magnetic resonance imaging. However, CP Ti’s static and fatigue strengths are too low to be used in some load-bearing medical applications. For example, small plates and screws are often used in the maxillofacial area of a skull (). However, depending on the injury type and locality of bone fixation, loads on implants can vary from 200 to 700 N. The maximum load for a 1-mm-diameter screw can create stresses as high as 900 MPa, which are significantly beyond the ultimate tensile strength of CP Ti and requires using stronger Ti alloys or stainless steels.

Recent studies have shown that the application of such SPD processing techniques as ECAP combined with Conform with a subsequent drawing of the material is the most effective way to produce long-length rods with nanoscale structures (38, ). Nanostructuring of titanium increases its strength and fatigue resistance to levels that exceed those reported for Ti-6Al-4V ELI (109, ). The ultimate tensile strength (UTS) in Ti after ECAP + drawing is almost twice that in the initial state after hot rolling. The strength becomes even higher when increasing the degree of straining during drawing without any dramatic reduction of ductility This is in contrast to conventional deformation processing, such as rolling, extrusion or drawing, when increasing accumulated strain and microstructure refinement results in strengthening but a concomitant reduction in ductility. This is because these processing techniques result in a subgrain type of microstructure which is characterized by pronounced metallographic and crystallographic textures as well as high volumes of low-angle grain boundaries. High strength with retained ductility allow the miniaturization of load-bearing implants made from the nanostructured Ti. Miniaturized Ti dental implants () and mini-plates have been designed using these principles ().

Nano-Ti dental implants. The reduced diameter of nano-Ti implants allows a reduction in damage during their insertion into the jaw, thus making implantation a less traumatic procedure for the patient. Another advantage is the possibility to install these implants in patients with a thin alveolar bone, where conventional implants cannot be used or additional intervention is required (105, 111). The research to date has shown that implants from nano-Ti also have better biological response, including increased cell survival and enhanced cell adhesion (109, 110). Previously, it was found that the colonization of fibroblasts on the surface of Grade 4 titanium increased significantly after nanostructuring and chemical etching (). Observations of patients in a clinical setting has shown that increasing the biological properties of nano-titanium contributes to the rapid engraftment of the implant and about 70% of nano-Ti implants could be loaded immediately after inserting. So far, over 7000 dental implants made from nanostructured Grade 4 Ti with diameters of 2.4 and 3.5 mm, as well as several implants with a diameter of 2.0 mm, have been inserted in several clinics in the Czech Republic (Fig.10). To date, not a single case of rupture or breakage of nano-Ti implants has been reported. The calculations and experimental results show that using available nanostructured titanium with UTS of 1330 MPa makes it possible to securely reduce the diameter of the implant down to 2.0 mm (Fig. 10a). This enables nano-Ti implants even in the case of alveolar bones narrower  than 4.5 mm.

Figure 10 2.0 mm diameter Nanoimplant® (www.timplant.cz/en/) from nanostructured Grade 4 Ti in a panoramic X-ray radiograph after surgery (a), and the control radiograph obtained after incorporation of the implant (b); image of a mini plate with six holes made from nanostructured Grade 4 Ti (c)

Nano-Ti plates for maxillofacial surgery. Using the fatigue endurance limit of conventional and nano-Ti (Table 1), it is possible to design nano-Ti plates with reduced thickness for maxillofacial surgery. It was shown that the plate thickness can be reduced from 0.9 to 0.7 mm without degradation of its mechanical performance [112]. While the standard plates withstood 17000±500 cycles, a nano-Ti plate with reduced cross section withstood 105000±800 cycles [112]. This result points to an enhancement of bending strength of the plate from nano-Grade 4 Ti despite its reduced thickness, where this is an important advantage over the standard item made from conventional Ti.

Table 1 Mechanical properties of conventionally processed and nanostructured Grade 4 Ti produced by ECAP-C and drawing. Data on Ti-6Al-4V ELI alloy are also presented for comparison [109].

| Processing/treatment conditions | UTS, MPa | YS, MPa | Elongation, % | Reduction of area, % | Fatigue strength at 107 cycles [MPa] |
| --- | --- | --- | --- | --- | --- |
| Conventional Ti (as-received) | 700 | 530 | 25 | 52 | 340 |
| nano-Grade 4 | 1330 | 1267 | 11 | 48 | 620 |
| Conventional Ti-6Al-4V ELI | 940 | 840 | 16 | 45 | 530 |

Surface modification to improve biointegration. Surface properties are an important aspect of an implant design to ensure effective osseointegration. Pure Ti has very low bioactivity (i.e. it is bioinert) and it does not bond directly to the human bone. As a result, the implant may shift and loosen during service life. A significant body of research has shown that grain refinement down to the nanoscale in CP Ti can increase the adhesion and proliferation of various bone-forming cell types (113, ,,,,). Additional surface modification can further improve the bioactivity of implants made from UFG Ti, including chemical etching and deposition of bioactive coatings (107, , , , , ).

HF-HNO3 – based solutions are used for acid treatment of the implant surface. HF acid interacts with the TiO2 oxide film and results in the formation of a dense film of fluorides and hydrides. In recent work (123) a mixture of acid etchants was used to reveal the effect of topography of the nano-Ti surface. Nanostructured Ti was found to produce rougher surfaces after etching. Similar results have been reported by numerous researchers (, , ), demonstrating that the specific relief on the nano-Ti surface facilitates higher rates of adhesion for both fibroblast (126) and pre-osteoblast (124) cells.

Biocompatible coatings can facilitate integration of the titanium implants into a human bone (). Therefore, research into synthesis of biocompatible coatings integrating inorganic (Ca-, P- containing phases) and organic (biologically active and bioinert molecules) components on titanium implants is quite relevant at present (, ), with recent results on bioactive coatings on nanostructured biometals (, , ).

Biodegradable metals

There has been a growing interest in the application of biodegradable metallic materials for manufacturing of devices in the biomedical industry (,). There are strict requirements on reliability, bioresorbability and biodegradability of materials used for the manufacturing of implants and stents. Nanostructured Mg and Fe can potentially satisfy all these requirements due to their bioresorbability and biodegradability. High strength may be achieved by grain refinement and corrosion performance controlled due to the second-phase particles' distributions. The required Young’s modulus, the increased possibility of bone adaptation and a controlled drug release option may be reached by micro- and macro-porosity (134, ).

The high potential of SPD-processed Mg alloys for applications as biodegradable materials was demonstrated in recent studies focused on their biocompatibility (). Significantly improved mechanical strength and lower corrosion rates without degradation of biocompatibility were observed in AZ31 Mg alloy after ECAP processing.  Acceptable toxicity to MG63 cells with grade I toxicity was demonstrated by AZ31 Mg alloy after multi-pass ECAP processing, which was comparable to other standard Mg alloys such as Mg–Ca and Mg–Zn, showing good biocompatibility in in vivo studies. However, a 3-pass back-pressure ECAP alloy indicated Grade II toxicity which may be attributed to a higher Mg and Al concentration leading to an osmolarity shock to the cells. Therefore, optimum SPD processing parameters should be selected for fabrication of Mg alloys showing the required mechanical, chemical and biological properties suitable for biomedical applications. As Mg alloys have an hcp lattice, significant attention must be paid also to the control of crystallographic texture in the ECAP-processed material. The latter provides an extra tool to effectively tune the mechanical properties and resorption rates without reduction of cytocompatibility (, , ). Biological properties of the surface can be further enhanced by additional surface modifications ().

Summary and conclusions

The results of this overview provide a clear demonstration that processing by SPD has the capability of producing superior properties in bulk nanostructured materials.  Based on the evidence available to date, there is now significant information on the underlying mechanisms that account for these special properties, opening new possibilities for the practical applications of these materials in  new structural and functional applications. Recent discoveries demonstrate new opportunities for SPD processing for improving other physical and chemical properties of materials.  These properties were mentioned only briefly in this report but nevertheless have achieved considerable advances in recent years (). These include, for example, increased superconductivity, thermoelectricity, giant magnetoresistance, improved hydrogen storage, and improved biocompatibility.

A general rule in modern materials science is that any material breakthrough in the twentieth century required, from the time of the initial innovation, about two decades to achieve widespread market acceptance ().  It appears that bulk nanostructured metallic materials, as produced by SPD processing, are also following this track. Although the first developments and research started at the beginning of the 1990s, it is important to note that there have been very significant developments in the commercialization of these materials in recent years and this is especially evident from the widespread production of advanced pilot articles having new functionalities (38).

There are three primary advantages associated with the application and commercialization of bulk nanostructured metals: markedly superior properties, the potential for efficient fabrication using SPD processing techniques such as ECAP-C and the possibility of using these materials to produce cutting-edge products. Furthermore, it is evident that many of these new applications involve, or will involve in the future, extreme environmental conditions requiring both exceptional strength and improved functional properties.

It is reasonable to anticipate that, in the very near future, the nanostructuring of materials by SPD processing will lead to new breakthroughs in the development of bulk solids having superior properties for advanced structural and functional applications.

Acknowledgements

R.Z.V. gratefully acknowledges the financial support from the Russian Science Foundation in the framework of the Project No. 20-63-47027 for research in his part of the publication. The work of T.G.L. was supported by the European Research Council under Grant Agreement No. 267464-SPDMETALS. We are especially grateful to all who provided support, comments, fruitful discussions and allowed us to cite their publications during the work on this paper. We especially thank our colleagues and friends from the International NanoSPD Steering Committee for drawing our attention to the major new activities in the field of SPD processing. We apologize to all collaborators whose contributions we may have overlooked. However, their comments on this paper will always be welcome and highly appreciated.

REFERENCES

Valiev RZ, Islamgaliev RK, Alexandrov IV. Bulk nanostructured materials from severe plastic deformation. Prog Mater Sci 2000;45:103-89.

Langdon TG. Twenty-five years of ultrafine-grained materials: Achieving exceptional properties through grain refinement. Acta Mater 2013;61:7035-59.

Z. Horita, K. Edalati, 2020. Severe plastic deformation for nanostructure controls. Mater. Trans. 61:2241

Valiev RZ, Langdon TG. Principles of equal-channel angular pressing as a processing tool for grain refinement. Prog Mater Sci 2006;51:881-981.

Zhilyaev AP, Langdon TG. Using high-pressure torsion for metal processing: fundamentals and applications. Prog Mater Sci 2008;53:893-979.

Estrin Y, Vinogradov A. Extreme grain refinement by severe plastic deformation: a wealth of challenging science. Acta Mater 2013;61:782–817.

A. Rosochowski, Severe Plastic Deformation Technology, 1st edition, Whittles Publishing, 2017

Valiev RZ, Estrin Y, Horita Z, Langdon TG, Zehetbauer MJ, Zhu YT. Producing bulk ultrafine-grained materials by severe plastic deformation. JOM 2006;58(4):33-9.

Beyerlein IJ, Toth LS. Texture evolution in equal-channel angular extrusion. Prog Mater Sci 2009;54:427-510.

. Zehetbauer MJ, Zhu YT, eds, Bulk nanostructured materials. Weinheim, Germany: Wiley; 2009.

Bachmaier A, Pippan R. Generation of metallic nanocomposites by severe plastic deformation. Int Mater Rev 2013;58:41-62

Valiev RZ, Estrin Y, Horita Z, Langdon TG, Zehetbauer MJ, Zhu YT. Fundamentals of superior properties in bulk nanoSPD materials. Mater Res Lett. 2016;4:1-21.

I.A. Ovid'ko, R.Z. Valiev, Y.T. Zhu, Review on superior strength and enhanced ductility of metallic nanomaterials, Progress in Materials Science 94 (2018), pp. 462-540

Straumal BB, Kilmametov AR, Ivanisenko Yu, Mazilkin AA, Kogtenkova OA, Kurmanaeva L, Korneva A, Zięba P, Baretzky B. Phase transitions induced by severe plastic deformation: steady-state and equifinality. Int J Mater Res 2015;106: 657-664.

Figueiredo R, Langdon TG. 2021. Deformation mechanisms in ultrafine-grained etals with an emphasis on the Hall-Petch relationship and strain rate sensitivity. J. Mater. Res. & Tech. 14:137-59

Valiev RZ, Zhilyaev AP, Langdon TG. Bulk nanostructured materials: fundamentals and applications. Hoboken, NJ, USA: Wiley; 2014.

Sabirov I, Enikeev NA, Murashkin MY, Valiev RZ. Bulk nanostructured materials with mutlifunctional properties. MA: Springer; 2015.

Sauvage X, Wilde G, Divinski SV, Horita Z, Valiev RZ. Grain boundaries in ultrafine grained materials processed by severe plastic deformation and related phenomena. Mater Sci Eng A 2012;540:1-12

Straumal BB, Kilmametov AR, López GA, López-Ferreño I, Nó ML, San Juan J, Hahn H, Baretzky B. High-pressure torsion driven phase transformations in Cu–Al–Ni shape memory alloys. Acta Mater 2017;125:274-85

Kilmametov A, Ivanisenko Yu, Mazilkin AA, Straumal BB, Gornakova AS, Fabrichnaya OB, Kriegel MJ, Rafaja D, Hahn H. The α→ω and β→ω phase transformations in Ti–Fe alloys under high-pressure torsion. Acta Mater 2018;144:337

Edalati K, Horita Z. Continuous high-pressure torsion. J Mater Sci 2010;45:4578-82.

Xu C, Schroeder S, Berbon PB, Langdon TG. Principles of ECAP-Conform as a continuous process for achieving grain refinement: Application to an aluminium alloy. Acta Mater 2010;58:1379-86.

L. Mishnaevsky Jr., E. Levashov, R.Z. Valiev, J. Segurado, I. Sabirov, N. Enikeev, S. Prokoshkin, A.V. Solov'yov, A. Korotitskiy, E. Gutmanas, I. Gotman, E. Rabkin, S. Psakh'e, L. Dluhos, M. Seefeldt, A. Smolin. Nanostructured titanium-based materials for medical implants: Modeling and development. Mater Sci Eng R. 2014;81:1-19

G. Faradi, H. Tarabzadeh, Mater. Trans., 2019, p. 1316

. Edalati K, Horita Z. A review on high-pressure torsion (HPT) from 1935 to 1988. Mat Sci Eng A 2016;652:325-52

Bridgman PW. Effects of high shearing stress combined with high hydrostatic pressure. Phys Rev 1935;48:825

Valiev RZ, Kaibyshev OA, Kuznetsov RI, Musalimov RSh, Tsenev NK. Dokl Akad Nauk SSSR (Reports of USSR Academy of Sciences) 1988;301(4):864

Lowe TC, Valiev RZ, editors. Investigations and applications of severe plastic deformation. Dordrecht, The Netherlands: Kluwer Academic Publishers; 2000.

Valiev RZ, Tsenev NK. In: Langdon TG, Merchant HD, Morris JG, Zaidi MA, editors. Hot deformation of aluminium alloys. Warrendale (PA): The Minerals, Metals and Materials Society; 1991. p. 319.

Zhu YT, Valiev RZ, Langdon TG, Tsuji N, Lu K. Processing of nanostructured metals and alloys via plastic deformation. MRS Bulletin 2010;35:977-81.

Whang SH, ed., Nanostructured metals and alloys: processing, microstructure, mechanical properties and applications. Cambridge, UK: Woodhead; 2011.

Rosochowski A, Olejnik L. Incremental equal channel angular pressing for grain refinement. Mater Sci Forum 2011;674:19–28.

Gzyl M, Rosochowski A, Boczkal S, Olejnik L. The role of microstructure and texture in controlling mechanical properties of AZ31B magnesium alloy processed by I-ECAP. Mater Sci Eng A 2015;638:20

Segal VM, Reznikov VI, Kopylov VI, Pavlik DA, Malyshev VF. Processes of structure evolution by plastic deformation in metals. Minsk: Nauka i Tekhnika; 1994.

Raab GI, Valiev RZ, Lowe TC, Zhu YT. Continuous processing of ultrafine grained Al by ECAP–Conform. Mater Sci Eng A 2004;382:30–4.

Ayati V, Parsa MH, Mirzadeh H. Deformation of pure Aluminum along the groove path of ECAP-Conform process. Adv Eng Mater 2015;18:319-23.

Duchek M, Kubina T, Hodek J, Dlouhy J. Development of the production of ultra-fine grained Titanium with the conform equipment. Mater and Technol 2013;47:515–518.

T.C. Lowe, R.Z. Valiev, X. Li, B. Ewing, Commercialization of bulk nanostructured metals and alloys. MRS Bulletin 46 (2021) pp 265-272

Murashkin MYu., Medvedev A, Kazykhanov V, Krokhin A, Raab GI, Enikeev NA, Valiev RZ.  Enhanced mechanical properties and electrical conductivity in ultrafine-grained Al 6101 alloy processed via ECAP-Conform. Metals 2015;5:2148-64.

Harai Y, Edalati K, Horita Z, Langdon TG. Using ring samples to evaluate the processing characteristics in high-pressure torsion, Acta Mater 2009;57:1147-53.

Edalati K, Horita Z. Scaling-up of high pressure torsion using ring shape. Mater Trans 2009;50:92-5.

Fujioka T, Horita Z. Development of high-pressure sliding process for microstructural refinement of rectangular metallic sheets. Mater Trans 2009;50:930-3.

Edalati K, Lee S, Horita Z. Continuous high-pressure torsion using wires. J Mater Sci 2012;47:473–8.

Hohenwarter A. Incremental high pressure torsion as a novel severe plastic deformation process: Processing features and application to copper. Mater Sci Eng A. 2015;626:80-5.

Stolyarov VV, Zhu YT, Lowe TC, Islamgaliev RK, Valiev RZ. A two step SPD processing of ultrafine-grained titanium. Nanostr Mater 1999;11:947-54.

Zhilyaev AP, Langdon TG. Microstructure and microtexture evolution in pure metals after ultra-high straining. J Mater Sci 2012;47:7888-93.

Zhang P, An XH, Zhang ZJ, Wu SD, Li SX, Zhang ZF, Figueiredo RB, Gao N, Langdon TG. Optimizing strength and ductility of Cu-Zn alloys through severe plastic deformation. Scr Mater 2012;67:871-4.

Lugo N, Llorca N, Cabrera JM, Horita Z. Microstructures and mechanical properties of pure copper deformed severely by equal-channel angular pressing and high pressure torsion. Mater Sci Eng A 2008;477:366–71.

Skiba J, Dominiak A, Wiśniewski TS, Pachla W, Kulczyk M, Przybysz S. Influence of severe plastic deformation induced by HE and ECAP on the thermo-physical properties of metals. Key Eng Mater 2015;641:278-85.

Asselli AAC, Leiva DR, Huot J, Kawasaki M, Langdon TG, Botta WJ. Effects of equal-channel angular pressing and accumulative roll-bonding on hydrogen storage properties of a commercial ZK60 magnesium alloy. Int J Hydrogen Energy 2015;40:16971-6.

Murashkin MYu, Enikeev NA, Kazykhanov VU, Sabirov I, Valiev RZ. Physical simulation of cold rolling of ultra-fine grained Al5083 alloy to study microstructure evolution. Rev Adv Mater Sci 2013;35:75-85.

Lima GF, Triques MRM, Kiminami CS, Botta WJ, Jorge Jr AM. Hydrogen storage properties of pure Mg after the combined processes of ECAP and cold-rolling. J Alloys Comp 2014;586:S405-8.

Polyakov AV, Semenova IP, Huang Y, Valiev RZ, Langdon TG. Fatigue life and failure characteristics of an ultrafine-grained Ti-6Al-4V alloy processed by ECAP and extrusion. Adv Eng Mater 2014;16:1038-43

Sabirov I, Perez-Prado MT, Molina-Aldareguia JM, Semenova IP, Salimgareeva GKh, Valiev RZ. Anisotropy of mechanical properties in high-strength ultra-fine-grained pure Ti processed via a complex severe plastic deformation route. Scr Mater 2011;64:69–72.

Gubicza J, Fogarassy Zs, Krallics Gy, Labar J, Torkoly T. Microstructure and mechanical behavior of ultrafine-grained titanium. Mater Sci Forum 2008;589:99-104.

Stepanova ND, Kuznetsova AV, Salishcheva GA, Raab GI, Valiev RZ. Effect of cold rolling on microstructure and mechanical properties of copper subjected to ECAP with various numbers of passes. Mater Sci Eng A 2012;554:105-15.

Fan Z, Jiang H, Sun X, Song J, Zhang X, Xie C. Microstructures and mechanical deformation behaviors of ultrafine-grained commercial pure (grade 3) Ti processed by two-step severe plastic deformation. Mater Sci Eng A 2009;527:45–51.

Sordi VL, Ferrante M, Kawasaki M, Langdon TG. Microstructure and tensile strength of grade 2 titanium processed by equal-channel angular pressing and by rolling. J Mater Sci 2012;47:7870-76.

Latysh VV, Semenova IP, Salimgareeva GH, Kandarov IV, Zhu YT, Lowe TC, Valiev RZ. Microstructure and properties of Ti rods produced by multi-step SPD. Mater Sci Forum 2006;503-504:763-8

Ferguson D, Chen W, Bonesteel T, Vosburgh J. A look at physical simulation of metallurgical processes, past, present and future. Mater Sci Eng A 2009;499:329-32.

Ivanisenko Yu, Kulagin R, Fedorov V, Mazilkin A, Scherer T, Baretzky B, Hahn H. High pressure torsion extrusion as a new severe plastic deformation process. Mat Sci Eng A 2016;664:247-56

Kilmametov A, Ivanisenko Yu, Straumal BB, Mazilkin AA, Gornakova AS, Kriegel MJ, Fabrichnaya OB, Rafaja D, Hahn H. Transformations of α' martensite in Ti–Fe alloys under high pressure torsion. Scripta Mater 2017;136:46-9.

Gleiter H. Nanocrystalline materials. Prog Mater Sci 1989;33:223-315.

Gleiter H. Nanostructured materials: basic concepts and microstructure. Acta Mater 2000;48:1.

P.W.J. Mckenzie, R. Lapovok et al, ECAP with back pressure for optimum strength and ductility in aluminium alloy 6016. Part 1: Microstructure, 58(9):3198-3211

O. Rank, R. Pippan, Mater. Trans., 2019, p.1270

Kolobov YR, Grabovetskaya GP, Ivanov KV, Ivanov MB. Grain boundary diffusion and mechanisms of creep of nanostructured metals. Interface Sci 22002;10(1): 31.

Divinski SV, Reglitz G, Rösner H, Wilde G, Estrin Y. Self-diffusion in Ni prepared by severe plastic deformation: effect of non-equilibrium grain boundary state. Acta Mater 2011;59:1974.

Wilde G, Divinski S., Mater. Trans., 2019, p. 1302.

Raabe D, Herbig M, Sandlöbes S, Li Y, Tytko D, Kuzmina M, Ponge D, Choi P P. Grain boundary segregation engineering in metallic alloys: a pathway to the design of interfaces. Curr Opin Solid State Mater Sci 2014;18:253–61.

Horita Z, Smith DJ, Furukawa M, Nemoto M, Valiev RZ, Langdon TG. An investigation of grain boundaries in submicrometer-grained Al-Mg solid solution alloys using high-resolution electron microscopy. J Mater Res 1996;11:1880.

J. Wang, Z. Horita, M. Furukawa, M. Nemoto, N.K. Tsenev, R.Z. Valiev, Y. Ma and T.G. Langdon, "An Investigation of Ductility and Microstructural Evolution in an Al-3% Mg Alloy with Submicron Grain Size," Journal of Materials Research 8, 2810-2818 (1993)

Schuh A., Lu K., MRS Bulletin, 2021, p.225.

Zhu YT, Liao XZ, Wu XL. Deformation twinning in nanocrystalline materials. Prog Mater Sci 2012;57:1-62.

Zhao Y, Bingert JF, Liao X, Cui B, Han K, Sergueeva AV, Mukherjee AK, Valiev RZ, Langdon TG, Zhu YT. Simultaneously increasing the ductility and strength of ultra-fine-grained pure copper. Adv Mater 2006;18:2949.

Lu K, Lu L, Suresh S. Strengthening materials by engineering coherent internal boundaries at the nanoscale. Science 2009;324:349-52.

Straumal BB, Kogtenkova OA, Gornakova AS, Sursaeva VG, Baretzky B. Review: grain boundary faceting-roughening phenomena. J Mater Sci 2016;51:382-404

Nurislamova GV, Sauvage X, Murashkin MYu, Islamgaliev RK, Valiev RZ. Nanostructure and related mechanical properties of an Al-Mg-Si alloy processed by severe plastic deformation. Phil Mag Lett 2008;88:459.

Liddicoat PV, Liao X-Z, Zhao Y, Zhu YT, Murashkin MY, Lavernia EJ, Valiev RZ, Ringer SP. Nanostructural hierarchy increases the strength of aluminium alloys. Nature Comm 2010;1:63.

Valiev RZ, Enikeev NA, Murashkin MYu, Kazykhanov VU, Sauvage X. On the origin of extremely high strength of ultrafine-grained Al alloys produced by severe plastic deformation. Scripta Mater 2010;63:949.

Sha G., Yao L., Liao X., Ringer S.P., Duan Z.C., Langdon T.G. Segregation of solute elements at grain boundaries in an ultrafine grained Al-An-Mg-Cu alloy, Ultramicroscopy 111 (2011) 500

Valiev RZ, Murashkin MYu, Bobruk EV, Raab GI. Grain refinement and mechanical behavior of the Al alloy, subjected to the new SPD technique. Mater Trans 2009;50:87-91.

Cheng S, Zhao YH, Zhu YT, Ma E. Optimizing the strength and ductility of fine structured 2024 Al alloy by nano-precipitation. Acta Mater 2007;55:5822-32.

Valiev RZ, Murashkin MYu, Sabirov I. A nanostructural design to produce high strength Al alloys with enhanced electrical conductivity. Scripta Mater 2014;76:13-6

Ma K., Zheng Y. Ey al, MRS Bulletin, 2021, p. 2021

Straumal BB, Kilmametov AR, Korneva A, Mazilkin AA, Straumal PB, Zięba P, Baretzky B. Phase transitions in Cu-based alloys under high pressure torsion. J Alloys Comp 2017;707:20-6

Straumal BB, Pontikis V, Kilmametov AR, Mazilkin AA, Dobatkin SV, Baretzky B. Competition between precipitation and dissolution in Cu–Ag alloys under high pressure torsion. Acta Mater 2017;122:60-71

M.V. Petrik, A.R. Kuznetsov, N.A. Enikeev, Yu.N. Gornostyrev, R.Z. Valiev, Peculiarities of interactions of alloying elements with grain boundaries and the formation of segregations in Al-Mg and Al-Zn alloys, Phys Metal Metallogr Vol. 119, No. 10 (2018) pp. 607-612

K. Edalati, Z. Horita, R.Z. Valiev, Transition from poor ductility to room-temperature superplasticity in a nanostructured aluminum alloy, Scientific Reports, (2018) 8:6740

N.Q. Chinh, M.Yu. Murashkin, E.V. Bobruk, J. Labar, J. Gubicza, Z. Kovacs, A.Q. Ahmed, V. Maier-Kiener, R.Z. Valiev, Ultralow-temperature superplasticity and its novel mechanism in ultrafine-grained Al alloys, Mater. Res. Lett. 2021;9:475.

Valiev RZ, Zhu YT. Recent findings in superior strength and ductility of ultrafine-grained materials. Trans MRS - Japan 2015;40:309-18.

Balasubramanian N, Langdon TG. The strength – grain size relationship in ultrafine-grained metals. Metall Mater Trans A 2016;47A:5827-36.

Valiev RZ, Enikeev NA, Langdon TG. Towards superstrength of nanostructured metals and alloys produced by SPD. Kovove Mater 2011;49:1.

Abramova MM, Enikeev NA, Valiev RZ, Etienne A, Radiguet B, Ivanisenko Y, Sauvage X. Grain boundary segregation induced strengthening of an ultrafine-grained austenitic stainless steel. Mater Lett 2014;136:349–52.

Scheriau S, Zhang Z, Kleber S, Pippan R. Deformation mechanisms of a modified 316L austenitic steel subjected to high pressure torsion. Mater Sci Eng A 2011;528:2776–86.

Bobylev S.V., Enikeev N.A., Sheinerman A.G., Valiev R.Z. Strength enhancement induced by grain boundary solute segregations in ultrafine-grained alloys, Int. J. Plast. 123 (2019) 133

Zhu YT, Han BQ, Lavernia EJ. In: Zehetbauer MJ, Zhu YT, editors. Bulk nanostructured materials, Weinheim, Germany: WILEY-VCH Verlag GmbH & Co; 2009, p. 89.

Koch CC. In: Zehetbauer MJ, Zhu YT, editors. Bulk nanostructured materials, Weinheim, Germany: WILEY-VCH Verlag GmbH & Co; 2009, p. 3.

Valiev RZ. Nanostructuring of metals by severe plastic deformation for advanced properties. Nat Mater 2004;3:511-6.

Valiev RZ, Alexandrov IV, Lowe TC, Zhu YT. Paradox of strength and ductility in metals processed by severe plastic deformation. J Mater Res 2002;17:5.

P. Kumar, M. Kawasaki and T.G. Langdon, “Review: Overcoming the Paradox of Strength and Ductility in Ultrafine-Grained Materials at Low Temperatures,” Journal of Materials Science, 51, 7-18 (2016).

M.Y. Alawadhi, S. Sabbaghianrad, Y. Huang and T.G. Langdon, “Evaluating the Paradox of Strength and Ductility in Ultrafine-Grained Oxygen-free Copper Processed by ECAP at Room Temperature,” Materials Science and Engineering, A802, 140546(1-10) (2021).

Islamgaliev RK, Nesterov KM, Bourgon J, Champion Y, Valiev RZ. Nanostructured Cu-Cr alloy with high strength and electrical conductivity. J Appl Phys 2014;115:194301

Murashkin M.Yu., Sabirov I., Sauvage X., Valiev R.Z. Nanostructured Al and Cu alloys with superior strength and electrical conductivity. J Mater Sci 2016;51:33

Lowe TC, Valiev RZ. Frontiers of bulk nanostructured metals in biomedical applications. In: Tiwari A,  Nordin AN, editors. Advanced Biomaterials and Biodevices, Wiley-Scrivener; 2014, p. 3-52

Brunette DM., Tengvall P, Textor M, Thomsen P. Titanium in Medicine. Springer-Verlag, Berlin 2001, p. 1019

Titanium in medical and dental applications, 1st Edition (ed. by F. Froes, M. Qian), Woodhead Publishing 2018, No. of pages 608

Geetha M, Singh AK, Asokamani R, Gogia AK. Ti based biomaterials, the ultimate choice for orthopaedic implants – A review. Prog Mater Sci 2009;54:397-425

R.Z. Valiev, I. Sabirov, E.G. Zemtsova, E.V. Parfenov, L. Dluhoš, T.C. Lowe, Nanostructured commercially pure Ti for development of miniturized biomedical implants, Chapter 4.3 in «Titanium in medical and dental applications», 1st Edition (ed. by F. Froes, M. Qian), Woodhead Publishing 2018, p. 393-417

Valiev RZ, Semenova IP, Latysh VV, Rack H, Lowe TC, Petruzelka J, Dluhos L, Hrusak D, Sochova J. Nanostructured titanium for biomedical applications. Adv Eng Mater 2008;10(8):B15-B17.

Polyakov AV, Dyakonov GS, Semenova IP, Raab GI, Dluhos L, Valiev RZ. Development and study of medical implants made from nanostructured titanium. Adv Biomat and Dev in Med 2015;2:63-9

Semenova IP, Klevtsov GV, Klevtsova NA, Dyakonov GS, Matchin AA, Valiev RZ. Nanostructured titanium for maxillofacial mini-implants. Adv Eng Mater 2016;18(7):1216-24

Estrin Y, Ivanova EP, Michalska A, Truong VK, Lapovok R, Boyd R. Accelerated stem cell attachment to ultrafine grained titanium. Acta Biomater 2011;7:900-6.

An B, Li Z, Diao X, Xin H, Zhang Q, Jia X, Wu Y, Li K, Guo Y. In vitro and in vivo studies of ultrafine-grain Ti as dental implant material processed by ECAP. Mater Sci Eng C 2016;67:34–41

Bagherifard S, Ghelichi R, Khademhosseini A, Guagliano M. Cell response to nanocrystallized metallic substrates obtained through severe plastic deformation. ACS Appl Mater Interfaces 2014;6:7963–85

Park JW, Kim YJ, Park CH, Lee DH, Ko YG, Jang JH, Lee CS. Enhanced osteoblast response to an equal channel angular pressing-processed pure titanium substrate with microrough surface topography. Acta Biomater 2009;5:3272–80

Lai M, Cai K, Hu Y, Yang X, Liu Q. Regulation of the behaviors of mesenchymal stem cells by surface nanostructured titanium. Colloids Surf B Biointerfaces 2012;97: 211–220

Nie FL, Zheng YF, Wei SC, Wang DS, Yu ZT, Salimgareeva GK, Polyakov AV, Valiev RZ. In vitro and in vivo studies on nanocrystalline Ti fabricated by equal channel angular pressing with microcrystalline CP Ti as control. J Biomed Mater Res Part A;2013(101A):1694–707

Elias CN. Titanium dental implant surfaces. Revista Materia 2010;15:138-42

Liu X, Chu PK, Ding C. Surface modification of titanium, titanium alloys, and related materials for biomedical applications. Mater Sci Eng R 2004;47:49

Yao ZQ, Ivanisenko Y, Diemant T, Caron A, Chuvilin A, Jiang JZ, Valiev RZ, Qi M, Fecht HJ. Synthesis and properties of hydroxyapatite-containing porous titania coating on ultrafine-grained titanium by micro-arc oxidation. Acta Biomater 2010;6: 2816–25

Zemtsova EG, Arbenin AY, Valiev RZ, Orekhov EV, Semenov VG, Smirnov VM. Two-level micro-to-nanoscale hierarchical TiO2 nanolayers on titanium surface. Materials 2016;9(12):1010

Nazarov DV, Zemtsova EG, Valiev RZ, Smirnov VM. Formation of micro-and nanostructures on the nanotitanium surface by chemical etching and deposition of titania films by atomic layer deposition (ALD). Materials 2015;8(12)

Estrin Y, Kasper C, Diederichs S, Lapovok R. Accelerated growth of preosteoblastic cells on ultrafine grained titanium. J Biomed Mater Res A 2009;90: 1239

Faghihi S, Zhilyaev AP, Szpunar JA, Azari F, Vali H, Tabrizian M. Nanostructuring of a titanium material by high‐pressure torsion improves pre‐osteoblast attachment. Adv Mater 2007;19:1069-73.

Kim TN, Balakrishnan A, Lee BC, Kim WS, Dvorankova B, Smetana K, Park JK, Panigrahi BB. In vitro fibroblast response to ultra fine grained titanium produced by a severe plastic deformation process. J Mater Sci Mater Med 2008;19:553

Zhang BG, Myers DE, Wallace GW, Brandt M, Choong PFM. Bioactive coatings for orthopaedic implants - recent trends in development of implant coatings. Int J of Molec Sci 2014;15:11878-921

Dorozhkin SV. Calcium orthophosphate deposits: preparation, properties and biomedical applications.  Mater Sci Eng C 2015;55:272-326

Lugovskoy A, Lugovskoy S. Production of hydroxyapatite layers on the plasma electrolytically oxidized surface of titanium alloys. Mater Sci Eng C 2014;43:527-532

E. Parfenov, L. Parfenova, V. Mukaeva, R. Farrakhov, A. Stotskiy, A. Raab, K. Danilko, N. Rameshbabu, R. Valiev, Biofunctionalization of PEO coatings on titanium implants with inorganic and organic substances, Surface Coatings and Technology, vol. 404 (2020) paper no. 126486

R.Z. Valiev, E.V. Parfenov, L.V. Parfenova, Developing nanostructured metals for manufacturing of medical implants with improved design and biofunctionality, Mater Trans, vol. 60, No. 7 (2019) pp 1356-1366

R. Balasubramanian, R. Nagumothu, E. Parfenov, R. Valiev, Development of nanostructured titanium implants for biomedical implants – A short review; Materials Today: Proceedings 46 (2021) 1195-1200

Li H, Zheng Y, Qin L. Progress of biodegradable metals. Prog Nat Sci:Mater Int 2014;24:414-22.

Zheng YF, Gu XN, Witte F. Biodegradable metals. Mater Sci Eng R 2014;77:1–34.

Waizy H, Seitz JM, Reifenrath J, Weizbauer A, Bach FW, Meyer-Lindenberg A,  Denkena B, Windhagen H. Biodegradable magnesium implants for orthopedic applications. J Mater Sci 2013;48:39–50.

Mostaed E, Hashempour M, Fabrizi A, Dellasega D, Bestetti M, Bonollo F, Vedani M. Microstructure, texture evolution, mechanical properties and corrosion behavior of ECAP processed ZK60 magnesium alloy for biodegradable applications. J  Mech Behav Biomed Mater 2014;37:307–22.

S Dobatkin, S Galkin, Y Estrin, V Serebryany, M Diez, N Martynenko, E Lukyanova, V Perezhogin. 2019. Grain refinement, texture, and mechanical properties of a magnesium alloy after radial-shear rolling. J. All. Comp. 774: 969-79

Merson ED, Poluyanov VA, Myagkikh PN, Merson DL, Vinogradov AYu. 2021. Inhibiting stress corrosion cracking by removing corrosion products from the Mg-Zn-Zr alloy pre-exposed to corrosion solutions. Acta Mater. 205: 116570

E.V. Parfenov, O.B. Kulyasova, V.R. Mukaeva, B. Mingo, R.G. Farrakhov, Ya. V. Cherneikina, A. Yerokhin, Y.F. Zheng, R.Z. Valiev, Influence of ultra-fine grain structure on corrosion behaviour of biodegradable Mg-1Ca alloy, Corrosion Science 163 (2020) 108303

Wang J, Tang J, Zhang P, Li Y, Wang J, Lai Y, Qin L. Surface modification of magnesium alloys developed for bioabsorbable orthopedic implants: a general review. J Biomed Mater Res B 2012;100:1691–701.

Valiev RZ, Estrin Y, Horita Z, Langdon TG, Zehetbauer MJ, Zhu YT. Producing bulk ultrafine-grained materials by severe plastic deformation: ten years later. JOM 2016;68:1216-26.

Eagar T. Bringing new materials to market. Tech Rev 1995;98:42–9.