## Slide 1
1. Ag NPrs
2. Add MHA shake 5 minutes
3. Centrifuge to remove excess PVP and TSCD
4. Add TEOS and water
5. Inject into DMA and ethanol solution
6. Stir 30 minutes
7. Add excess ethanol, centrifuge
8. Repeat step 7 x 2
9. Into final BF
Test stability
Amount MHA
Extra purification
Amount of DMA base
Reaction time
Extra purification
Removal of oxygen