Electrokinetic generation of iron-rich barriers in soils: realising the potential for nuclear site management and decommissioning.

Jamie M. Purkisa,Frances Burrella, James R. Brydieb, James Grahamc, Laurence Hopkinsond, and Andrew B. Cundya*

a School of Ocean and Earth Science, University of Southampton, National Oceanography Centre (Southampton), European Way, Southampton, SO14 3ZH, UK

b CanmetENERGY, Natural Resources Canada, Devon, Alberta, T9G 1A8, Canada

c National Nuclear Laboratory, Central Laboratory, Sellafield, Seascale, Cumbria, CA20 1PG, UK

d School of Applied Sciences, University of Brighton, Lewes Road, Brighton, BN2 4GJ, UK

Corresponding author: A.Cundy@soton.ac.uk

SUPPORTING INFORMATION

SI1: Supporting information for Figure 6: Pilot scale experiment, conducted to inform set-up of the large-scale experiment detailed in Figures 3, 4, and 5 of main paper.

Plate electrodes (LWH 0.2 x 28 x 18 cm; anode, mild steel, cathode, stainless steel) were placed in silica sand (14 kg) with 1 mM NaNO3 electrolyte saturated to 50%, with a 50 V electric field (1 V.cm-1) applied, in a 50 x 30 x 20 cm (length x width x height (LWH); 30,000 cm3) container. The electrodes were slightly smaller than the width and depth of the container, 28 cm wide by 18 cm high (504 cm2). Initial current was 110 mA, treatment time was 47 days.

Cathode

plate

Cathode

plate

Anode

plate

Anode

plate

Figure S1 – Experimental set-up for pilot scale (sub-metre) experiment with cathode and anode plates highlighted. Cell dimensions: 50 x 30 x 20 cm LWH.