Synthesis and Characterization of UV Organic Light-Emitting Electrochemical Cells (OLECs) using Phenanthrene Fluorene Derivatives for Flexible Applications.

Sasikumar Arumugama, b, Yi Lia, James E. Pearceb, Katie L. Courta, Edward H. Jackmanb, Oliver J. Wardb, John Tudora, David C. Harrowvenb and Steve P. Beebya*

aSchool of Electronics and Computer Science, University of Southampton, Southampton, UK

SO17 1BJ

bSchool of Chemistry, University of Southampton, Southampton, UK SO17 1BJ

*Corresponding Author, spb@ecs.soton.ac.uk

Scheme 1.  Synthesis of the active fluorene-phenanthrene systems 5a-b

Figure 1. (a) Schematic drawing of the spray coated UV light emission through ITO electrode and (b) UV light top emission device fabricated on self-assembled monolayer (SAM) treated silver glass substrates.

Figure 2. Absorption measurement for solution (a) UV emitters 5a (b) 5b and thin film state for UV emitters (c) 5a and (d) 5b.

Figure 3. Photoluminescent (PL) measurement for solution (a) UV emitters 5a (b) 5b and thin film state for UV emitters (c) 5a and (d) 5b.

Figure 4: cross sectional view SEM images of spray coated UV OLECs (a) on ITO glass substrate, bottom to top, 120 nm thick ITO layer, spin coated 100 nm PEDOT:PSS layer, spin coated 600 nm thick UV emission layer 5a, sputtered 100 nm thick silver top electrode; (b) on ITO glass substrate, bottom to top, 120 nm thick ITO layer, spin coated 100 nm PEDOT:PSS layer, spray coated 600 nm thick UV emission layer 5b, sputtered 100 nm thick silver top electrode;

Figure 5: Current and Voltage sweep (I/V) curve for UV emitters (a) 5a and (c) 5b, on ITO glass substrates. Electroluminescent (EL) spectrum of spray coated OLECs on pre-coated ITO glass slides with (b) 5a (d) 5b.

Table 1: collection of electroluminescent data of UV OLEC devices 1, 2 and 3.

| Devices | EL Peak (nm) | Von (V) | Vmax (V) | Jmax (mA/cm2) | Lmax (µW/cm2) | Lifetime (min) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 394 | 3 | 8 | 190 | 14.52 | <1 |
| 2 | 398 | 3 | 5 | 215 | 20.57 | <1 |
| 3 | 410 | 2.5 | 10 | 195 | 6.28 | <1 |

Table 2: Table shows the device architecture, emission, and their application methods.

| Devices | Device Architecture | Emission | Deposition |
| --- | --- | --- | --- |
| 1 | Glass/ITO/PEDOT:PSS/molecule 5a/Silver | Bottom Emitting | Spin Coating |
| 2 | Glass/ITO/PEDOT:PSS/molecule 5b/Silver | Bottom Emitting | Spray Coating |
| 3 | Glass/silver/ molecule 5b/ PEDOT:PSS/ AgNW | Top Emitting | Spray Coating |

Figure 6: Cross sectional view SEM images of spray coated UV OLECs on silver glass substrate, top to bottom: silver nanowires 100 nm, PEDOT:PSS 50 nm, 5b emission layer 600 nm, SAM treated sputtered silver 100 nm.

Figure 7: Current and Voltage sweep (I/V) curve for UV emitters