Flexible thermoelectric fabrics based on self-assembled tellurium nanowires with a large power factor

Sasikumar Arumugam1*, Samuel Perry2, Iris Nandhakumar2, and Steve Beeby1, Senior Member, IEEE

1Smart Electronic Materials and Systems Research Group, 2School of Chemistry, University of Southampton, UK, *Corresponding author e-mail: sa1d13@soton.ac.uk

Figure 1: SEM images of plain view of P3HT: TeNW (top left) P3HT: TeNW: S2- (top right) P3HT: TeNW:SET, (bottom left) P3HT: TeNW: SPh (bottom right) for 50:50 ratio

| 60:40 Ratio 0.01M | Overnight doping method |  |  | Dip method |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | σ (S/m) | S (µV/K) | PF (µW/mK2) | σ (S/m) | S (µV/K) | PF (µW/mK2) |
| TeNW:P3HT | 412 | 135 | 7.5 | 400 | 135 | 7.2 |
| S2-:P3HT | 109 | 113 | 1.3 | 109 | 113 | 1.3 |
| SET:P3HT | 450 | 127 | 7.2 | 470 | 127 | 7.5 |
| SPh:P3HT | 1840 | 143 | 36.6 | 1840 | 143 | 37.6 |

Figure 2: cross sectional SEM images of P3HT: TeNW (top left) P3HT: TeNW: S2- (top right) P3HT: TeNW:SET, (bottom left) P3HT: TeNW: SPh (bottom right) for 40:60 ratio

| 80:20 Ratio 0.01M | Overnight doping method |  |  | Dip method |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | σ (S/m) | S (µV/K) | PF (µW/mK2) | σ (S/m) | S (µV/K) | PF (µW/mK2) |
| TeNW:P3HT | 400 | 148 | 8.7 | 813 | 135 | 14.8 |
| S2-:P3HT | 109 | 137.6 | 2.0 | 310 | 120 | 4.4 |
| SET:P3HT | 511 | 125.2 | 8.0 | 452 | 125 | 7 |
| SPh:P3HT | 1949 | 143.5 | 40 | 1990 | 140 | 39 |

Figure 3: SEM images of plain (top left) and cross sectional (top right) view of P3HT: TeNW (20:80 ratio) and SEM images of plain (bottom left) and cross sectional (bottom right) view of P3HT: TeNW: S2- (20:80 ratio)

Figure 4: SEM images of plain (top left) and cross sectional (top right) view of P3HT: TeNW:SET (20:80 ratio) and SEM images of plain (bottom left) and cross sectional (bottom right) view of P3HT: TeNW: SPh (20:80 ratio)

| 80:20 Ratio 0.07M | overnight doping method |  |  |
| --- | --- | --- | --- |
|  | σ (S/m) | S (µV/K) | PF (µW/mK2) |
| TeNW:P3HT | 550 | 148 | 12.0 |
| S2-:P3HT | 235 | 140 | 4.6 |
| SET:P3HT | 553 | 130 | 9.3 |
| SPh:P3HT | 2270 | 145 | 47.7 |