Extraction of Attenuation and Backscattering Coefficient along Hollow Core Fiber Length using Two-Way Optical Time Domain Backscattering

Xuhao Wei1, Eric Numkam Fokoua2, Francesco Poletti1, and Radan Slavík1*

1Optoelectronics Research Centre, University of Southampton, Southampton, SO17 1BJ, UK

2Microsoft UK, Romsey, SO51 9DL, UK

KEYWORDS: fiber optics, characterization of hollow-core fiber, backscattering coefficient, distributed loss, Optical Time Domain Reflectometry.

Optical Time Domain Reflectometry (OTDR) is a key technique to characterize fabricated and installed optical fibers. It is also widely used for distributed sensing. OTDR of emerging hollow-core fibers (HCFs) has been demonstrated only very recently, being almost 30 dB weaker than in the glass-core optical fibers. However, it has been challenging to extract useful data from the OTDR traces of HCFs, as the longitudinal variation in the fiber’s geometry, notably the core size or the longitudinal variations of the air pressure within the core result in commensurate changes of the backscattering strength. This is, however, necessary for continuous improvement of HCFs fabrication and subsequently improvement in their performance such as minimum achievable loss, potentially enabling use of HCF in a significantly broader range of applications than used today. Here, we demonstrate, for the first time, that the distributed loss and backscattering coefficient in antiresonant HCFs can be separated, obtaining key data about the fiber distributed loss and uniformity. This is enabled by using OTDR traces obtained from both ends of the HCF.

INTRODUCTION

For today’s conventional optical fibers such as standard single-mode fiber (SMF), optical time domain reflectometry (OTDR) is routinely used both in manufacturing and in installation environments. It provides comprehensive information such as attenuation, position of faults, high loss (e.g., due to excessive bending during installation, dirty connector, or a bad splice), and position of connectors1, 2, all by accessing only one end of the fiber and providing results within minutes.

When interpreting OTDR traces, attenuation is typically extracted from the slope of the measured distributed signal, which originates from Rayleigh backscattering in the fiber glass core that is constant along the fiber length in today’s SMFs.

OTDR has been also used in the emerging low-loss hollow-core fibers (HCFs) such as the (double) nested antiresonant nodeless fibers (NANFs/DNANFs)3, 4. Extracting of attenuation using OTDR presented here has been instrumental in the latest step to finesse their fabrication, resulting in recent lowest  attenuation reported of any optical fiber ever made  at <0.11 dB/km, with preliminary results shown in Ref. 5. In these HCFs, the dominant backscattering mechanism is usually the backscattering from the air/gas in the core region6. Subsequently, the strength of the backscattering signal (characterized by the backscattering coefficient B) can vary due to air pressure/composition within the core along the HCF length, which can change with time as the air can move within the core region7, 8. Further, it has been predicted that the backscattering coefficient also changes with the core size6, which varies at micrometer-level in today’s low-loss HCFs9. This has made evaluation of the distributed HCF attenuation coefficient challenging, as the OTDR signal depends simultaneously on the backscattering coefficient and attenuation, both expected to vary along the fiber length.

Similar phenomena were observed in very early SMFs in which the backscattering coefficient also changed along the fiber length, not allowing the attenuation coefficient to be directly extracted from the OTDR traces. It has been, however, shown that by measuring the OTDR trace from both fiber ends, it is possible to extract the distributed attenuation coefficient and the backscattering coefficient10. Here, we adapt this two-way OTDR measurement technique to measure distributed backscattering coefficient and attenuation coefficient along the low loss antiresonant HCFs. It has already been instrumental in developing world lowest-attenuation HCFs5. Besides introducing this technique, we also show here error analysis of this powerful method, considering measurement errors and found that the measured value of the backscattering coefficient B agrees with predictions made via simulations within the measurement error. Accumulated loss extracted from the OTDR agrees with cut-back measurements, further confirming accuracy of the demonstrated method. The level of achieved accuracy has already proven to be instrumental in further developments of low-loss HCF, with achieved attenuation below that achievable in today’s glass-core fibers. Further attenuation reduction is expected with help of here-presented technique. This is promising to revolutionize capability of science and technology fields that are already using fiber optics (optical communications11, high-power fiber laser 12 or high-power laser delivery13,  etc.), but also empower new fields where current optical fibers have limited use due to their impairments such as quantum communications and computing14.

PRINCIPLE OF TWO-WAY OTDR

We consider a HCF with length L and mark its beginning (z = 0) as “Start of Pull” (SOP) and its end (z = L) as “End of Pull” (EOP), Fig. 1. Subsequently, we consider measuring two OTDR traces when launching OTDR pulses into the SOP (Fig. 1 (a)) and EOP (Fig. 1 (b)) ends, respectively. Example of measured traces using a 2.0-km long HCF sample with NANF geometry (end-face shown as inset in Fig. 1 (a)) is shown in Fig. 1 (c). We refer to this sample as HCF-1 and give further details on it in the Experimental Results section.

In Fig. 1 (c), at first glance, we see both measured traces decreasing along the propagation direction due to the HCF under test attenuation, similarly to OTDR traces of an SMF fiber. More detailed observation, however, shows discrepancies. For example, around z = 1.8 km, EOP launch trace (red, dashed) is almost flat, suggesting very small HCF attenuation, while the SOP launch trace (black, solid) decreases with propagation distance significantly, suggesting high HCF attenuation. As we show later, this is due to the variation in the backscattering coefficient B that in this example decreases with z around z = 1.8 km. This example suggests that the backscattering coefficient and attenuation variation can be separated when analyzing SOP and EOP launch traces, which is confirmed by theoretical analysis shown in the following section.

Fig. 1. OTDR with an SMF pigtail connected into the HCF under test via (a) SOP end (Inset: Cross section of HCF-1 (NANF type)) and (b) EOP end. (c) Measured traces on HCF-1 sample .

ANALYSIS OF TWO-WAY OTDR

Derivations. The backscattered power received from the SOP and EOP launch can be expressed as:

|  | PSOPz=PSOP0Bze-20zαudu, | (1) |
| --- | --- | --- |

|  | PEOPz=PEOP0Bze-2ZLαudu. | (2) |
| --- | --- | --- |

Here, P0 is the launched power into the HCF from SOP (subscript “SOP”) and EOP (subscript “EOP”) ends, respectively. Bz and αz are backscattering and attenuation coefficients at point z along the HCF.

By applying natural logarithm and summing Eq. (1) and (2), we obtain:

|  | lnPSOPz+lnPEOPz= lnPSOP0+lnPEOP0+2lnBz -20Lαudu. | (3) |
| --- | --- | --- |

By defining A=0Lαudu as the total HCF loss, we can obtain the backscattering coefficient from Eq. (3) as:

|  | Bz=exp⁡(12lnPSOPz+12lnPEOPz -12lnPSOP0-12lnPEOP0+A). | (4) |
| --- | --- | --- |

When all variables are converted into dB, we obtain:

|  | BzdB=12(PSOPzdB+PEOPzdB) -12(PSOP, dB0+PEOP, dB0)+AdB. | (5) |
| --- | --- | --- |

Subsequently, accumulated loss is obtained from Eq. (1) and (4):

|  | 0zαudu=14lnPEOPz-lnPSOPz-lnPEOP0+lnPSOP0+12A. | (6) |
| --- | --- | --- |

In dB it is then:

|  | 0zαududB=14PEOPzdB-PSOPzdB +14(PSOP, dB0-PEOP, dB0)+12AdB. | (7) |
| --- | --- | --- |

The HCF attenuation coefficient at point z is then obtained from the derivate of Eq. (7):

|  | αzdB=ddz 0zαududB =14ddzPEOPzdB- ddzPSOPzdB . | (8) |
| --- | --- | --- |

The backscattering coefficient BzdB is then evaluated using Eq. (5), where the total HCF loss AdB is evaluated from Eq. (7) by putting z = L.

Practical considerations and calibration. The first practical consideration regards the differentiation of data measured experimentally to obtain attenuation coefficient from Eq. (8), as differentiation of noisy experimental data usually produce large noise variation. We will use approach adopted in analysis of the SMF OTDR traces in which the accumulated loss of 0zαududB given in Eq. (7) is first fitted with a polynomial, and it is subsequently differentiated to obtain the attenuation coefficient αzdB.

To find PSOPzdB and PEOPzdB, we need to calibrate our OTDR, for which we use a 3.5% Fresnel back-reflection from the flat-cleaved SMF, Fig. 2 (a). Subsequently, we evaluate all quantities relative to the powers expected inside the SMF at its output: this point is shown in Fig. 2 (b) as Pref. The detail of calibration will be shown later.

Further, we need to derive the backscattering coefficient (Eq. (5)) from the quantities that can be measured experimentally rather than PSOP, dB0, PEOP, dB0, and AdB used in Eq. (5). We consider experimentally-measurable quantities of power at the launching SMF output,  Pa (Fig. 2 (b)) and at the output of the HCF under test (Fig. 2 (c)), Pb. Below we show derivation for SOP launch, as EOP launch can be treated identically. Firstly, the difference between the power measured after and before the HCF under test is due to the HCF loss AdB and coupling loss CdB (Fig. 2 (c)):

|  | PSOP, dBa-PSOP,dBb=CdB+AdB. | (9) |
| --- | --- | --- |

Further, light propagating in the SMF tail experiences two times coupling loss (2CdB) when backscattered plus Fresnel loss FdB (FdB = 0.15 dB) when entering SMF into the HCF:

|  | PSOP,dB0=PSOP,dBa-2CdB-FdB. | (10) |
| --- | --- | --- |

Note that the Fresnel loss for the SMF-HCF direction is already accounted for, as Pa is measured after light experience this Fresnel loss in the forward direction (Pref,dB=PdBa+FdB). Eq. (9) and Eq. (10) lead to:

|  | PSOP, dB0=2PSOP, dBb-PSOP,dBa+2AdB-FdB, | (11) |
| --- | --- | --- |

and similarly for the opposite direction:

|  | PEOP,dB0=2PEOP,dBb-PEOP,dBa+2AdB-FdB. | (12) |
| --- | --- | --- |

We now can evaluate the total HCF loss AdB by using Eq. (7) and putting z = L:

| AdB=0LαududB =14PEOP,dBL-PSOP,dBL +14PSOP,dB0-PEOP,dB0+12AdB, giving: | (13) |
| --- | --- |
| AdB=12PEOP,dBL-PSOP,dBL +12(PSOP,dB0-PEOP,dB0). | (14) |

Using Eq. (11) and (12) to replace PSOP,dB0 and PEOP,dB0 in Eq. (14) we get:

| AdB=12PEOP,dBL-PSOP,dBL +122PSOP,dBb-PSOP,dBa-2PEOP,dBb+PEOP,dBa. | (15) |
| --- | --- |

We then put Eq. (11), (12), and (15) into Eq. (5) to obtain the backscattering coefficient from measured quantities:

|  | BzdB=12PSOP,dBz+12PEOP,dBz +PSOP,dBa-2PSOP,dBb+12PSOP,dBL -12PEOP,dBL+FdB. | (16) |
| --- | --- | --- |

The accumulated loss A(z)dB can be then obtained from Eq. (7) using Eq. (11), (12), and (15) as:

|  | A(z)dB=14PEOP,dBz-PSOP,dBz +12(2PSOP,dBb-PSOP,dBa-2PEOP,dBb +PEOP,dBa)+14(PEOP,dBL-PSOP,dBL). | (17) |
| --- | --- | --- |

In regards to the attenuation coefficient αzdB,  Eq. (8), it does not require PSOP,dB0, PEOP,dB0 or AdB and even calibration of the OTDR is not necessary.

Now, having all the parameters of interest related directly to the measurable quantities, we can estimate accuracy with which we can evaluate them.

Fig. 2. Set-up for calibrating the OTDR instrument (a) and to measure powers of  Pa b,Pb (c) used to evaluate quantities of PSOP0 or  PEOP0.

Error analysis. Firstly, we estimate measurement errors. To evaluate the error of the OTDR measurements of PSOP,dBz and PEOP,dBz, we performed repeated measurements of the HCF-1 sample, Fig. 3. The peak-to-peak variation between the traces at any given distance z is below 0.4 dB. Thus, we estimate uncertainty in measuring PSOP,dBz  and PEOP,dBz as ±0.2 dB. The error of the measured powers of PSOP,dBa, PEOP, dBa, PSOP,dBb, and PEOP,dBb is given by the accuracy of the used power meter, which is given by the manufacturer as ±5%, corresponding to ±0.2 dB.

Fig. 3. Six backscattering traces measured on HCF-1 sample.

With the above estimation of the measurement errors, the error in evaluated BzdB given by Eq. (16), calculated as peak-to-peak errors (all errors summed up) is as follows:

|  | ±ΔBzdB=±(0.5×0.2+0.5×0.2+ 0.2+2×0.2+0.5×0.2+0.5×0.2)=±1.0 dB. | (18) |
| --- | --- | --- |

In regards to error in αzdB, it does not contain directly any of the measured powers (Eq. (8)) and thus their error should not contribute to the error in αzdB. It also does not contain the OTDR data directly, but only their derivatives (Eq. (8)), which we will smooth out by performing earlier-mentioned polynomial fit. Thus, we expect the error in αzdB will depend dominantly on the quality/accuracy of this polynomial fit. Other parasitic effects may also play a role, e.g., when measuring an HCF with sub-atmospheric air pressure inside, air will be getting in during the measurement. This could be reduced by measuring OTDR from both ends simultaneously using two instruments. The most important conclusion, however, is that the accuracy of  αzdB is not influenced by accuracy of any measured powers and being so, it can be significantly more accurate than accuracy of the power measurements, making this method potentially very accurate.

OTDR System. The custom OTDR system we built for measuring the backscattering in HCFs is shown in Fig. 4, and was firstly demonstrated Ref. 3. To enhance the overall sensitivity of the OTDR (FOTR-203 from FS.com), the OTDR pulses were amplified before injecting them into the HCF under test. This was achieved by employing a "Pulse Amplification" unit with two inline optical circulators that ensure the backscattered signal is directed back into the OTDR instrument. Detailed discussion can be found in Ref. 3.

Fig. 4. (a) The setup of the used highly sensitive OTDR system and (b) the detail of the implemented Pulse Amplification unit. PD: photodetector, AOM: acousto-optic modulator, BPF: bandpass filter.

Using this OTDR system, the launched pulses were amplified by more than 28 dB, enabling measurement of the backscattering signal in HCFs with spatial resolution of 1.5 m (10 ns pulses), as demonstrated in Ref. 3.

OTDR Calibration. We calibrate the OTDR following the procedure shown in Fig. 2 (a), where we used 10 ns flat-top pulses. The measured OTDR trace is in Fig. 5. As the 3.5% reflection (corresponding to -14.5 dB) is very strong and beyond the dynamic range of the OTDR detector, we placed a variable optical attenuator at the output and set it to 20.0 dB by comparing the output power with and without the attenuator. This reduced the back-reflected light by 40.0 dB, as light pass through the attenuator in both directions. The detected peak from the 3.5% back-reflecting end-facet should thus be -14.5-40.0= -54.5 dB below light launched into the fiber, as schematically shown in red in Fig. 5. As we measured the back-reflected peak of -37.2 dB (Fig. 5), we need to subtract 17.3 dB from the measurement of -37.2 dB to obtain the correct value of -54.5 dB. 17.3 dB is thus our calibration constant of the OTDR relative trace.

In Fig. 5 we see that the backscattering from the SMF is 15.8 dB below that of the 3.5% end-facet. As the used 10 ns pulse length corresponds to OTDR signal received from 1 m of SMF, we get the backscattering coefficient of the SMF after our calibration as -54.5 – 15.8 = -70.3 dB/m, shown in red in Fig. 5. This value is consistent with SMFs15, providing us with verification of the calibration as well as providing us with accurate value of the backscattering coefficient of our SMF.

Fig. 5. The measured backscattering from the SMF pigtail and Fresnel reflection (attenuated by 40 dB) at its end.

The above calibration gives us relative powers (in dB), however, we also require absolute powers (in dBm) for evaluation of BzdB and AzdB, Eq. (16) and (17). To obtain it, we measured pulse power of Pref=Pa+0.15=41.65 dBm. Thus, the Fresnel reflection that is expected at -54.5 dB below power of 41.65 dBm is -12.85 dBm, which gives us absolute calibration of the OTDR traces. The calibrated measured trace from Fig. 5 in absolute power (dBm) is then shown in Fig. 6.

Fig. 6. The calibration of the measured backscattering from the SMF pigtail and Fresnel reflection (attenuated by 40 dB) at its end.

EXPERIMENTAL RESULTS

Used samples. To demonstrate the capability and accuracy of the developed technique, we characterized three HCF samples, which we mark as HCF-1, HCF-2, and HCF-3, Table 1. The core sizes we refer to are those measured at one of the HCF sample end-facets analyzing SEM (Scanning Electron Micrograph) images.

Table 1. Parameters of characterized HCFs.

| Sample | HCF-1 | HCF-2 | HCF-3 |
| --- | --- | --- | --- |
| Type | NANF | NANF | DNANF |
| Core size, µm | 34.7 | 31.0 | 26.7 |
| Length, km | 2.0 | 0.68 | 6.5 |
| Air pressure, atm | 1 | 1 | 0.25* |

* Close-to “as-drawn”, which has sub-atmospheric air pressure. Value estimated based on backscattering level6.

The HCF-2 sample that has relatively large bending loss was initially measured on a standard fiber bobbin (diameter of 16 cm) and subsequently rewound and remeasured on a large bobbin (diameter of 32 cm).

Measured OTDR traces (calibrated). We measured the backscattering in HCF-1, HCF-2, and HCF-3, and calibrated them as described earlier, as shown in Fig. 7. We removed data at both ends of the samples to avoid the influence from the dead zone of the instrument.

Fig. 7. Calibrated backscattering traces when launching light from the SOP and EOP for (a) HCF-1, (b) HCF-2 on a small (solid) and large (dashed) bobbin, and (c) HCF-3.

Attenuation coefficient. We calculated accumulated loss as described earlier when discussing Eq. (17) and Eq. (8). Results are shown in Fig. 8 for all three HCF samples. To obtain attenuation coefficients, we first fitted this accumulated loss data with a polynomial function and subsequently differentiated it. All accumulated loss traces were fitted by the 1st, 2nd, ... order polynomials and the Coefficient of Determination (R2) was obtained for each fit. Subsequently, we used fit with the polynomial order from which R2 did not change within four digits. For example, for HCF-1, the R² values were 0.9932, 0.9956, 0.9972, and 0.9972 for the 1st, 2nd, 3rd, and 4th order polynomial fit, respectively. Subsequently, we chose the 3rd order, as R2 did not change between the 3rd and 4th order. We repeated this analysis for HCF-2 and HCF-3 samples, which suggested using cubic fit for all three measured samples, all shown in Fig. 8. The attenuation coefficients profiles (derivatives of the fitted curves) are then shown in Fig. 9 (a-c).

Fig. 8. The accumulated loss for all three HCF samples and their 3rd order polynomial fits (red dashed lines).

Backscattering coefficient. The backscattering coefficients of the three samples are then calculated using Eq. (16) and are shown in Fig. 10. A variation of about ±0.5 dB along the length is observed for all three samples. This can be caused by the core size variations 6 or air pressure variation inside the core 7. In Fig. 10 (b), backscattering coefficient for the HCF-2 sample spooled on different size bobbins (having different attenuation coefficients) shows remarkably similar value, showing negligible cross-sensitivity of the attenuation changes on the evaluation of the backscattering coefficient.

DISCUSSION

We compare the attenuation coefficients obtained from the two-way OTDR analysis to average attenuation coefficient obtained via cutback method, Table 2. Results for HCF-1 and HCF-3 show good agreement between the two techniques. For HCF-2, the fiber has been re-wound between the measurements to a smaller and back to a larger spool, which may have slightly altered the attenuation, possibly explaining the OTDR result to be slightly higher than expected from the cut-back method.

Fig. 9. Attenuation coefficients for (a) HCF-1, (b) HCF-2, and (c) HCF-3.

Table 2. Attenuation coefficient extracted from the OTDR measurement and its comparison to average attenuation coefficient measured by cutback method.

| Sample | Attenuation coefficient variation along the length, OTDR, dB/km | Average attenuation coefficient from Cutback, dB/km |
| --- | --- | --- |
| HCF-1 | 0.69 – 1.20 | 0.85±0.03 |
| HCF-2 | 0.66 – 0.96 (32-cm) | 0.6±0.1 |
| HCF-3 | 0.17 – 0.25 | 0.21±0.01 |

Fig. 10. Backscattering coefficients for (a) HCF-1, (b) HCF-2, and (c) HCF-3.

We also compare the obtained backscattering coefficients with the prediction6, as shown in Fig. 11 and Table 3. The stars shown in Fig. 11 are the backscattering coefficient level at SOP sides. The uncertainties are marked in color regions, which combines the variation of backscattering coefficient shown in Fig. 10 along the HCF samples lengths and the error of ±1 dB we analyzed earlier. The core size range is estimated based on the relationship between backscattering coefficient variation and core size predicted in Ref. 6 (here we use 0.25 µm/dB for the calculation). For HCF-1 and HCF-2, both at atmospheric-pressure air-filled, they agree with the prediction. The HCF-3 shows a lower backscattering coefficient; however, we know that this sample was sealed after the fiber draw and thus the air pressure inside it is expected below 1 atm, qualitatively in line with our measurement. As its backscattering coefficient is about 6 dB lower than expected, we estimate air pressure inside this sample of 0.25 atm, which is consistent with earlier reports showing as-drawn HCFs to have air pressure as low as 0.2 atm16.

Fig. 11. Comparison between the extracted backscattering coefficient of three samples and the predicted value in Ref. 6.

Table 3. Backscattering coefficient extracted from the OTDR measurement and its comparison to the prediction in Ref. 6.

|  | Backscattering coefficient variation along the length + uncertainty, OTDR, dB/m | Backscattering coefficient from theory (1 atm) dB/m |
| --- | --- | --- |
| HCF-1 | -99.9 – -97.2 | -100.3 – -99.6 |
| HCF-2 | -99.3 – -96.2 (32-cm) | -99.6 – -98.4 |
| HCF-3 | -104.9 – -102.2* | -98.1 – -97.2 |

* HCF-3 had sub-atmospheric pressure, as it has been “as drawn”.

CONCLUSION

We have demonstrated that an HCF’s distributed attenuation and backscattering coefficients can be accurately obtained from OTDR traces by using two-way OTDR measurement. By analyzing in detail three low loss antiresonant HCFs, we demonstrated the capability of the used method in separating loss from backscattering coefficient variation. In terms of loss, we obtained good agreement between the loss extracted via two-way OTDR and the cutback method. Slight variation of the attenuation coefficient along the length (e.g., between 0.17 and 0.25 dB/km over 6.5-km HCF-3 sample length) can be useful in developing low-loss HCFs. In terms of the backscattering coefficient, we achieved a close agreement with values expected from simulations6. The observed slight variation along the length can be attributed to air pressure variations or HCF core size variation6, suggesting this method can give direct insight into the longitudinal uniformity of the drawn HCFs, providing valuable feedback to their manufacturing as well as quality. We believe the demonstrated method will be powerful tool in further development of HCFs, enabling approaching their fundamental limits and providing next-generation optical fibers to a multitude of applications including optical communications and manufacturing, but also fields of long-distance distributed sensing or unamplified transmission of qubits over large distances.

ASSOCIATED CONTENT

AUTHOR INFORMATION

Corresponding Author

Radan Slavík - r.slavik@soton.ac.uk

Present Addresses

Xuhao Wei - Optoelectronics Research Center (ORC), University of Southampton, Southampton, SO17 1BJ, UK.

Eric Numkam Fokoua - Microsoft UK, Romsey, SO51 9DL, UK.

Francesco Poletti - Optoelectronics Research Center (ORC), University of Southampton, Southampton, SO17 1BJ, UK.

Radan Slavík - Optoelectronics Research Center (ORC), University of Southampton, Southampton, SO17 1BJ, UK.

Funding Sources

EPSRC Airguide (EP/P030181/1), VACUUM (EP/W037440/1), and FASTNET (EP/X025276/1).

ACKNOWLEDGMENT

The data underpinning the research presented are accessible through the University of Southampton research repository (DOI: 10.5258/SOTON/P1182). For the purpose of open access, the author has applied a creative commons attribution (CC BY) license to any author accepted manuscript version arising.

References

(1) Barnoski, M.; Jensen, S. Fiber waveguides: a novel technique for investigating attenuation characteristics. Appl. Opt. 1976, 15 (9), 2112-2115.

(2) Barnoski, M. K.;  Rourke, M. D.;  Jensen, S.; Melville, R. Optical time domain reflectometer. Appl. Opt. 1977, 16 (9), 2375-2379.

(3) Wei, X.;  Shi, B.;  Richardson, D. J.;  Poletti, F.; Slavík, R. Distributed Characterization of Low-loss Hollow Core Fibers using EDFA-assisted Low-cost OTDR instrument, Optical Fiber Communication Conference (OFC), 2023, W1C. 4.

(4) Slavík, R.;  Fokoua, E. R. N.;  Bradley, T. D.;  Taranta, A. A.;  Komanec, M.;  Zvánovec, S.;  Michaud-Belleau, V.;  Poletti, F.; Richardson, D. J. Optical time domain backscattering of antiresonant hollow core fibers. Opt. Express 2022, 30 (17), 31310-31321.

(5) Chen, Y.; Petrovich, M. N.; Numkam Fokoua, E.; Adamu. A. I.; Hassan, M.R.A.; Sakr, H,; Slavík, R.; Bakhtiari Gorajoobi. S.; Alonso, M.; Fatobene Ando, R.; Papadimopoulos, A.; Varghese, T.; Wu, D.; Fatobene Ando, M.; Wisniowski, K.; Sandoghchi, S. R.;  Jasion, G. T.; Richardson, D.J.; Poletti, F. Hollow Core DNANF Optical Fiber with <0.11 dB/km Loss. Optical Fiber Communication Conference (OFC), 2024, Th4A.8.

(6) Numkam Fokoua, E.;  Michaud-Belleau, V.;  Genest, J.;  Slavík, R.; Poletti, F. Theoretical analysis of backscattering in hollow-core antiresonant fibers. APL Photonics 2021, 6 (9).

(7) Wei, X.;  Shi, B.;  Wheeler, N. V.;  Horak, P.;  Poletti, F.; Slavík, R. Distributed Monitoring of Evacuation of Hollow Core Fibers. Frontiers in Optics + Laser Science, 2023, FTu1D.1.

(8) Elistratova, E.;  Kelly, T. W.;  Davidson, I. A.;  Sakr, H.;  Bradley, T. D.;  Taranta, A.;  Poletti, F.;  Slavík, R.;  Horak, P.; Wheeler, N. V. Distributed measurement of hollow-core fiber gas filling and venting via optical time-domain reflectometry, Conference on Lasers and Electro-Optics Europe & European Quantum Electronics Conference (CLEO/Europe-EQEC), 2023, ce_2_4.

(9) Budd, L.;  Taranta, A.;  Fokoua, E. N.; Poletti, F. Longitudinal Non-Destructive Characterization of Nested Antiresonant Nodeless Fiber Microstructure Geometry and Twist, Optical Fiber Communication Conference (OFC), 2023, W4D.2.

(10) Di Vita, P.; Rossi, U. Backscattering measurements in optical fibers: separation of power decay from imperfection contribution. Electronics Letters 1979, 15 (15), 467-469.

(11) Agrell, E.;  Karlsson, M.;  Poletti, F.;  Namiki, S.;  Chen, X. V.;  Rusch, L. A.;  Puttnam, B.;  Bayvel, P.;  Schmalen, L.; Tao, Z. Roadmap on optical communications. Journal of Optics 2024, 26 (9), 093001.

(12) Nampoothiri, A. V.;  Jones, A. M.;  Fourcade-Dutin, C.;  Mao, C.;  Dadashzadeh, N.;  Baumgart, B.;  Wang, Y.;  Alharbi, M.;  Bradley, T.; Campbell, N. Hollow-core optical fiber gas lasers (HOFGLAS): a review. Optical Materials Express 2012, 2 (7), 948-961.

(13) Cooper, M.;  Wahlen, J.;  Yerolatsitis, S.;  Cruz-Delgado, D.;  Parra, D.;  Tanner, B.;  Ahmadi, P.;  Jones, O.;  Habib, M. S.; Divliansky, I. 2.2 kW single-mode narrow-linewidth laser delivery through a hollow-core fiber. Optica 2023, 10 (10), 1253-1259.

(14) Antesberger, M.;  Richter, C. M.;  Poletti, F.;  Slavík, R.;  Petropoulos, P.;  Hübel, H.;  Trenti, A.;  Walther, P.; Rozema, L. A. Distribution of telecom entangled photons through a 7.7 km antiresonant hollow-core fiber. Optica Quantum 2024, 2 (3), 173-180.

(15)https://www.corning.com/media/worldwide/coc/documents/Fiber/product-information-sheets/PI-1424-AEN.pdf.

(16) Rikimi, S.;  Chen, Y.;  Kelly, T. W.;  Davidson, I. A.;  Jasion, G. T.;  Partridge, M.;  Harrington, K.;  Bradley, T. D.;  Taranta, A. A.; Poletti, F. Internal gas composition and pressure in as-drawn hollow core optical fibers. J. Lightwave Technol. 2022, 40 (14), 4776-4785.