WPPF Analysis Results

# General information

| Analysis date | 2024/08/15 09:56:15 |  |  |
| --- | --- | --- | --- |
| Sample name |  | Measurement date | 2024/08/15 09:47:16 |
| File name | XRD_SAPO11_Calcined_Large_Batch.txt | Operator |  |
| Comment |  |  |  |

# Qualitative analysis results

| Phase name | Formula | Space group | Phase reg. detail | DB card number | Content(%) |
| --- | --- | --- | --- | --- | --- |
| O80 Si40 | O80 Si40 | 74 : Imma | CIF file | - | 100 |

# Lattice parameters

| Phase name | a(A) | b(A) | c(A) | alpha(deg) | beta(deg) | gamma(deg) | V(A^3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| O80 Si40 | 8.3102(13) | 18.304(3) | 13.388(2) | 90.000000 | 90.000000 | 90.000000 | 2036.5(6) |

# Crystallite size and lattice strain

| Phase name | Crystallite size(A) | Distribution RSD | Strain(%) | Distribution type |
| --- | --- | --- | --- | --- |
| O80 Si40 | 194(3) | - | 0.46(14) | - |