WPPF Analysis Results

# General information

| Analysis date | 2024/08/06 15:29:54 |  |  |
| --- | --- | --- | --- |
| Sample name |  | Measurement date | 2023/07/11 17:06:14 |
| File name | XRD_SAPO11_Calcined.txt | Operator |  |
| Comment |  |  |  |

# Qualitative analysis results

| Phase name | Formula | Space group | Phase reg. detail | DB card number | Content(%) |
| --- | --- | --- | --- | --- | --- |
| O80 Si40 | O80 Si40 | 74 : Imma | CIF file | - | 100 |

# Lattice parameters

| Phase name | a(A) | b(A) | c(A) | alpha(deg) | beta(deg) | gamma(deg) | V(A^3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| O80 Si40 | 8.3854(14) | 18.501(4) | 13.537(2) | 90.000000 | 90.000000 | 90.000000 | 2100.2(7) |

# Crystallite size and lattice strain

| Phase name | Crystallite size(A) | Distribution RSD | Strain(%) | Distribution type |
| --- | --- | --- | --- | --- |
| O80 Si40 | 398(16) | - | 0.27(11) | - |