WPPF Analysis Results

# General information

| Analysis date | 2024/08/09 10:38:39 |  |  |
| --- | --- | --- | --- |
| Sample name |  | Measurement date | 2023/07/06 14:11:00 |
| File name | XRD_SAPO11_Calcined_Dried_Batch2_0_1Si_9417_094D_06Jul23.txt | Operator |  |
| Comment |  |  |  |

# Qualitative analysis results

| Phase name | Formula | Space group | Phase reg. detail | DB card number | Content(%) |
| --- | --- | --- | --- | --- | --- |
| O80 Si40 | O80 Si40 | 74 : Imma | CIF file | - |  |

# Lattice parameters

| Phase name | a(A) | b(A) | c(A) | alpha(deg) | beta(deg) | gamma(deg) | V(A^3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| O80 Si40 | 8.386890 | 18.520950 | 13.531200 | 90.000000 | 90.000000 | 90.000000 | 2101.844285 |

# Crystallite size and lattice strain

| Phase name | Crystallite size(A) | Distribution RSD | Strain(%) | Distribution type |
| --- | --- | --- | --- | --- |
| O80 Si40 | 787(30) | - | 0.557(19) | - |