# Stabilisation of FeCoNiCuPt high-entropy alloy nanopar- ticles by surface capping†

Anurag Sharma,a and Andrew L. Hector ∗a

High-entropy alloys (HEA) are a distinct class of materials made up of multiple principal compo- nents (≥5) in near-equimolar ratios, resulting in extraordinary properties, including high catalytic activity, corrosion and oxidation resistance, and tunable magnetic properties. In nanoparticle form, these alloys are highly promising for a variety of advanced applications such as catalysis, magnetic storage, and biomedical technology [Zoubi et al., Nano Energy, 2023, 110, 108362]. This study used isolating medium-assisted solid-state reaction to synthesise FeCoNiCuPt HEA nanoparticles with ultrafine NaCl particles as the isolating medium [Meng et al., Mater. Adv., 2024, 5, 719]. The nanoparticles were stabilised with a range of hydrophobic and hydrophilic capping agents such as

polyethylinimine, Polyvinylpyrrolidone, stearic acid, octadecylamine etc, introduced before or after the removal of the isolating medium. The formation of single-phase nanoparticles & chemical com- position of FeCoNiCuPt was validated by X-ray diffraction & energy-dispersive X-ray spectroscopy. Transmission electron microscopy and dynamic light scattering were used to determine particle sizes, effective capping agent thickness, and particle stability. The results highlight the successful synthesis of FeCoNiCuPt nanoparticles, effect of capping agents on the control of particle size, and the sta- bility of capped nanoparticle suspensions in water and organic solvents. The study emphasises the importance of selecting the appropriate capping agent to maintain nanoparticle stability and prevent agglomeration.

and found strong ferromagnetism with low coercivity values (< 1000 Am−1) 3. The FeCoNiTiAl HEA synthesised by Xiang Liu demonstrated good nonlinear optical features at 1030 and 1560 nm and has significant potential for progress in the pulsed laser field in harsh environments 4. The FeCoNi-based HEA developed by Y. Liao can absorb light across the spectrum (250–2500 nm), demonstrating 99% photothermal conversion efficiency under 1 solar irradiation 5. FeCoNiCuPt performs exceptionally well in the methanol oxidation and hydrogen evolution reactions and shows

2.70 times more electrochemically active surface area compared to a commercial Pt/C catalyst 2. FeCoNiCuIr HEA also performs well in the oxygen evolution process, attaining a low overpoten-

tial of 360 mV at 10 mA·cm−2 and retaining >94% of the current

after 10 hours 6. These examples demonstrate the remarkable

magnetic, optical & catalytic capabilities of FeCoNi-based HEAs.

# Introduction

High-entropy alloys (HEA) are made up of several elements (≥ 5) in about an equimolar ratio (with 5% to 35% variability) 1. J. W. Yeh describes a "high-entropy alloy" as an alloy material with the maximum mixing entropy, resulting in solid solution phases, un- like other non-equiatomic compositions 1,2. HEA with transition metals like Fe, Co, and Ni have attracted special attention be- cause of their optical, photonic, catalytic, & magnetic properties. Bazioti investigated a series of materials based on FeCoNiAlMnx

a School of Chemistry and Chemical Engineering, University of Southampton, Highfield, Southampton, United Kingdom

∗ Corresponding author: Email, a.l.hector@soton.ac.uk

† Supplementary Information available: See DOI: 00.0000/00000000.

HEAs perform noticeably better when synthesised as nanopar- ticles. Compared to their bulk counterparts, their physical and chemical properties change dramatically as the surface-to- volume ratio, structural disorder, and quantum confinement ef- fect increase. When Pan et al. loaded FeCoNiMnCr nanoparti- cles into N-doped carbon nanotubes, zinc-air batteries demon- strated improved stability (200 hours) and power density (214 mW·cm−2) compared to bulk FeCoNiMnCr because of their larger surface area and constituent element interaction 7. FeCoNiM- nCr nanoparticles outperformed bulk FeCoNiMnCr in bifunctional oxygen reaction activity applications because they offer more ac- tive sites and tunable surface chemistry 7. Debabrata Das syn- thesised NbCrTaVW HEA nanoparticles and bulk and discovered that when the bulk alloy was milled to ∼12 nm crystallite size, it

changed from being diamagnetic to superparamagnetic 8, show- ing small coercivity ( ∼0) and saturation magnetisation approach- ing ∼7 emu·g−1. Larger bulk domains fragmented and acted as superparamagnetic spins as particle size reduced to nanoscale 8. Overall, FeCoNi-based HEA nanoparticles are a promising re- search field and an important material class for future functional nanomaterials.

Smaller nanoparticles exhibit novel quantum effects and change the electronic structure of HEA materials, but their greater surface energy causes Ostwald ripening, aggregation, and sur- face energy reduction. Uncontrolled nanoparticle aggregation harms its applications and must be prevented 9. Even though HEA nanoparticles have tremendous potential, stabilising colloids and preserving small particle size during processing after synthesis and storage is challenging. In particular, HEA nanoparticles made via solid-state techniques tend to settle or aggregate together over time, especially when dissolved in solvents like ethanol 9. Upama Das also found that nanoparticle suspension stability depends on solvent choice. In ethanol and acetone, nanoparticles were seen to grow and aggregate instantly 10. Thus, nanoparticle stability, dispersibility, and physical property tunability necessitate efficient surface capping.

Surfactants, ligands, and polymers were being utilised to cap nanoparticles to control Ostwald ripening, particle size, shape, and stability 11. These compounds inhibit nanoparticle growth and aggregation by binding to and lowering surface en- ergy 12. Thiols, amines, and surfactants like oleylamine, oleic acid, and PEG derivatives are common capping materials applied on nanoparticles. Dey applied oleylamine as a capping agent and solvent on HEA nanoparticles with varied combinations of Pd, Pt, Rh, Ir, Ni, Fe, Co, and Sn and obtained particles with

<15 nm diameters 13. Cora reported the synthesis of FeCoNiRuPt HEa nanoparticles using oleylamine and oleic acid as surfactants, which restricted Ostwald ripening and particle growth, keep- ing the average particle size <5 nm 14. Jiayue Sun produced AuAgCuPtPd HEA nanoparticles, which ranged in diameter from

0.5 to 3 nm and were capped using thiolated polymer ligands 15. In this work, copper and platinum were chosen as the con- stituent elements to incorporate in FeCoNi-based, 5-element Fe- CoNiCuPt HEA nanoparticles. Copper, like zinc or other antiox- idant metals, tends to stabilise the alloy by reducing the rate at which the nanoparticles oxidise or dissolve, resulting in increas- ing the durability of HEA nanoparticles 16. Pt and FePt are well- known for their high-performance electrocatalytic properties 17. FePt alloys have significantly high magnetic anisotropy too 18. Combining Cu and Pt with the well-studied FeCoNi group can enhance the durability, catalytic activity, and magnetic properties

in HEA by creating multi-element "cocktail" effects 16–18.

Solid-state reaction as a synthesis method yields a clean, or- ganic surfactant (ligand)-free surface of the product. In the liter- ature, the isolating medium—which often uses NaCl, KCl, or MgO has been frequently employed to produce FePt, FeCuPt, and other multi-metallic Pt alloys 1,18,19. These isolating mediums behave as a substrate (separating matrix) and ensure heat is applied evenly and particles stay separated, preventing nucleated particles from aggregating and preventing nanoparticle sintering as the anneal-

ing process progresses, leading to a small particle, single-phase alloy with high thermal stability 1,20. That’s why the isolating medium-assisted solid-state reaction method was chosen to syn- thesise the FeCoNiCuPt HEA nanoparticles and study the effect of different capping agents on the particle size growth of capped Fe- CoNiCuPt HEA nanoparticles and their suspension stability. Chao Meng and their group had synthesised the ultra-small (3-7 nm) FeCoNiCuPt HEA nanoparticles by the same synthesis method to investigate their electrocatalytic properties 1.

In situ (during NaCl dissolution) and post-synthesis (after washing away NaCl and suspending in ethanol) capping treat- ments were performed on nanoparticles to determine the best method for applying capping agents to maintain dispersion and suspension stability and to control Ostwald ripening and parti- cle growth. The thirteen capping agents evaluated included poly- mers like Pluronic P123 and polyvinylpyrrolidone, surfactants like sodium dodecyl sulphate (SDS) and hexadecyltrimethylammo- nium bromide (CTAB), amines like hexadecylamine, oleylamine, octylamine, and octadecylamine, organic acids like citric, oleic, and stearic acid, and other common stabilizers like octadecene and polyethylenimine-linear. The capped and uncapped HEA nanoparticles were characterised using X-ray diffraction (XRD), energy-dispersive X-ray spectroscopy (EDS), transmission elec- tron microscopy (TEM), and dynamic light scattering (DLS) to evaluate their crystallographic structure, elemental composition, particle size distribution of the metal core and capping layer of nanoparticles, and stability of suspension. The objective was to identify capping agents that resulted in small particle sizes, mini- mal aggregation and good stability of the FeCoNiCuPt nanoparti- cle suspension.

# Experimental

## General procedure for the synthesis of FeCoNiCuPt HEA nanoparticles

For the synthesis of 1 mmol (432.1 mg) FeCoNiCuPt nanopar- ticles, the previously reported isolating medium-based solid- state reaction method was used 2, where 1 mmol of precursors Fe(C5H7O2)3 (0.3528 g), Co(C5H7O2)3 (0.356 g), Ni(C5H7O2)2 (0.2568 g), Cu(CH3COO)2 (0.1816 g), and Pt(C5H7O2)2 (0.3936

g) were added together in 1400 mL of a 1:1 hexane/ethanol mix- ture to prepare a precursor solution at 50oC while stirring con- tinuously till complete dissolution of precursors. Ultrafine NaCl powder (grain size <10 µm) purchased from Sun Science Ltd (300 times the total precursor weight, ∼463.78 g) was mixed

into the precursor solution and this was heated and stirred at

80oC until the solvent had all evaporated. The resultant powder was transferred to a Lenton split tube furnace (model no. CSC 12, max. temperature 1200oC) in a quartz boat and heated un- der 5% hydrogen and 95% argon environment at 10oC/minute to 600oC, where it stayed for 3 hours before cooling to room temper- ature. Since some powder adhered to the quartz boat, the product weighed 457.3 g. Fourteen batches of 13.72 g of sintered pow- der were dissolved separately in 90 mL of DI water. The mixture was put in three 50 mL capacity centrifuge tubes, 30 mL each, and centrifuged (4500 rpm, 30 minutes) three times with adding

30 mL DI water after the previous suspension was decanted and once with adding 30 mL ethanol, using Heraeus Megafuge 8 cen- trifugation machine. Each batch of nanoparticles was collected together and stored by suspending them in 50 mL ethanol at - 20oC for post-synthesis capping and characterisation. Sintered powder for in situ capping was stored separately.

  - Procedure for capping of FeCoNiCuPt nanoparticles Thirteen capping agents were applied to FeCoNiCuPt nanoparti- cles by two distinct methods. In "post-synthesis" capping the cap- ping agents were added after the nanoparticles had been purified, washed, and stored in ethanol. In "in situ" capping the capping

agents were incorporated into the washing of the annealed pow- der while the sodium chloride was being removed.

## Post-synthesis capping of FeCoNiCuPt nanoparticles

0.3 mmol of each hydrophilic capping agent—Pluronic P123 (1.74 g), polyvinylpyrrolidone (3g), SDS (0.0865 g), CTAB (0.1093 g), polyethylenimine-linear (1.5 g), and citric acid (0.0576 g)—were dissolved in 90 mL of water separately, form- ing 3.33 mM solutions. Six batches of nanoparticles suspended in ethanol were centrifuged for 30 minutes, and the ethanol was decanted. The nanoparticles were suspended into the capping agent solutions, ultrasonicated for 5 minutes and stirred for 1 hour. Similar centrifuge steps were followed for these mixtures, where nanoparticles were washed and centrifuged (4500 rpm, 30 minutes) three times with 30 mL DI water and once with 30 mL ethanol. The resultant capped materials were collected and sus- pended in 50 mL of DI water.

For the hydrophobic capping agents, 0.3 mmol of the solid or liquid capping agent —hexadecylamine (0.068 g), stearic acid (0.0853 g), octadecylamine (0.0848 g), oleic acid (density: 0.895 g/cm3, 0.0946 mL), oleylamine (density: 0.813 g/cm3,0.0987 mL), octadecene (density: 0.789 g/cm3, 0.096 mL), and octy- lamine (density: 0.782 g/cm3, 0.0497 mL)—were dissolved sep- arately in 90 mL toluene at room temperature, forming a 3.33 mM solution. Seven batches of stored nanoparticle suspensions were centrifuged for 30 minutes and the ethanol decanted before mix- ing in the capping agent solution. The mixture was ultrasonicated for 5 minutes and stirred for 1 hour. These 90 mL mixtures were centrifuged (4500 rpm, 30 minutes) in three centrifuge tubes in equal amounts, with 30 mL of toluene added in each bottle after the previous suspension was decanted. This centrifuging process was repeated thrice. The capped nanoparticles were collected and suspended in 50 mL of toluene.

## In situ capping of FeCoNiCuPt nanoparticles

The hydrophilic agents Pluronic P123 (1.74 g), polyvinyl pyrroli- done (3g), SDS (0.0865 g), CTAB (0.1093 g), polyethylenimine- linear (1.5 g), and citric acid (0.0576 g)—were combined with 90 mL of water until complete dissolution resulted in 3.33 mM solu- tions. Later, 13.72 g of sintered powder was added to each solu- tion and stirred for 1 hour. Similar centrifuge methods were used for these solutions, with nanoparticles cleaned and centrifuged and washed (4500 rpm, 30 minutes) three times with 30 mL DI water and once with 30 mL ethanol. The resulting capped mate-

rials were collected and suspended in 50 mL of DI water.

0.3 mmol of each hydrophobic capping agent —hexade- cylamine (0.068 g), stearic acid (0.0853 g), octadecylamine (0.0848 g), oleic acid (0.0946 mL), oleylamine (0.0987 mL), octadecene (0.096 mL), and octylamine (0.0497 mL)—was dis- solved in 90 mL of toluene at room temperature, forming a 3.33 mM solution. After adding 13.72 g of sintered powder, the solu- tions were stirred for 1 hour. These solutions were mixed with 90 ml of DI water in a separating funnel by shaking the funnel for 15 minutes, to dissolve the NaCl. The funnel was rested hori- zontally until both liquids separated. Water was separated out of the mixture. The remaining mixture inside the separating funnel was centrifuged three times (4500 rpm, 30 minutes) in three cen- trifuge tubes, with 30 mL of toluene added to each bottle after decanting the preceding supernatant, and the capped materials were collected and suspended in 50 mL toluene.

## X-ray diffraction (XRD)

The phase purity and structural parameters of FeCoNiCuPt were determined using a Rigaku SmartLab diffractometer employing a copper source of Kα radiation with λ = 1.5406 Åat ambient tem- perature 21. An XRD scan was taken in 35o-100o 2θ range, with 0.01o step size in Bragg-Brentano geometry. Rietveld refinement of the XRD pattern using GSAS II was applied to extract the lat- tice parameters. The background was fitted using the Chebyshev function, and the instrumental peak shape was defined from a standard LaB6 sample. The Rietveld-refined XRD pattern of Fe- CoNiCuPt was plotted by OriginPro software.

## Energy-dispersive X-ray spectroscopy (EDS)

A Zeiss Sigma 500 VP FESEM with Oxford Instruments Ultim 170 EDS detector was used to determine the material’s elemental composition. The ethanol dispersion was centrifuged (4500 rpm, 30 minutes) to extract the uncapped nanoparticles, then left to evaporate any remaining ethanol for an hour. For EDS measure- ment, powder was placed on a stub covered with carbon tape.

## Transmission Electron Microscopy (TEM)

The morphology and particle size distribution of all the capped and uncapped FeCoNiCuPt nanoparticles were examined using an FEI Tecnai T12 Transmission Electron Microscope fitted with a Morada G2 digital camera (11 MP) at 120 kV maximum ac- celerating voltage and 400,000x maximum magnification. The suspended particles were ultrasonicated for 5 minutes, drop-cast on the carbon grids and left to dry for one hour to get rid of the residual solvent prior to TEM analysis. To estimate particle size distribution and average diameter, 200 spherical nanoparti- cle diameters were manually measured from TEM micrographs using ImageJ software 22,23. The kernel density distribution func- tion was used to measure particle frequency throughout a size range 24.

## Dynamic light scattering (DLS)

Anton Paar’s Litesizer DLS 701 instrument was used to examine the particle size distribution and for zeta potential measurement of the capped nanoparticles. The instrument was equipped with laser light of wavelength 658 nm from a single-frequency laser diode, providing 40 mW, with a particle diameter measurement range of 0.3 nm-10 µm and a zeta potential measurement range of >±1000 mV. The suspended capped nanoparticles were ul- trasonicated for 5 minutes and filtered with a 100 nm syringe filter to remove any agglomerates. The particle size distribution of particles suspended in water and toluene was measured us- ing disposable and quartz cuvettes, respectively. Omega cuvettes and univettes were used to measure nanoparticle zeta potential in water and toluene.

# Results and discussion

PDF Card No.: 9014285, Fe PDF Card No.: 9011619, Co PDF Card No.: 2100640, Ni PDF Card No.: 4105681, Cu PDF Card No.: 1011103, Pt

yobs ycalc

yobs-ycalc

Bragg position

intensity (arb. unit)

The XRD pattern of the uncapped FeCoNiCuPt HEA alloy was Rietveld-refined, with 1.694 goodness of fit (χ2) and 2.307% weighted profile R-factor (Rw) showing a strong alignment be- tween the calculated pattern and the observed profile. The Rietveld-refined XRD pattern of the single-phase FeCoNiCuPt HEA nanoparticles is displayed in Fig. 1.

40	50	60	70	80	90	100

2θ (degree)

Fig. 1 The Rietveld refined XRD patterns of the uncapped FeCoNiCuPt sample and corresponding PDF standard patterns of constituent elements of the Fm3m (225) space group. Red circles, black line, blue lines and green vertical signs represent the observed (yobs), calculated (ycalc), the difference between the observed and calculated spectra (yobs-ycalc), and Bragg positions.

The diffraction pattern of the synthesised FeCoNiCuPt mate- rial (uncapped) can be indexed by the database of individual el- ements, Fe (PDF code: 9014285), Co (PDF code: 9011619), Ni (PDF code: 2100640), Cu (PDF code: 4105681), and Pt (PDF

code: 1011103), as shown in Fig. 1. The diffraction peaks at 42.27o, 49.21o, 72.15o, 87.33o, and 92.30o 2θ values can be indexed to the 111, 200, 220, 311 and 222 reflections of cu- bic Fm3m (225) space group material, with lattice parameter a=3.699(8) Å, consistent with the previously reported values 2. The atomic radius of platinum is comparatively larger (∼139 pm)

than that of the other elements (∼124-128 pm) in the alloy. When

FeCoNiCuPt is produced, its average lattice spacing becomes in- termediate between the constituent element lattice spacings, pro-

ducing HEA XRD peaks that show up in between the pure element peaks 2, as seen in Fig. 1.

The elemental distributions of uncapped FeCoNiCuPt HEA are shown in Fig. 2 (a-e). The elements Fe, Co, Ni, Cu, and Pt are uniformly distributed together, indicating their alloying in HEA nanoparticles. Fig. 2 (f) represents the EDS spectra showing the atomic weight of constituent elements, % of Fe, Co, Ni, Cu, and Pt as 22.5%, 23.2%, 22.1%, 14.9% and 17.3% respectively, which are close to the equal proportions range stated by J. W. Yeh, prov- ing the synthesis of FeCoNiCuPt HEA 1. Chao Meng suggests that the copper precursor (Cu(CH3COO)2) reacts with NaCl during an- nealing at high temperature (600oC), resulting in the formation of water-soluble salts like CuCl2 that dissolve during the wash- ing process to collect HEA nanoparticles, resulting in reduced Cu content 1,25.

The EDS spectra in Fig. 2 (f) show carbon and oxygen Kα peaks at 0.277 keV and 0.525 keV, respectively 26. The carbon peak in the EDS spectra comes from mounting the sample on carbon tape (Supplementary Fig. S1 (b)), as well as due to the presence of adventitious carbon because of the deposition of carbonaceous materials on the sample when they are exposed to the environ- ment 27. The presence of oxygen, as shown in supplementary Fig. S1 (c), may be due to surface particle oxidation while wash- ing because FeCoNi-based HEA are vulnerable to oxidation in air and water, though previous research shows a much lower rate of oxidation of FeCoNiCuPt HEA nanoparticles than monometallic counterparts 28.

Fig. 2 (a-e) Elemental mapping images of uncapped FeCoNiCuPt HEA particles, and (f) its EDS spectra.

  - TEM analysis of uncapped FeCoNiCuPt nanoparticles The TEM micrographs of uncapped FeCoNiCuPt HEA nanoparti- cles are presented in Fig. 3, where Fig. 3 (a) shows the TEM

micrograph of particles analysed after 1 hour of washing out the

isolating medium and Fig. 3 (b) shows particles analysed after 10 days of washing, which were stored in ethanol at -20oC. The TEM particle size distributions were computed using about 200 parti- cles in the field of view of a single TEM micrograph. Although the distributions are based on individual micrographs, examin- ing a large number of particles increases their statistical signifi- cance and provides a good estimate of particle size distribution.

Most nanoparticles are spherical, with darker black circles sug- gesting thicker and overlapped particles and lighter black circles showing individual nanoparticles. This difference in appearance is explained by the electron beam’s higher scattering in areas with overlapping particles or thicker samples. Electrons interact with more material as they move through thicker regions of the sam- ple, which causes more scattering and a lower transmitted beam intensity 29.

Fig. 3 TEM image micrographs of uncapped FeCoNiCuPt nanoparticles taken (a) after 1 hour and (b) after 10 days of washing out he isolating medium and storing in ethanol at -20oC.

Within 10 days of storage in ethanol, the average particle size of uncapped nanoparticles increased by 165% from 4.74 nm to

12.57 nm. Fig. 3(b) reveals agglomeration of two or more par- ticles in uncapped FeCoNiCuPt nanoparticles after 10 days, re- sulting in darker and larger spheres. The minimum and maxi- mum particle sizes observed for the sample analysed after 1 hour of washing are 1.45 nm and 13.87 nm, respectively, compared to 2.33 nm and 33.11 nm, respectively, for particles held for 10

days. The D10, D50 and D90 values representing the smallest 10%, 50% and 90% of the particles by size, respectively, had the aver- age particle sizes of 2.04 nm, 3.27 nm, and 4.28 nm, respectively, increasing to 2.85 nm, 6.24 nm, and 10.81 nm for the sample

stored in ethanol for 10 days. Fig. 4(a) displays the particle size distribution for both samples, indicating a decrease in the number of smaller nanoparticles and a shift in the size distribu-

tion to larger uncapped FeCoNiCuPt nanoparticles over time. It is clear that particle size and agglomeration increase over time, even when suspensions are stored in ethanol at a low tempera- ture. Due to the increase in specific surface area with the decrease in particle size, nanoparticles contain a huge amount of surface energy, which challenges the system’s thermodynamic behaviour to reach a minimum energy, resulting in the Ostwald ripening and agglomeration of nanoparticles 30,31. A large amount of re- pulsive force is required to defeat the thermodynamic interac- tion between nanoparticles, and that’s why the need for cap- ping agents arises 31,32. To prevent nanoparticle agglomeration and stabilise the suspension, 13 capping agents were employed, including polymers, surfactants, amines, acids, etc. These cap- ping agents were separated into two groups according to their hydrophilic or hydrophobic nature.

## TEM analysis of hydrophobic agent-capped FeCoNiCuPt nanoparticles

The particle size distribution plots of nanoparticles with hy- drophobic capping agents are given in Fig. 4 (b)-(h), with red and black lines indicating in situ and post-synthesis capping, re- spectively. Supplementary Figs. S2 & S3 show their TEM mi- crographs. The particle size distribution was plotted using the kernel smooth distribution function, as this estimate is nonpara- metric and can be used in almost any situation, regardless of par- ticle size or aggregation 24. Octadecylamine-capped nanoparti- cles, both in situ and post-synthesis, exhibited the lowest average particle sizes among the seven hydrophobic capping agents. Post- synthesis octadecylamine-capped nanoparticles have an average particle size of 3.77 nm, nearly 10% smaller than in situ-capped nanoparticles (4.19 nm). The minimum and maximum particle sizes for octadecylamine-capped nanoparticles post-synthesis are

1.04 and 10.69 nm, whereas in situ caps vary from 1.33 to 11.62 nm. This result indicates that octadecylamine is an effective hy- drophobic capping agent under both capping conditions, helping to limit the increase in particle size.

Post-synthesis octadecylamine-capped nanoparticles have a

∼20% lower particle size than uncapped FeCoNiCuPt nanopar- ticles (4.74 nm) observed one hour after washing. Similar trends are seen for the minimum and maximum particle sizes of octadecylamine-capped nanoparticles in comparison to uncapped nanoparticles, showing that nanoparticles start agglomerating just after washing away the NaCl 33,34. D90 values for octadecene and oleic acid are <5 nm, while for octadecylamine and stearic acid D90 values are <4 nm, as shown in Fig. 4, which are sig- nificantly lower than the particle size of uncapped nanoparticles. So, octadecylamine and stearic acid performed most effectively in retaining smaller particles among the examined hydrophobic agents.

## TEM analysis of hydrophilic agent-capped FeCoNiCuPt nanoparticles

Fig. 5 (a)–(f) shows particle size distribution graphs of all hy- drophilic capping agents, with red and black lines representing in situ and post-synthesis capping agent introduction. See supple-

Fig. 4 Particle size distribution plots of nanoparticles from analysis of TEM micrographs for (a) uncapped FeCoNiCuPt nanoparticles analysed after 1 hour (black) and 10 days (red) and nanoparticles capped by hy- drophobic capping agents (b) hexadecylamine, (c) oleic acid, (d) oley- lamine, (e) octadecene, (f) stearic acid, (g) octylamine, and (h) octade- cylamine, where red and black lines represent the in situ capped and post-synthesis capped nanoparticles, respectively.

Fig. 5 TEM micrograph particle size distribution plots for hydrophilic agents capped nanoparticles (a) Pluronic P123, (b) polyvinylpyrrolidone,

(c) SDS, (d) CTAB, (e) polyethylenimine (linear), and (f) citric acid, where red and black lines represent in situ and post-synthesis capped nanoparticles, respectively.

cles, unreacted precursors, undissolved isolating medium, or ex- cess capping agents by a series of washing operations 20,35. It is important to make sure that the NaCl particles have completely dissolved and been eliminated by water centrifugation and ultra- sonication before adding capping agents to the nanoparticles fol- lowing sintering. This method ensures that the isolating medium

is fully dissolved and that the capping agents only interact with

the dispersed, pure nanoparticles. When employing hydrophilic

mental Figs. S4 & S5 for their TEM micrographs. Pluronic P123- capped nanoparticles exhibited the smallest average particle size among the six hydrophilic agents, with average particle sizes of capping in situ and post-synthesis being 3.79 nm and 3.32 nm, respectively. Post-synthesis Pluronic P123-capped nanoparticles range from 1.13 to 12.49 nm, whereas in situ octadecylamine- capped nanoparticles range from 1.20 to 14.84 nm. The average particle size of all hydrophilic agent-capped nanoparticles is <5 nm (SDS has ∼5 nm average particle size), whether applied in situ or post-synthesis.

The examination of 26 capped samples using 13 capping agents in two techniques found that 22 samples preserved D90 values below 5 nm, of which 15 samples had D90<4 nm, highlighting the importance of capping agents in controlling nanoparticle size dispersion. Out of the thirteen capping agents tested, the size dispersion of most of the nanoparticles was smaller when cap- ping was done post-synthesis than in situ. This difference in size may be caused by the elimination of weakly bound nanoparti-

capping agents, the size of the nanoparticles is mostly determined by the properties of the capping agent since the sintered powder was rinsed completely with water, dissolving the NaCl. As a re- sult, the size of the hydrophilic agent-capped nanoparticles is not significantly affected by whether they are added in situ or post- synthesis. In contrast, if hydrophobic capping agents are added in situ while the sintered powder still contains NaCl, they will coat both the nanoparticles and the NaCl matrix, as the hydrophobic capping agents are dissolved in toluene, and toluene is unable to dissolve NaCl. So the toluene suspension has the potential to interfere with NaCl dissolution, leaving residual salt in the end product. This is demonstrated by the TEM micrographs of oley- lamine and hexadecylamine (both hydrophobic) displayed in Fig. 6 (a) and (b), respectively, in which undissolved NaCl particles can be observed. The post-washing capping method is there- fore advantageous for hydrophobic capping agents since it guar- antees the elimination of NaCl, cleaner surfaces, and enhanced capping agent-nanoparticle contact, all of which reduce the risk

of nanoparticle aggregation.

Fig. 6 TEM micrographs of FeCoNiCuPt HEA nanoparticles showing residual NaCl particles when capped with (a) oleylamine and (b) hex- adecylamine introduced prior to washing (in situ capping) out the NaCl particles .

TEM analysis allowed us to analyse the particle size of individ- ual nanoparticles; however, capped particles consist of a metal core, surface coating, and solvent molecules that are tightly asso- ciated with the coating. As a result, a capped nanoparticle’s en- tire hydrodynamic diameter may be significantly larger than the individual particle size determined by TEM 36. DLS analysis in- volves studying thousands of particles suspended in a solvent to provide a detailed hydrodynamic particle size distribution. The sizes of the particles are determined by examining the Brownian motion of nanoparticles, which occurs due to their random move- ment as a result of collisions with solvent molecules. A laser is directed at the dispersed nanoparticles to facilitate this measure- ment. The hydrodynamic diameter (DH ) of the capped nanopar- ticles was measured by employing the Stokes & Einstein equation within the instrument, which is affected by temperature and the dynamic viscosity of the solvent 37, as shown in equation 1.

eration can result in the grouping of nanoparticles, which leads to their identification as larger particle clusters. The combined hydrodynamic size of these clusters is substantially greater than the size of individual particles, as measured by DLS. Moreover, the presence of even a few large particles and grouped clusters can result in a significant shift towards higher values in the re- sultant hydrodynamic diameter, particularly when measurements are conducted in intensity- or volume-weighted modes 38.

## DLS analysis of hydrophilic agent-capped FeCoNiCuPt nanoparticles

Table 1 summarises the number-weighted particle size distribu- tion of capped FeCoNiCuPt nanoparticles by DLS. The most fre- quent particle size is denoted by DM , while the smallest 10%, 50%, and 90% particles are denoted by D10, D50, and D90, respec- tively.

The most frequent particle size (DM ) of all these hydrophilic agent-capped nanoparticles lies in the range of 10-80 nm, includ- ing both the metal core and the capping layer. As depicted in Table 1, Pluronic P123 gives the smallest hydrodynamic diame- ter with the most frequent particle size (DM ) of 10.6 nm, which is consistent with the smallest metal core sizes found in TEM re- sults. On the other hand, when post-synthesis capping is per- formed, CTAB, citric acid, and polyethylenimine have DM ≥ 70 nm. Although the particle size of CTAB-capped nanoparticles is relatively larger than that of other nanoparticles, the particles are mainly distributed within the same size range, as shown in Table

1. There is no significant effect of washing on polyvinylpyrroli- done and SDS-capped nanoparticles. It is apparent that DLS pro- files of most of the nanoparticles capped post-synthesis show sig- nificantly larger particle size distribution and DM values in com- parison to particles capped in situ. This could be due to the delay in the capping process, allowing the nanoparticles to agglomer- ate before capping, which was confirmed by TEM micrographs of uncapped FeCoNiCuPt nanoparticles (Fig.3), showing increased particle size and agglomeration with time 33. If capping occurs during washing, the nanoparticles are capped immediately af- ter they detach with isolating medium, preventing agglomeration and stabilising the surface of nanoparticles right away after being exposed 33.

## DLS analysis of hydrophobic agent-capped FeCoNiCuPt nanoparticles

The D10, D50, D90, and DM values in the table 1 represent the number-weighted particle size distribution of FeCoNiCuPt nanoparticles capped with hydrophobic agents as determined by DLS. For FeCoNiCuPt nanoparticles capped with hydropho- bic agents, the DM values vary from as low as 5.9 nm for post-

H =

D	 kBT

3πηD

(1)

synthesis octadecene to a maximum of 61 nm for in situ oley- lamine capping. Nanoparticles capped with oleic acid, oley-

where kB represents Boltzmann constant, T represents temper- ature, & η is viscosity of solvent.

The particles were weighted by numbers in place of intensity or volume; the size of the most frequent particle in the solutions can be found by number-weighted particle size distribution. Agglom-

lamine, and octadecene tend to have a smaller hydrodynamic diameter after washing out the NaCl particles. The distribution of octylamine and hexadecylamine particle sizes is not substan- tially impacted by washing. In contrast to particles capped post- synthesis, nearly all of the in situ hydrophobic capped particles

Table 1 The experimentally observed particle sizes and zeta potential (ZP) of capped FeCoNiCuPt nanoparticles; D10, D50, and D90 represents the average particle size of smallest 10%, 50%, and 90% particles respectively and DM represents the most frequent particle size

|  |  |  | Post-synthesis |  |  |  |  | In situ |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Capping agent | D10 (nm) | D50 (nm) | D90 (nm) | DM (nm) | ZP (mV) | D10 (nm) | D50 (nm) | D90 (nm) | DM (nm) | ZP (mV) |
| Pluronic P123 | 11.4 | 48.4 | 53.1 | 50.6 | -23.2 | 3.1 | 9.9 | 11.9 | 10.6 | -17.1 |
| Polyvinylpyrrolidone | 23.4 | 39.9 | 55.0 | 44.5 | -18.3 | 26.4 | 47.6 | 71.7 | 53.5 | -25.6 |
| Sodium dodecyl sulphate | 15.4 | 41.6 | 43.5 | 43.0 | -16.2 | 17.7 | 35.8 | 46.7 | 39.1 | -12.9 |
| CTAB | 71.9 | 77.2 | 82.6 | 80.2 | 22.3 | 30.0 | 43.3 | 58.5 | 47.6 | 25.3 |
| Polyethylinimine linear | 41.9 | 65.8 | 94.0 | 74.5 | 32.9 | 15.1 | 29.9 | 37.8 | 33.0 | 32.0 |
| Citric acid | 35.0 | 64.9 | 92.0 | 73.5 | -24.4 | 4.6 | 22.1 | 39.6 | 43.9 | -26.8 |
| Hexadecyl amine | 22.2 | 26.6 | 34.0 | 28.8 | 9.8 | 6.4 | 19.4 | 25.2 | 21.3 | 16.6 |
| Oleic acid | 3.7 | 11.8 | 15.2 | 12.9 | 13.8 | 8.8 | 24.4 | 28.5 | 25.8 | 15.9 |
| Oleylamine | 4.2 | 15.9 | 19.4 | 17.1 | 33.3 | 48.5 | 56.6 | 73.4 | 61.0 | 24.2 |
| Octadecene | 2.5 | 5.4 | 6.8 | 5.9 | 17.9 | 8.1 | 19.2 | 28.6 | 22.0 | 19.1 |
| Stearic acid | 15.5 | 51.0 | 68.3 | 56.6 | 24.2 | 7.6 | 28.1 | 33.3 | 29.9 | 5.1 |
| Octylamine | 7.1 | 13.2 | 19.4 | 15.0 | 25.2 | 6.1 | 9.4 | 13.0 | 10.5 | 17.8 |
| Octadecyl amine | 5.0 | 20.1 | 24.2 | 21.6 | 21.3 | 2.4 | 6.3 | 8.4 | 7.0 | 11.5 |

exhibit a wider particle distribution (D90-D10). This indicates that when a hydrophobic agent was added directly to toluene, the inhibition of NaCl particle dissolution resulted in particle size growth and agglomeration 20,35, which was also established by TEM micrographs of hydrophobic-capped nanoparticles.

The difference between the hydrodynamic radius obtained from DLS and the particle radius determined by TEM can pro- vide insights into the approximate thickness of the capping layer on the surface of the particles. However, it is complicated for particles surrounded by hydrophilic capping agents, as the DLS also adds the size of water molecules surrounding the capping agent because the surface of hydrophilic agents forms a hydra- tion layer by surrounding water molecules. That’s why the actual size of the capping layer as well as the actual hydrodynamic par- ticle size may be smaller than the size calculated by DLS 39,40. This explains why FeCoNiCuPt particles capped with hydrophilic agents have substantially larger diameters than those coated with hydrophobic agents.

## Zeta potential of hydrophilic agent-capped FeCoNiCuPt nanoparticles

Zeta potential (ZP) refers to the electrical potential at the sur- face of a nanoparticle in relation to its surrounding medium. A higher zeta potential leads to increased repulsion between nearby nanoparticles, thereby preventing agglomeration and enhancing stability. Generally, nanoparticles with a zeta potential magni- tude of |ZP| ≤ 10 mV are considered highly unstable and prone to agglomeration; 10-20 mV are unstable or relatively stable, and 20-30 mV are moderately stable, while particle suspensions with

|ZP| ≥ 30 mV are regarded as highly stable 41,42. Suspended nanoparticles need |ZP| ≥ 30 mV to stabilise electrostatically, while |ZP| ≥ 20 mV is required for steric stabilisation 43.

The zeta potential values of all the capped nanoparticles are shown in Table 1, where polyethylenimine-linear capped nanoparticles are highly stable, as they have |ZP| ≥ 30 mV in both coating cases, in situ and post-synthesis. Pluronic P123 is a copolymer consisting of two hydrophobic polypropylene oxides and one hydrophilic polyethylene oxide block. The polyethylene oxide blocks have an affinity for interacting with water molecules and develop a negative charge, giving rise to a negative zeta po-

tential 44, as can be seen in Table1. The presence of polar groups in polyvinylpyrrolidone can lead to a negative zeta potential 45. Both Pluronic P123 and polyvinylpyrrolidone are non-ionic poly- mers, and the formation of hydration shells through their inter- action with water molecules can also be the result of a negative potential 39,40. Polyethylenimine-linear is cationic in nature due to the presence of amino groups 46 in this polymer. Nanoparticles capped by polyethylenimine-linear show the highest stability in all the analysed hydrophilic agents, with ZP values of 32 mV and

32.9 mV capped in situ and post-synthesis, respectively. CTAB is also a cationic surfactant 47, giving moderate stability to nanopar- ticles (ZP≥ 20 mV). There is no noticeable impact from the timing of the wash on nanoparticles coated with either of these cationic

agents. SDS acts as an anionic surfactant 48, which does not show greater stability (|ZP|≤ 20 mV) to our nanoparticle suspensions, while citric acid gives moderate stability to suspended nanopar- ticles (20≤|ZP|≤ 30 mV), which has three carboxylate groups functioning as a triprotic acid 49. These carboxylate groups ad-

here to the surfaces of nanoparticles, contributing to a net nega- tive charge 50, as depicted in Table 1.

## Zeta potential of hydrophobic agent-capped FeCoNiCuPt nanoparticles

Nanoparticles suspended in toluene (hydrophobic agent-capped nanoparticles) typically exhibit a lower zeta potential compared to their water-soluble versions, as depicted in Table 1. This dif- ference arises because water is a polar solvent, while toluene is nonpolar. The polarity of the surrounding environment can influ- ence the surface charge of the capped nanoparticles and provide better electrostatic stability 51. All capped hydrophobic nanopar- ticles exhibit a positive zeta potential, which is a result of the posi- tive surface charge of the metal nanoparticles. Electron lone pairs of amines, such as hexadecylamine, oleylamine, octylamine, and octadecylamine, interact with these surface charges, contribut- ing to the positive zeta potential 52,53. None of the hydropho- bic nanoparticles capped in situ exhibit good stability, except oleylamine-capped nanoparticles, which have a ZP value of 24.2 mV and are moderately stable. This confirms the TEM analysis that adding a hydrophobic capping agent after washing out the NaCl particles (post-synthesis capping) is a more effective tech-

nique. The only hydrophobic capping agent that exhibits high stability (ZP = 33.3 mV) of capped nanoparticles suspended in toluene is oleylamine-capped post-synthesis nanoparticles.

Analysing DLS plots of capped nanoparticles provides insight into the effective thickness of the metal core and capping layer together 54, which can lead us to the quantitative analysis of surrounding capping thickness 55 and its effect on the stability of nanoparticles. Especially for hydrophilic nanoparticles sus- pended in water, water as a suspension medium gives the ben- efit of a hydration layer, which significantly impacts their sta- bility by providing the electrostatic and steric barrier and in- creasing the long-term stability of nanoparticles in water suspen- sion 56. It is observable in Table 1 that most of the hydrophilic agent-capped nanoparticles have a higher particle size, which leads them to higher values of zeta potential and greater sta-

biltiy 39,40,56. Larger hydrodynamic diameter particles often has

more stable suspension (|ZP|> 20 mV), while the majority of nanoparticle suspensions with unstable zeta potentials (|ZP|< 20 mV) typically have low hydrodynamic diameters. This is be- cause the hydration layer of nanoparticles in stable suspension is often thicker, resulting in higher steric stabilisation and less tendency of agglomeration 39,56. Polyethylenimine linear capped nanoparticles were still able to have greater stability with a DM value of 33 nm when capped in situ, showing no particular ef- fect of washing on their stability. Nanoparticles dispersed in toluene do not have this advantage due to their non-polar na- ture and have a reduced electrostatic interaction 51. According to the Derjaguin–Landau–Verwey–Overbeek theory 57, hydropho- bic particles should have stronger steric repulsion and van der Waals forces in order to compensate for the absence of electro- static interactions and achieve suspension stability. Greater sta- bility can also result from capping materials that can improve electrostatic interaction with the suspension and other particles. As can be seen in Table 1 for oleylamine-capped nanoparticles. A higher hydrodynamic diameter could help them gain steric stabil- ity, but observing Table 1, most of the nanoparticles suspended in toluene lack the high hydrodynamic diameter and higher stability. It can also be seen that most of the particles capped post-synthesis have relatively higher stability (i.e., oleylamine, stearic acid, octy- lamine and octadecylamine). All things considered, zeta poten- tial analysis of capped FeCoNiCuPt nanoparticles shows that oley- lamine and polyethylenimine are efficient capping agents that im- prove suspension stability and inhibit agglomeration. It can also be claimed that hydrophilic agents are more stable because of the additional hydration impact, and it has been demonstrated once more that in order to achieve good stability, hydrophobic agents had to be added after the isolating medium had been completely washed out.

# Conclusions

In conclusion, the medium-assisted solid-state reaction for the synthesis of HEA nanoparticles looks promising, where ultrafine NaCl particles of less than 10µm size were used as the isolat- ing medium. The XRD measurements and Rietveld refinement of the resultant FeCoNiCuPt confirm the formation of a single-phase FCC crystal structure with Fm3m (225) space group. EDS results

prove the uniform distribution of all constituent elements, with atomic weight lying well within the range of the prior-defined HEA composition. TEM analysis of uncapped FeCoNiCuPt HEA nanoparticles shows the growing agglomeration of particles with time and an average particle size increment of about 165% in just 10 days, showing the inability of low-temperature ethanol sus- pension to withstand the thermodynamic need of agglomeration. For this reason, the need for a suitable capping agent arose to be utilised to achieve the required particle size and good suspension stability.

The effect of thirteen different capping agents on the parti- cle size and stability of FeCoNiCuPt nanoparticle suspensions was analysed by TEM micrographs, DLS analysis, and their respective zeta potentials. Hydrophilic capping agents were successful in preventing the particle size growth beyond 5 nm, with Pluronic P123-capped nanoparticles having the smallest average particle size and polyethylenimine-linear showing the highest stability of nanoparticle suspension. It can be claimed that nanoparticles capped by hydrophilic agents retain the particles at a smaller av- erage size and give more stability to the suspension because of the additional hydration impact.

Of all the hydrophobic agents, octadecylamine and stearic acid performed the best at retaining small particles, and oleylamine- capped nanoparticles were most stable, especially those that were capped post-synthesis. However, capping with hydropho- bic agents was difficult without a separate washing step due to the hindrance of the dissolution of the NaCl isolating medium. It has been demonstrated that in order to achieve good stability, hy- drophobic agents need to go through the post-synthesis capping method.

The zeta potential and hydrodynamic diameter of capped nanoparticles were examined in order to determine the effec- tive thickness of the capping layer and how it affected the sta- bility of nanoparticle suspension. Polyethylenimine-linear capped nanoparticles come out as a great option, with a small average particle size (<5 nm) as well as high stability (|ZP|>30 mV) in suspension. This synthesis and capping strategy is expected to be applicable to various HEAs with distinct compositions.

# Author contributions

Anurag Sharma developed the original draft of the manuscript, investigated all of the experiments, and performed formal anal- ysis of the results. Andrew L. Hector, the corresponding author, monitored the research, assisted with article review, and provided supervision throughout the experimental design, methodological development, and data analysis. Both authors evaluated and ap- proved the final version of the manuscript.

# Conflicts of interest

There are no conflicts to declare.

.

# Data availability

The original data of XRD, EDS, TEM, DLS, and zeta potential will be available from the University of Southampton institu- tional repository; DOI will be supplied at proof stage. The

standard X-ray patterns of individual elements, Fe (PDF code: 9014285), Co (PDF code: 9011619), Ni (PDF Code: 2100640), Cu (PDF Code:  4105681), and Pt (PDF Code:  1011103)

can be obtained from Crystallography Open Database, (COD), https://www.crystallography.net/cod/index.php.

# Acknowledgements

The authors thank EPSRC for a studentship to AS (EP/W524621/1) and instrumentation funding (EP/K00509X/1, EP/K009877/1 and EP/V007629/1). We also thank Anton Paar for providing access to the DLS instrumentation. AS extends sincere thanks to Regan Doherty, James Thompson, and the Biomedical Imaging Unit at Southampton General Hospital for their support and guidance in conducting TEM measurements. Special thanks are also due to Dr. Daniel Zabek for his valuable suggestions regarding DLS analysis.

# References

- J.-W. Yeh, S.-K. Chen, S.-J. Lin, J.-Y. Gan, T.-S. Chin, T.-T.

Shun, C.-H. Tsau and S.-Y. Chang, Advanced Engineering Ma- terials, 2004, 6, 299–303.

- C. Meng, X. Wang, Z. Li, C. Wu, L. Chang, R. Liu and W. Pei,

Materials Advances, 2024, 5, 719–729.

- C. Bazioti, O. M. Løvvik, A. Poulia, P. Carvalho, A. Azar,

P. Mikheenko, S. Diplas and A. E. Gunnæs, Journal of Alloys and Compounds, 2022, 910, 164724.

- X. Liu, J. Li, Z. Li, H. Chu, Z. Pan, H. Pan, S. Zhao and D. Li,

Advanced Optical Materials, 2024, 12, 2302043.

- Y. Liao, Y. Li, R. Zhao, J. Zhang, L. Zhao, L. Ji, Z. Zhang,

X. Liu, G. Qin and X. Zhang, National Science Review, 2022, 9, nwac041.

- C. Cai, Z. Xin, X. Zhang, J. Cui, H. Lv, W. Ren, C. Gao and

B. Cai, Catalysts, 2022, 12, 1050.

- S. Pan, H. Shi, Y. Yu, Y. Li, Y. Chen, C. Li, Y. Sun, Z. Yang and

F. Luo, Chemical Communications, 2024, 60, 11778–11781.

- D. Das, Y. Getahun, F. S. Escobar, R. Romero, A. A. El-Gendy and C. Ramana, The Journal of Physical Chemistry C, 2022, 126, 14255–14263.

- S. Shrestha, B. Wang and P. Dutta, Advances in Colloid and Interface Science, 2020, 279, 102162.

- U. Das, N. K. Daimari, R. Biswas and N. Mazumder, Discover Applied Sciences, 2024, 6, 320.

- A. Heuer-Jungemann, N. Feliu, I. Bakaimi, M. Hamaly, A. Alki- lany, I. Chakraborty, A. Masood, M. F. Casula, A. Kostopoulou,

E. Oh et al., Chemical reviews, 2019, 119, 4819–4880.

- J. Liu, C. Liang, X. Zhu, Y. Lin, H. Zhang and S. Wu, Scientific Reports, 2016, 6, 32631.

- G. R. Dey, C. R. McCormick, S. S. Soliman, A. J. Darling and

R. E. Schaak, ACS Nano, 2023, 17, 5943–5955.

- C. M. Da Silva, H. Amara, F. Fossard, A. Girard, A. Loiseau and V. Huc, Nanoscale, 2022, 14, 9832–9841.

- J. Sun, A. Leff, Y. Li and T. J. Woehl, Nanoscale, 2023, 15, 10447–10457.

- J. Zhu, Y. Yang, L. Chen, W. Xiao, H. Liu, H. D. Abruña and

D. Wang, Chemistry of Materials, 2018, 30, 5987–5995.

- X. Zhang, H. Li, J. Yang, Y. Lei, C. Wang, J. Wang, Y. Tang and

Z. Mao, RSC Advances, 2021, 11, 13316–13328.

- J. He, B. Bian, Q. Zheng, J. Du, W. Xia, J. Zhang, A. Yan and

J. P. Liu, Green Chemistry, 2016, 18, 417–422.

- S. Dong, Y. Ju, Y. Jiang, C. Meng, R. Liu, C. Wu and W. Pei,

Journal of Alloys and Compounds, 2022, 909, 164748.

- X. Du, Y. Liu, L. Li, W. Chen and Y. Cui, Journal of Materials Research, 2014, 29, 2921–2927.

- A. Kumar, A. Sharma, M. Sharma, V. Singh, A. Dhaka and R. S. Dhaka, Journal of Alloys and Compounds, 2023, 966, 171506.

- C. A. Schneider, W. S. Rasband and K. W. Eliceiri, Nature Methods, 2012, 9, 671–675.

- B. Cermenek, B. Genorio, T. Winter, S. Wolf, J. Connell,

M. Roschger, I. Letofsky-Papst, N. Kienzl, B. Bitschnau and

V. Hacker, Electrocatalysis, 2020, 11, 203–214.

- Y. Gao, D. Li, R. Zhang, Y. Guo, L. Chen, G. Tian, R. Liu and

G. Ge, Spectrochimica Acta Part B: Atomic Spectroscopy, 2022,

198, 106550.

- J. Zhang and X. Li, Biomedical Journal of Scientific & Technical Research, 2023, 53, 5.

- M. A. Skinner, D. N. Burrows, G. P. Garmire, J. A. Menden- hall, D. H. Lumb, A. D. Holland and P. J. Pool, EUV, X-Ray, and Gamma-Ray Instrumentation for Astronomy VI, 1995, pp. 163–178.

- L. H. Grey, H. Y. Nie and M. C. Biesinger, Applied Surface Sci- ence, 2024, 653, 159319.

- B. Song, Y. Yang, M. Rabbani, T. T. Yang, K. He, X. Hu,

Y. Yuan, P. Ghildiyal, V. P. Dravid and M. R. Zachariah, ACS Nano, 2020, 14, 15131–15143.

- P. Neoptolemou, N. Goyal, A. J. Cruz-Cabeza, A. A. Kiss, D. J. Milne and T. Vetter, Powder Technology, 2022, 399, 116827.

- A. Tsuda and N. V. Konduru, NanoImpact, 2016, 2, 38–44.

- P. Bélteky, A. Rónavári, D. Zakupszky, E. Boka, N. Igaz, B. Sz- erencsés, I. Pfeiffer, C. Vágvölgyi, M. Kiricsi and Z. Kónya, International Journal of Nanomedicine, 2021, 16, 3021–3040.

- E. M. Hotze, T. Phenrat and G. V. Lowry, Journal of Environ- mental Quality, 2010, 39, 1909–1924.

- N. I. Anaraki, A. Sadeghpour, K. Iranshahi, C. Toncelli,

U. Cendrowska, F. Stellacci, A. Dommann, P. Wick and

A. Neels, Nano Research, 2020, 13, 2847–2856.

- B. J. Babalola, O. O. Ayodele and P. A. Olubambi, Heliyon, 2023, 9, e14070.

- D. Li, N. Poudyal, V. Nandwana, Z. Jin, K. Elkins and J. P. Liu,

Journal of Applied Physics, 2006, 99, year.

- S. K. Filippov, R. Khusnutdinov, A. Murmiliuk, W. Inam, L. Y. Zakharova, H. Zhang and V. V. Khutoryanskiy, Materials Hori- zons, 2023, 10, 5354–5370.

- R. F. Domingos, M. A. Baalousha, Y. Ju-Nam, M. M. Reid,

N. Tufenkji, J. R. Lead, G. G. Leppard and K. J. Wilkinson,

Environmental Science & Technology, 2009, 43, 7277–7284.

- V. Filipe, A. Hawe and W. Jiskoot, Pharmaceutical Research, 2010, 27, 796–810.

- V. Figueroa, B. Velasco, L. G. Arellano, V. Domínguez-Arca,

A. Cambón, A. Pardo, A. Topete, L. C. Rosales-Rivera, J. A. Soltero and S. Barbosa, Journal of Molecular Liquids, 2024, 398, 124240.

- E. Firlar, S. Çınar, S. Kashyap, M. Akinc and T. Prozorov, Sci- entific Reports, 2015, 5, 9830.

- C. Jacobs and R. H. Müller, Pharmaceutical Research, 2002,

19, 189–194.

- V. R. Patel and Y. Agrawal, Journal of Advanced Pharmaceutical Technology & Research, 2011, 2, 81–87.

- J. D. Clogston and A. K. Patri, in Characterization of Nanopar- ticles Intended for Drug Delivery, Springer, 2011, vol. 697, pp. 63–70.

- A. Abuelsamen, S. Mahmud, N. H. Mohd Kaus, O. F. Farhat,

S. M. Mohammad, F. S. R. Al-Suede and A. M. S. Abdul Majid,

Polymers for Advanced Technologies, 2021, 32, 2541–2551.

- M. Sikder, J. Wang, B. A. Poulin, M. M. Tfaily and

M. Baalousha, Environmental Science: Nano, 2020, 7, 3318–

3332.

- M. M. Mady, W. A. Mohammed, N. M. El-Guendy and A. A. Elsayed, International Journal of Physical Sciences, 2011, 6, 7328–7334.

- F. Mindivan, Materials Testing, 2017, 59, 729–734.

- M. S. A.M. Bekmukhametova, R.R. Kashapov, Mental Health Clinician, 2017, 10, 164–168.

- M. A. Dheyab, A. A. Aziz, M. S. Jameel, O. A. Noqta, P. M. Kha- niabadi and B. Mehrdel, Scientific Reports, 2020, 10, 10793.

- F. Alzoubi, O. A. Noqta, T. AlZoubi, H. AlJabaly, H. Alkhateeb,

M. Alqadi and G. Makhadmeh, Results in Engineering, 2023,

18, 101206.

- A. M. Djerdjev and J. K. Beattie, Physical Chemistry Chemical Physics, 2008, 10, 4843–4852.

- F. Dumestre, B. Chaudret, C. Amiens, M. Respaud, P. Fejes,

P. Renaud and P. Zurcher, Angewandte Chemie International Edition, 2003, 42, 5213–5216.

- K. Quast, Minerals Engineering, 2016, 85, 130–137.

- A. Muthuvel, M. Jothibas, C. Manoharan and S. J. Jayakumar,

Research on Chemical Intermediates, 2020, 46, 2705–2729.

- A. Asaikkutti, P. S. Bhavan, K. Vimala, M. Karthik and

P. Cheruparambath, Journal of Trace Elements in Medicine and Biology, 2016, 35, 7–17.

- S. Chen, L. Li, C. Zhao and J. Zheng, Polymer, 2010, 51, 5283– 5293.

- B. Derjaguin, N. Churaev, V. Muller, B. Derjaguin, N. Churaev and V. Muller, Surface Forces, 1987, 293–310.