# Appendix 5.10 – 5-Ply laminate Data Batch 6

5 ply laminate with carbon tabbing – batch 6

| Sample No. | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Maximum Force (N) | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1331.65 | 2.21 | 12.63 | 0.99 | 37169.38 | Through thickness shear leading to in plane shear with some delamination |
| 2 | 1205.51 | 2.1 | 12.6 | 0.82 | 31897.79 | Ductile failure nearly cup/cone |
| 3 | 1241.03 | 2.07 | 12.57 | 0.95 | 32291.46 | Ductile failure |
| 4 | 1351.52 | 2.24 | 12.59 | 1.01 | 38115.05 | End failure |
| 5 | 1363.94 | 2.39 | 12.62 | 0.99 | 41139 | Initially through thickness shear then brittle |
| 6 | 1141.85 | 2.36 | 12.6 | 0.81 | 33954.09 | Through thickness shear |
| 7 | 1270.70 | 2.35 | 12.61 | 0.91 | 37655.41 | In plane shear and then finally brittle |
| 8 | 1296.70 | 2.4 | 12.61 | 0.95 | 39243.26 | Through thickness shear |
| 9 | 1207.08 | 2.37 | 12.63 | 0.87 | 36131.69 | Through thickness shear |
| 10 | 1365.31 | 2.41 | 12.61 | 1.06 | 41491.78 | End failure |
| 11 | 1422.27 | 2.3 | 12.61 | 1.06 | 41250.04 | Initiated by through thickness shear and failed in brittle failure |

| Sample No. N=10 | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Young’s Modulus (GPa) | Maximum Force (N) |
| --- | --- | --- | --- | --- | --- | --- |
| Mean | 1290.69 | 2.291 | 12.61 | 0.95 | 147.88 | 37303.54 |
| Standard Deviation | 85.4 | 0.12 | 0.017 | 0.09 | 3.11 | 3454.34 |
| Variance | 6.62 | 5.25 | 0.14 | 9.22 | 2.10 | 9.26 |