# Appendix 5.26 – Cure Optimisation

# Introduction

The aim of this work is to optimise the cure time/temperature of SF95/ST86 CBS materials to maximise the number of parts that can be produced with a direct heated nickel tool.

DMTA and DSC analysis were performed on samples to evaluate their thermal properties and the degree of cure.

# Experimental

The samples were lay up on a steel plate (500x500x1 mm) and inserted in the oven already in temperature to simulate the high gradient of the nickel tool. The temperature ramp seen by the material was mapped with a thermocouple.

Samples for low temperature material:

- 4x SF95

- ST86 CBS

DMTA and DSC Analysis (SF95/ST86)

The DMTA samples were evaluated by Dynamic Mechanical Thermal Analysis (Rheodyne Thermal Analyser MkIII) using an operating program of 25°C to 260°C at 3°C/min, at a frequency of 1Hz, with a small frame in dual cantilever mode.

The DSC samples were evaluated by Differential Scanning Calorimetry (Mettler Toledo DSC821e), weekly calibrated with three indium samples, using a purge gas of nitrogen at a flow of 50-60 ml/min.

The program used was from 25°C to 260°C at 10°C/min.

# Results and Discussion

SF95 / ST86

The following graph shows an example of oven temperature and ramp measured in the material. The data was also used to calibrate the coefficients for a calculated ramp that has been used for other temperatures.

Temperature ramp

The actual ramp was mapped to try to separate its influence on the cure of the material. A theoretical cure profile was calculated and a subsequent time was added to the total oven time to reach 100% cure. This should help optimising the process when the actual ramp of the nickel tool is known.

The following graph shows a cure profile vs time calculated using the actual temperature ramp and the exponential law. Assuming that the cure time at 130(C is 30’ the samples should be fully cured after 38’ from the insertion of the plate in the oven. The effect of the ramp is to require further 8’.

Cure profile (PID8692)

| Sample | Material | PID | Temp cure | Oven time | Equivalent cure time | Tg1 (°C) | Peak Tan  (°C) | Tg2(°C) | Delta H (J/g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | SF95 | 8695 | 120 | 68 | 60' | 111.16 | 128.34 | 111.19 | - |
| 2 | ST86 CBS |  | 120 | 68 | 60' | 117.25 | 134.8 | 115.71 | - |
| 3 | SF95 | 8692 | 130 | 38 | 30' | 110.66 | 125.78 | 105 | - |
| 4 | ST86 CBS |  | 130 | 38 | 30' | 119.74 | 138.58 | 122.27 | - |
| 5 | SF95 | 8705 | 130 | 28 | 20' | 105.03 | 121.92 | 98.74 | - |
| 6 | ST86 CBS |  | 130 | 28 | 20' | 108.6 | 136.54 | 92 | - |
| 7 | SF95 | 8694 | 130 | 48 | 40' | 113.8 | 128.16 | 111.23 | - |
| 8 | ST86 CBS |  | 130 | 48 | 40' | 112.17 | 133.96 | 119.26 | - |
| 9 | SF95 | 8693 | 135 | 30 | 20' | 106.92 | 126.66 | 103.08 | - |
| 10 | ST86 CBS |  | 135 | 30 | 20' | 115.68 | 138.52 | - | - |
| 11 | SF95 | 8691 | 135 | 40 | 30' | 112.54 | 128.1 | 108.34 | - |
| 12 | ST86 CBS |  | 135 | 40 | 30' | 116.6 | 142.56 | 112 | - |

The DSC trace showed an enthalpy peak only in the ST86 sample of the PID8705, correspondent with the worst condition of 20’@130(C.

Tg1 for ST86 – SF95

Tg1, Peak Tan d and Tg2 for SF95

Tg1, Peak Tan d and Tg2 for ST86 CBS

Some DMTA values found for ST86 CBS (40’@130(C and 30’@135) are not coherent.

# Conclusions

SF95: The Tg1 expected is about 115(C, the values found range from 105 to 114, with 111 for the “standard” cure cycle of 60’ at 120(C. Taken that as reference the 30’ at 130(C cure is equivalent, 20’ at 135(C instead appear to be slightly under-cured. The fastest cure could be 25’ at 135(C.

ST86 CBS: Tg1 expected about 115(C, the values found range from 109 to 120. As for SF95 the 30’ at 130(C is equivalent and 25’ at 135(C can be considered the minimum.