# Appendix 5.8 – 3-Ply laminate Data Batches 2 and 3

Batch 2

| Sample No. | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Maximum Force (N) | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1069.04 | 1.51 | 12.53 | 0.79 | 20226.60 | Cup/cone ductile failure |
| 2 | 1204.75 | 1.38 | 12.54 | 0.80 | 20848.52 | Through thickness shear |
| 3 | 1148.44 | 1.42 | 12.49 | 0.80 | 20368.44 | Complex |
| 4 | 1222.37 | 1.4 | 12.49 | 0.83 | 21374.42 | Complex |
| 5 | 1269.32 | 1.45 | 12.48 | 0.88 | 22969.59 | Through thickness shear |
| 6 | 1164.44 | 1.45 | 12.49 | 0.82 | 21088.55 | Through thickness shear, delamination and there are some cup/cone ductile failure |
| 7 | 1108.81 | 1.41 | 12.52 | 0.77 | 19574.13 | Complex some cup/cone ductile |
| 8 | 1355.25 | 1.47 | 12.51 | 1.01 | 24922.64 | Through thickness shear and then in plane shear |
| 9 | 1223.22 | 1.46 | 12.55 | 0.90 | 22413.14 | Through thickness shear initially some split plies and some ductile cup/cone failure on the upper and lower surface |
| 10 | 1180.38 | 1.42 | 12.54 | 0.84 | 21018.73 | Through thickness shear |

| Sample No. N=10 | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Young’s Modulus (GPa) | Maximum Force (N) |
| --- | --- | --- | --- | --- | --- | --- |
| Mean | 1194.60 | 1.437 | 12.51 | 0.84 | 148.10 | 21480.47 |
| Standard Deviation | 81.28 | 0.038 | 0.025 | 0.07 | 5.14 | 1569.02 |
| Variance | 6.80 | 2.67 | 0.20 | 8.34 | 3.47 | 7.30 |

Batch 3

| Sample No. | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Maximum Force (N) | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1131.87 | 1.41 | 12.52 | 0.80 | 19981.21 | In plane shear failure |
| 2 | 1186.30 | 1.47 | 12.53 | 0.86 | 21850.66 | In plane shear failure |
| 3 | 1315.31 | 1.46 | 12.51 | 0.96 | 24023.63 | Complex |
| 4 | 1316.88 | 1.43 | 12.54 | 0.95 | 23614.55 | Through thickness shear failure |
| 5 | 1321.51 | 1.39 | 12.53 | 0.93 | 23016.33 | Complex |
| 6 | 1235.75 | 1.44 | 12.54 | 0.88 | 22314.73 | Through thickness shear and brittle failure |
| 7 | 1302.94 | 1.35 | 12.55 | 0.90 | 22075.00 | Complex |
| 8 | 1157.19 | 1.41 | 12.54 | 0.80 | 20460.67 | In plane shear |
| 9 | 1102.50 | 1.35 | 12.59 | 0.72 | 18738.57 | Through thickness shear |

| Sample No. N=10 | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Young’s Modulus (GPa) | Maximum Force (N) |
| --- | --- | --- | --- | --- | --- | --- |
| Mean | 1230.03 | 1.412 | 12.54 | 0.87 | 149.08 | 21786.15 |
| Standard Deviation | 87.79 | 0.043 | 0.023 | 0.08 | 4.36 | 1751.15 |
| Variance | 7.14 | 3.06 | 3.06 | 9.10 | 2.93 | 8.04 |