# Appendix 5.25 – Paint Process

| Gurit Paint Process |  |  |  |
| --- | --- | --- | --- |
| Ensure you are familiar with PPE AND Health and safety requirements before commencing. Refer to product MSDS and TDS as required. |  |  |  |
| Step | Process | Comments | Care Point |
| Panel Preparation | Degrease | Degrease panel with 3911W water based degreaser using wipe on wipe off process | Change clothes frequently. Minimum 1 wet and 1 dry. |
|  | Degrease | Degrease panels with 3608S solvent based degreaser using wipe on wipe off process | Change clothes frequently. Minimum 1 wet and 1 dry. |
|  | Abrade | Sand surface lightly with P320 using block to remove resin residue and minor defects | Do not break through to substrate |
|  | Tak | Tak off panel | Do not touch panel with bare hands. D3047 Gamos Tak. |
|  | Blow off | Blow off panel | RW Greef #610501257 |
|  | Degrease | Degrease panels with 3608S solvent based degreaser using wipe on wipe off process | Change clothes frequently. Minimum 1 wet and 1 dry. |
|  | Tak | Tak off panel | Do not touch panel with bare hands. |
|  | Blow off | Blow off panel with de-ionised air |  |
| Primer Application | 2 coats |  |  |
|  | Mixing ratio | Activate DP5150 at 2:1 with DP3170 and adjust viscosity to 19 seconds +/- 1 second @ 19°C using 3365 thinner. Pot life is 60 to 90 minutes once activated. | Use thread protectors for exposed riv nuts to prevent paint build up. |
|  | Booth Setup | 18.3°C 0.52m/s airflow, 45% RH |  |
|  | Spraygun Setup | Use GTI gravity fed spray gun. Use 1.3mm fluid tip and aircap 110. Air pressure 2.2 bar at the heel gun. |  |
|  | Flash B/T Coats | 10 mins between coats |  |
|  | Flash B/F Bake | 30 minutes at 18.3°C 0.52m/s airflow, 45% RH | Ensure humidity is above the minimum |
|  | Bake Time | 45 minutes at 70°C on the gauge, air temp 68-69°C, panel temp 66-68°C (at 1 m distance from the floor) |  |
|  | Film Build | 90-100 microns |  |
|  | Cool | Cool to ambient temperature before sanding |  |
| ## Inspection | Sanding | Use P400 soft sponge abrasive on edges and contours |  |
|  | Tak | Tak off panel | Do not touch panel with bare hands. |
|  | Blow off | Blow off panel |  |
|  | Degrease | Degrease panel with 3911W water based degreaser using wipe on wipe off process | Change clothes frequently. Minimum 1 wet and 1 dry. |
|  | Tak | Tak off panel | Do not touch panel with bare hands. |