Development of CFRP Class A Body Panels and Structural Components for Automotive Applications


Appendix 5.25 – Paint Process 

	Gurit Paint Process

	Ensure you are familiar with PPE AND Health and safety requirements before commencing. Refer to product MSDS and TDS as required.

	Step
	Process
	Comments
	Care Point

	Panel Preparation
	Degrease
	Degrease panel with 3911W water based degreaser using wipe on wipe off process
	Change clothes frequently. Minimum 1 wet and 1 dry.

	
	Degrease
	Degrease panels with 3608S solvent based degreaser using wipe on wipe off process
	Change clothes frequently. Minimum 1 wet and 1 dry.

	
	Abrade
	Sand surface lightly with P320 using block to remove resin residue and minor defects
	Do not break through to substrate

	
	Tak
	Tak off panel
	Do not touch panel with bare hands. D3047 Gamos Tak.

	
	Blow off 
	Blow off panel
	RW Greef #610501257

	
	Degrease
	Degrease panels with 3608S solvent based degreaser using wipe on wipe off process
	Change clothes frequently. Minimum 1 wet and 1 dry.

	
	Tak
	Tak off panel
	Do not touch panel with bare hands.

	
	Blow off
	Blow off panel with de-ionised air
	

	Primer Application
	2 coats
	

	
	Mixing ratio
	Activate DP5150 at 2:1 with DP3170 and adjust viscosity to 19 seconds +/- 1 second @ 19°C using 3365 thinner. Pot life is 60 to 90 minutes once activated.
	Use thread protectors for exposed riv nuts to prevent paint build up.

	
	Booth Setup
	18.3°C 0.52m/s airflow, 45% RH
	

	
	Spraygun Setup
	Use GTI gravity fed spray gun. Use 1.3mm fluid tip and aircap 110. Air pressure 2.2 bar at the heel gun.
	

	
	Flash B/T Coats
	10 mins between coats
	

	
	Flash B/F Bake
	30 minutes at 18.3°C 0.52m/s airflow, 45% RH
	Ensure humidity is above the minimum

	
	Bake Time
	45 minutes at 70°C on the gauge, air temp 68-69°C, panel temp 66-68°C (at 1 m distance from the floor)
	

	
	Film Build
	90-100 microns
	

	
	Cool
	Cool to ambient temperature before sanding
	

	Inspection
	Sanding
	Use P400 soft sponge abrasive on edges and contours
	

	
	Tak
	Tak off panel
	Do not touch panel with bare hands.

	
	Blow off
	Blow off panel
	

	
	Degrease
	Degrease panel with 3911W water based degreaser using wipe on wipe off process
	Change clothes frequently. Minimum 1 wet and 1 dry.

	
	Tak
	Tak off panel
	Do not touch panel with bare hands.








C A Squires


237

