#### Table of Contents

ENGINEERING DOCTORATE INTRODUCTION					2

ABSTRACT											3

PUBLICATIONS										4

ACKNOWLEDGEMENTS									5

TABLE OF CONTENTS									6

TABLE OF FIGURES									11

LIST OF TABLES										15

1. Introduction										19

  - Structural Applications of CFRP in the Automotive Industry		19

  - Surface Characterisation of CFRP Composites				20

2. Structural Applications of CFRP within the Automotive Industry		22

  - Introduction 									22

  - Carbon Fibre Composites							22

    - 0° Unidirectional Carbon Fibre					23

    - Carbon Composite Classifications				25

  - Compression Testing							26

    - Compression Testing Methods					26

    - IITRI Compression Test Method					27

    - ASTM Standard D 695 Modified					28

    - Background								28

    - Previous Data							29

  - Geometric Effects								30

    - Thickness Effects							31

    - Edge Effects								33

    - Surface Effects							34

  - The Effects of Voids/Defects 						35

    - Issues Associated with CFRP as a Structural Component	35

    - Voids, Fibre Volume Fraction and Matrix Effects		36

    - Fibre Waviness and Fibre Misalignment				38

    - The Effect of Defects on Failure Mechanisms			39

  - Typical Failures								40

    - Environment Induced Failures					42

  - Analytical Models								43

    - Mathematical Models						43

    - Finite Element Analysis Approaches				46

  - Summary									48

  - Experimental Methodology							49

    - Unidirectional Carbon Fibre Test Panel Production		49

    - Curing Cycle for the Test Panel					51

    - Tabbing of the Test Panel						52

    - Mechanical Testing							54

    - Analysis of Results							55

    - Experimental Variation						56

      - Thickness Variation					56

      - Edge Variation						57

      - Surface Variation					58

    - Analytical Techniques						60

      - Optical Microscope					60

      - Scanning Electron Microscope (SEM)		61

      - Talyscan							62

      - X-Ray Tomography Unit				63

  - Results and Discussion							65

    - Thickness Quantification						65

    - Test Programme Methodology					67

    - Edge Quality Assessment						68

    - Surface Quantification						72

    - Independent Test Centre Results					76

    - Test Facility Differences						77

    - X-Ray Tomography – Failure Progression Analysis		81

  - Discussion									90

    - Effects of Manufacture						90

    - Effect of Edge Quality and Surface Preparation			90

    - Effect of Compression Rig Design				91

    - Failure Modes							92

    - X-Ray Tomography – Failure Progression Analysis		94

  - Conclusions									95

3. Surface Characterisation of CFRP Composites					96

  - Introduction									96

  - Car Body Sheet (CBS)							96

  - Defects in a Class A Surface						99

    - Porosity within a Carbon Prepreg Substrate			100

    - Print Through (Fibre Strike Through)				101

    - Long and Short Term Waviness					103

  - Methods for Assessing Surface Quality					105

    - Surface Roughness							106

    - Commercial Industry Standards					108

  - Environmental Characterisation						110

    - LAB Colour Change							112

    - Specular Gloss							115

  - Summary									116

  - Experimental Methodology							117

    - Manufacturing Route for CBS 95					117

      - Kitting of the Aston Martin DB9 Bonnet		117

      - Lay-up of the Aston Martin DB9 Bonnet		120

    - Analytical Methods							122

      - Proscan 2000						122

      - Polishing Method					124

      - Optical Microscope					125

      - Dynamic Mechanical Analysis (DMA)			126

      - Thermal Imaging Camera				128

    - Environmental Analysis						128

      - MINOLTA Spectrophotometer CM-500 Series	128

      - Gloss Analysis						129

  - Results and Discussion							130

    - Porosity: Sink Marks and Pin holing				131

    - Worm Tracks								139

    - Fibre Bridging							141

    - Teddy Bears Ears							146

    - Print Through							150

    - Environmental Effects on CBS 95					158

      - LAB Colour Change					158

      - Test Verification						164

      - Microscopical Analysis					166

  - Discussion									169

    - Surface Anomalies							169

    - Environmental Effects						171

  - Conclusions									173

4. Discussions and Major Conclusions						174

  - Structural Applications							174

  - Surface Characterisation							175

    - Environmental Characterisation					177

  - Major Conclusions								179

  - Further Work									181

    - Structural Applications 						181

    - Surface Characterisation						182

5. Appendices										184

  - Works Instruction 								184

  - T600-50C Data Sheet							193

  - Resin Data Sheet								194

  - Cure Cycle Data								199

  - Euler Buckling Equations							200

  - Fishbone Diagram								201

  - 2-Ply Laminate Data							202

  - 3-Ply Laminate Data							203

  - 4-Ply Laminate Data							205

  - 5-Ply Laminate Data							207

  - Compressive Test Data from Edge Quantification Panels		208

  - Student t Test								211

  - ITC Test Results								212

  - Gurit UK Test Results							213

  - Wet and Dry Panel Compressive Data					215

  - Grit Blasting Panels Compressive Data					217

  - Release Stitch A Compressive Data					218

  - Release B Compressive Data						219

  - Release Stitch G Compressive Data					221

  - CT Scan Specimens							223

  - CBS 86 and SF 95 Data Sheets						224

  - Arizona Environmental Test Description					234

  - Florida Environmental Test Description					235

  - Ohio Environmental Test Description					236

  - Paint Process								237

  - Cure Optimisation								238

6. Glossary of Terms									242

7. References and Bibliography								245