# 2.	Structural Application of CFRP within the Automotive Industry

2.1	Introduction

There has been significant increase in research on testing of composite fibre tensile properties. However, this effort has not resulted in any improvement of the reliability of compressive testing for composite materials, which becomes the design limit in engineering applications. Composites are becoming a common material choice in many engineering applications. However, these applications are not only exposed to tensile stresses, they are also under compressive and shear. There is very little research into the relationship between compressive testing of a test specimen and the validity of the result related to real life applications. It is critical that the compressive strength for a given material used in engineering applications i.e. a car chassis, is reliable and maintains repeatability and reproducibility.

The purpose of this present review is to research the factors that influence the repeatability and reproducibility of the final compressive test specimen. First, there is a review of the common testing methods, followed by an assessment of the previous data that has been accumulated by Gurit. A survey of geometric effects that may dominate the failure mechanism of the compressive test specimen is given, followed by a review of the failure mechanisms of the compressive specimens. Finally, there is a review of the existing mathematical and computational models, which try to predict the compressive strength of unidirectional lay-ups.

2.2	Carbon Fibre Composites

Carbon fibre is a high strength, high modulus synthetic fibre that is used in a variety of structural and electrical applications. Carbon fibre is most commonly manufactured by heating, oxidising, and carbonising polyacrylonitrile polymer fibres, which gives the best carbon fibre properties, but fibres can also be made from pitch or cellulose. The resulting carbon fibres are typically moulded with a polymer matrix into high strength composite materials for structural applications or are used in their pure form for electrical and friction applications.

Carbon fibre composites have competitive structural properties compared to traditional materials. They are up to six times stronger than steel in the dominant fibre direction, yet five times lighter in overall component weight. In comparison to aluminium, carbon fibre composites are eight times stronger, twice as stiff yet still 1.5 times lighter [1]. These properties are only achievable as composites can be tailored to have dominant characteristics for the specific application that it is being designed and manufactured for.

2.2.1	0( Unidirectional Carbon Fibre

A unidirectional (UD) fabric is one in which the majority of fibres run in one direction only. A small amount of fibre or other material may run in other directions with the main intention being to hold the primary fibres in position, although the other fibres may also offer some structural properties. True unidirectional fabrics offer the ability to place fibre in the component to give reinforcement exactly where it is required, and in the optimum quantity (no more or less than required). As well as this, UD fibres are straight and un-crimped (crimping is when there is waviness present in the fabric). This results in the highest possible fibre contribution (in the fibre direction) from a fabric in composite component construction. For mechanical properties, unidirectional fabrics can only be improved on by the use of prepreg unidirectional tape, where there is no secondary material at all holding the unidirectional fibres in place. In these prepreg products only the resin system holds the fibres in place, Figure 2.1 is a schematic diagram of a unidirectional material.

Figure 2.1 – Example of unidirectional fibres

There are various methods of maintaining the primary fibres in the unidirectional position, including weaving, stitching, and bonding. As with other fabrics the surface roughness of a unidirectional fabric is determined by two main factors; the combination of tex and thread count of the primary fibre, and the amount and type of the secondary fibre. The drape, surface smoothness, and stability of a fabric are controlled primarily by the construction style. While the areal weight, porosity, and (to a lesser degree) wet out, are determined selecting the appropriate combination of fibre tex and numbers of tows per cm.

Warp or weft unidirectional material can be made by the stitching process (warp knitting). However, in order to gain adequate stability, it is usually necessary to add a mat or tissue to the face of the fabric. Therefore, with the amount of stitching thread required to assemble the fibres, there is a relatively large quantity of secondary, parasitic material in this type of UD fabric, which tends to reduce the laminate properties e.g. if a certain weight is specified for a component, but if warp knitting is required then some of the weight is consumed in the transverse direction, therefore reducing the unidirectional material, thus reducing the stiffness. Furthermore, the high cost involved in the set up of the 0( layer of a stitching line and the relatively slow speed of production means that these fabrics can be relatively expensive compared to the manufacture of unidirectional prepreg material.

2.2.2	Carbon Composite Classifications

Carbon fibres are usually grouped according to the modulus band in which their properties fall, these bands are (Figure 2.2 – [2]):

- Commercial Grade Carbon (CGC)

- High Strength Carbon (HSC)

- High Elongation Carbon (HEC)

- Intermediate Modulus Carbon (IMC)

- High Modulus Carbon (HMC)

Figure 2.2 – Tensile properties for a select number of the carbon fibres available to construct unidirectional material are shown, as characterised by the five categories above

The properties of the carbon fibres in Figure 2.2 are the individual fibres tested without any resin. However when fibres are incorporated into a resin matrix it then becomes possible to measure the properties of the fibres in compression or under shear.

The filament diameter of most types of fibre is 5-7 (m, these are then collected together to form a tow. A tow can be anything from 6000 filaments and multiples of this thereafter up to 48,000. The tow sizes are used to determine the weight of the fabric produced, so the more filaments within the tow the heavier the fabric will be.

2.3	Compression Testing

Despite three decades of research efforts to date, composite compressive strength still remains an unresolved subject in the understanding of the behaviour of composites. Prior to 2003, no reliable analytical or empirical expression has been obtained which can provide reasonable predictions or assessment of the compressive strength of unidirectional composites [4]. Recent research activities in this area are concentrated mostly on improving the testing techniques. Previous research found that although significant progress has been made in characterising the behaviour of unidirectional composites under compression, no similar advancement has been achieved in predicting and understanding compressive strength [3].

Unlike tensile properties, the resin matrix in which they are placed heavily influences the compression and shear properties of composites. Here, the resin has to hold the fibres straight as columns when loaded in compression. It is the adhesive properties of the resin to the fibres that come into play under shear. Furthermore, some composites behave quite differently under compressive loading, due to their molecular structure.

2.3.1	Compression Testing Methods

At present, the most commonly used test configuration for determining the compressive properties of high performance unidirectional composite materials is a specimen of uniform width and thickness, with adhesively bonded tabs at each end (Figure 2.3). To load this specimen the two most common methods currently in use are the IITRI (Illinois Institute of Technology Research Institute) compression test method, defined by ASTM Standard D 3410 [4], which introduces loading via shear transfer using wedge grips, and ASTM D 695 (Modified) [5], which introduces the loading directly on the ends of the specimen.

Figure 2.3 – Example of a compression test specimen

2.3.2	IITRI Compression Test Method

The IITRI method was developed to avoid seating problems encountered when using the conical wedges of the older style Celanese rig [6]. The load is introduced by shear onto the tabbed regions of the compressive test specimen using a wedging action. The gauge length is 12.7mm. The IITRI Test rig is shown in Figure 2.4.

Figure 2.4 – Schematic of the IITRI compression test fixture – [6]

2.3.3	ASTM Standard D 695 Modified

The ASTM D 695 M method is widely used throughout the composites industry. This method is primarily intended for testing rigid polymers but does include high performance composites within its scope. It involves lightly clamping the specimen to a thick steel plate so it cannot buckle. The ends protrude about 3mm beyond the plate and loading is directly through the ends. The gauge length is recommended to be 10mm, and the specimen is limited to a width of 12.5mm. Figure 2.5 shows an example of the ASTM D 695 test rig.

Figure 2.5 – ASTM D 695 M Compression test rig

2.3.4	Background

The IITRI and Modified ASTM D 695 test methods have become the most widely used shear and end loaded test fixtures, respectively [7]

The IITRI was added to ASTM 3410 in 1987, as method B. This method is generally perceived as generating acceptable results with minimal data scatter when performed properly. Although this test method is frequently used to determine the compressive response of composite materials, it is not without it shortfalls. The most widely voiced complaint [7] about the IITRI test method is the mass of the fixture itself, some 45kg. In addition to being physically difficult to handle, the mass of the IITRI fixture increases the fabrication cost. However, the IITRI test method remains the most popular shear-loaded test method to determine the compressive response of composite materials.

One other compression test in use at the present time is the ASTM D 695 Modified test method. This method is simple to use, the rig is relatively inexpensive to fabricate. One common complaint of the D 695 Modified test method is that it must make use of two separate specimens to obtain both compressive strength and modulus [7]. The strength determination is made using a tabbed specimen with a relatively short (10mm) gauge section. This short gauge section is required to prevent gross buckling of thin (1-2mm) test specimens. The use of such a short gauge section was an early criticism of this test method, until studies indicated that the gauge length does not influence the measure of compressive strength provided buckling is prevented [8].

One aspect of the D 695 fixture, which is frequently overlooked, is the bolt torque used to clamp the stabilising lateral supports together. Increased bolt torque allows more of the applied load to be carried by the lateral supports through friction, thus increasing the (apparent) compressive strength.

2.3.5	Previous Data

Recently, Gurit have been improving their production, manufacturing and testing techniques as part of continuous improvement activities to address these issues and improve the test variation within the compression testing results. The alterations that Gurit have introduced over the last few years have had a positive effect by increasing their compressive strength results for HSC 500 (500gsm) unidirectional carbon specimens with a fibre volume fraction of 55% from an average of 800MPa to 1000MPa. In Figure 2.6, the compressive test results achieved by Gurit have been plotted (data accessible to date).

Figure 2.6 – Data from the Gurit Testing Data Base - [9]

Figure 2.6 is to be interpreted as a spread of results that gives a trend example. The range means for this data are highly varied, this could be due to several factors:

- The operator that manufactured and tested the specimens

- The preparation method used

The compressive strength of unidirectional fibre composites is an important parameter but is nevertheless much misunderstood. There is neither agreement on how to measure it, or what are the physical processes that give rise to failure. It is important because it provides a limiting design criterion. Furthermore, we cannot start to understand the compressive failure of more complex laminates until we understand that of the simplest, for example unidirectional laminates.

2.4	Geometric Effects

The geometric effects that can influence the compressive strength of a unidirectional carbon test specimen are thickness of the specimen, the condition of the edges (the rougher the edges are the more likely cracks can initiate), and the condition of the surface of the specimen (if the surface has been poorly treated, there is an increased chance of fibre damage). There are also internal defects that can affect the compressive test specimen such as voids, FVF and matrix, these are discussed later in Section 2.5.

2.4.1	Thickness Effects

The number of fibres per cm can define at a given fibre volume fraction the weight of the fabric and this in turn defines the ply thickness. The different weights of cured unidirectional carbon fibre are defined in Table 2.1 with the corresponding ply thickness (these values have a 2% tolerance level for the acceptance criterion).

|  | Fibre volume fraction |
| --- | --- |
|  | 0.35 | 0.36 | 0.44 | 0.48 | 0.52 | 0.56 |
| Fibre weight g/m² | Ply thickness (mm) |
| 150 | 0.24 | 0.23 | 0.19 | 0.17 | 0.16 | 0.15 |
| 200 | 0.32 | 0.31 | 0.25 | 0.23 | 0.21 | 0.20 |
| 300 | 0.48 | 0.46 | 0.38 | 0.35 | 0.32 | 0.30 |
| 400 | 0.63 | 0.62 | 0.51 | 0.46 | 0.43 | 0.40 |
| 450 | 0.71 | 0.69 | 0.57 | 0.52 | 0.48 | 0.45 |
| 500 | 0.79 | 0.77 | 0.63 | 0.58 | 0.53 | 0.50 |
| 600 | 0.95 | 0.93 | 0.76 | 0.69 | 0.64 | 0.60 |

Table 2.1 – Ply Thickness Data from the Gurit Composites Materials Handbook [2]

Few researchers have investigated the effect of laminate thickness on the compressive behaviour of unidirectional carbon fibre composites. This is due to the difficulty in obtaining reliable test results. Existing test methods have not provided precise compressive properties to date of thick composite laminates (2.5mm and above) due to the fact that all problems related to testing become more serious and complicated with thicker composites. As the specimen increases in thickness, a higher percentage of the load must be transmitted at the end, thus increasing the chances of premature failure such as end crushing (Figure 2.7) – for more details refer to Section 2.6.

Figure 2.7 – Image showing end failure mechanism

Lee and Soutis [10] found from post failure examination, that brooming failure (transverse splitting of the composite) combined with longitudinal splitting, interlaminar cracking, fibre breakage and kink-band formation (fibre microbuckling) were all observed in specimens that were 2-3mm thick. The brooming failure was located near the tab ends suggesting that local stress concentration may be partly responsible for this type of failure.

In the thicker specimens of 4-8mm, failure occurred at the ends of the specimens (Figure 2.8) at the load introduction point. The measured failure strengths of these thicker specimens were less than that obtained from the thin specimens (2-3mm). This type of failure was not observed with the thinner specimens. Figure 2.8 has been taken from [10]. There is evidence to show that as the specimen increases in thickness the apparent compressive strength decreases.

Figure 2.8 – Average compressive strength as a function of specimen thickness for T600/924C unidirectional laminates – [10]

Figure 2.8 suggests that the optimum thickness for the compressive specimen is 2mm. The thickness of compressive specimens recommended in BS EN ISO 14126:1999 [11] is 2mm ( 0.2mm. The ASTM D695 Modified [5] standard recommends a thickness of 2mm ( 0.5mm.

Dr Adams [12] of Wyoming Test Fixture Inc has been studying the compressive test method for more than 20 years and his recommendation for specimen thickness of a compressive test specimen is 2.5mm, which is 0.5mm thicker than current international standards recommend (ASTM D695 M). However, increasing the thickness of composite materials may increase the likelihood of multiple flaws being grouped in the same local area. There may also be offsetting improvements due to larger size, such as the likely arrest of damage as it spreads from local stress concentration areas, which is not present in test coupons due to their small size and cut edges.

A number of production-related variations may occur in larger structures, which are more easily avoided in smaller structures, and should not appear in test coupons. Typical of these are fabric joints and overlaps where individual rolls of fabric terminate, and flaws in the fabric where individual strands terminate during production of the fabric. Other factors, which are more likely in larger components, include fibre waviness, large-scale porosity, large resin rich areas, and resin cure variations through the thickness.

2.4.2	Edge Effects

The quality of the edge of compressive specimens is significant to a compression strength test. Odom and Adams [12] proposed a sequence of events for the failure of a specimen whose final failure mode was described as transverse, branched transverse or split transverse. The model is shown in Figure 2.9 below, but these indicate that the initial failure occurs at, or near, one free edge of the specimen. They also suggest that although the area, location and propagation of the crack initiation vary along the free edge the occurrence was observed repeatedly.

Figure 2.9 – Failure Progression for compression specimens exhibiting transverse failure modes – [12]

2.4.3	Surface Effects

The surface of a compressive specimen is determined by the method of compressive test that is to be used. The compression testing methods discussed in the following Section 2.5 use a tabbed specimen as shown in Figure 2.3. Due to the nature of this compressive test specimen the surface of the carbon fibre component has to be of suitable roughness to guarantee very good secondary adhesion for the tabbing. This process indicates that the carbon specimen has to have had some kind of surface preparation technique in order to guarantee the secondary adhesion. On the other hand, the surface cannot be too rough as this has been known to induce fibre kinking [13].

Release ply fabrics such as peel plies are used as release materials directly against laminates or bond lines where a clean textured finish is required for subsequent bonding or painting. Using peel ply when laying up the test laminate is a very inviting option as it is easy to incorporate, and it also reduces contamination within the panel as it seals off the surfaces, rather than them being exposed to the atmosphere. However, there have been past incidents at Gurit UK and generally within the composites industry [peel ply paper] when the peel ply itself has been contaminated during manufacture, resulting in poor quality laminates. There are different grade meshes available – depending upon the surface roughness required, and they are produced either from Nylon( or polyester.

Surface preparation techniques can also be used, these include grit blasting and the use of sandpaper (hand or machine to abrade or “key” the surface). These methods are not as desirable as the use of peel plies in manufacturing as they are an additional stage in the manufacturing process, which therefore adds time and further cost to the process. There is a higher risk of contamination to the laminate as it is exposed to the atmosphere during manufacture. The process generates dust and debris which if not removed can act as a weak-bonding layer between the laminate and the tabbing. These abrasion processes are operator sensitive process, therefore can be very aggressive, poorly controlled and unrepeatable. This can lead to the formation of stress raisers and the unintended reduction in sample thickness.

2.5	The Effects of Voids/Defects and the Environment

Voids are one of the most common defects encountered during the manufacture of carbon fibre reinforced polymers and can have detrimental effects on the mechanical properties of the material. In general, such flaws cause a decrease in the strength of the laminate and leave it exposed to greater susceptibility to water penetration and environmental conditions [13].

Voids are not the only defects that affect the mechanical properties of unidirectional carbon fibre detrimentally. The other defects that will be discussed in the following sections are fibre volume fraction, matrix effects, fibre waviness, fibre misalignments, fibre fracture and kink bands.

2.5.1	Issues Associated with CFRP as a Structural Component

The manufacturing of CFRP can introduce a range of defects. For example, misalignment can occur when the tows are fed into to the prepreg machine and are not aligned perpendicular to the centre point. Also the intermediate handling and storage of the CFRP can affect the condition, and even through to the final cure cycle where temperature, dwell time and vacuum level play important roles in the overall quality of the laminate.

The mechanisms operating in composites during loading, damage progression, failure modes, and ultimately strength are all affected by the nature and micro-geometry of the composite components; fibres, matrix, and interface. For example, the properties of a unidirectional composite are highly sensitive to the degree of fibre alignment, which affects the mechanisms that operate during loading, and the failure mode. The matrix, used in carbon/epoxy systems, is ductile compared with the fibres, and its main role is to transfer load to the fibres. Since the modulus of the matrix is significantly lower than that of the fibres it is carrying only a small portion of the applied load.

2.5.2	Voids, Fibre Volume Fraction and Matrix Effects

One of the most common categories of manufacturing defects are voids, these are areas of trapped air that are found within the resin and between plies/fibres within composites.

Micrographic studies have revealed that voids are the commonest of all defects found in vacuum bag mouldings. The types of voids, which occur in fibre-reinforced plastics, have been classified in many different ways over the years, e.g. the terms thread-, fabric-, general-, interstitial-, planer-, micro-, needle-, pocket-, and interconnected-voids have all been used [14, 15, 16, 17]. These different terms can, however, be reduced to two basic types – voids along individual filaments (within fibre bundles or tows) and voids between lamina. At low void contents (< 1.5%) the shape tends to be spherical and of diameter 5-20(m. At higher contents the voids are cylindrical and the length can be an order of magnitude greater than the diameters quoted [18]. In general the larger dimension is oriented parallel to the fibre axis.

There are several causes of void formation, but only two of these have been the focus of significant study and modelling [15,19]. Firstly, the entrapment of gases (most often wet air), and secondly, volatiles arising from the resin itself. The trapped air originates from the different stages of the manufacturing process, (1) from the initial manufacturing stage, due to either air bubbles being trapped in the viscous resin or between the fibres and (2), voids may be formed by volatile components or contaminates, which vaporise during the high temperature part of the cure cycle. Hence the voids are areas within the composite where there are no matrix or fibres present.

Work conducted by Sharez et al [20] showed a clear relationship between void content and compressive strength. They found a 10% reduction in compressive strength for every 1% increase in void content. This trend, however, was only found to be true for materials with a void content of less than 4%. At a greater void content than this, the trend was not uniform. This gives some clues as to the homogeneity of the material, and suggests that at lower void contents, the voids are distributed more evenly.

Budiansky and Fleck [21] suggest that voids may contribute to the compressive failure of composites. They largely attribute failure initiation to fibre microbuckling, but imply that as the void content increases, the initial fibre misalignment increases. However, there are reports [13] that state if the void content remains under 1% of the total measured volume the effect that the voids will have on the overall mechanical properties of the laminate are negligible.

The interfaces play an important role in the behaviour of the composite. As adhesion between the fibres and matrix improves, the load transfer is more efficient and the mechanical characteristics of the composite are enhanced. In addition, the interface strength affects the path of crack propagation in the material. For example, Wo [22] shows that if the interface is weaker than the matrix, a crack that initiates perpendicular to the fibres may turn and propagate parallel to them along the interface. Additionally, Fibre Volume fraction (FVF) plays an important role in the strength and quality of the laminate. The fibre volume fraction can be calculated using the following equation:

Equation 2.1 - [23]

Where FWF = Fibre Weight Fraction.

The Rule of Mixtures (given below) supports this; this states that the modulus of a unidirectional fibre composite (EC) is proportional to the volume fractions (FVF and MF (Matrix fraction)) of the material in the composite.

Equation 2.2 – [23]

2.5.3	Fibre Waviness and Fibre Misalignments

It is important to distinguish between fibre waviness and fibre misalignments. Fibre waviness can be defined by a distinctive sinusoidal type of wave for the fibre, as well as fibre mis-orientation with respect to the neutral fibre axis (x-direction). Fibre misalignment is defined as the partial or localised mis-orientation of the fibres with respect to the neutral axis only and this can lead to kinking of the fibres [24].

Unidirectional prepregs are stored on large rolls (in excess of 100 linear metres) after manufacture, which is a possible cause for induced waviness. The fibre waviness at this stage will depend on the tightness and diameter of the roll of uncured material. Fibre misalignment is thought to originate in the manufacturing of fibre tows (i.e. fibre bundles) in the prepregs. This problem can also appear during the laying up process, as it is very hard and time consuming to position/align every ply with respect to the previous one, such that all fibres are perfectly aligned in the unidirectional fibre reinforced composite structure.

Fibre waviness is thought to occur as a result of a variety of manufacturing induced phenomena in polymer-matrix continuous fibre composites. These include mismatches in thermal expansion between the fibre, matrix and tool plate, the temperature gradients or temperature history experienced by the part during processing, volumetric shrinkage of the matrix, visco-elastic nature of the matrix and consolidation of the uncured material [25].

Figure 2.10 shows three types of fibre orientation in identical composite panels under the same loading conditions. Panel A will have the optimum mechanical properties because the fibres are perfectly aligned and parallel to the loading axis. Panels B and C will suffer from a significant reduction in compressive strength and stiffness because of the fibre mis-orientation defects present in them. Joyce et al [26] concluded that straight fibre regions are relatively stiff and strong in the main loading direction, and wavy or misaligned fibre regions are relatively compliant and weak.

Figure 2.10 – Fibre orientation relative to loading – [26]

2.5.4	The Effect of Defects on Failure Mechanisms

Many potential engineering applications for high performance composite laminates involve compressive loading. Therefore, the compressive response of unidirectional composites is an essential part of the basic property data required for design optimisation. Compressive strength is one of the dominant limiting factors, as the compressive strength of the fibre reinforced polymer composite is usually 50-60% of their tensile strength [8]. Compressive deformation behaviour of unidirectional composites is influenced by many factors, including fibre and matrix properties and manufacturing induced imperfections such as voids. Given the complexities involved in the compressive deformation behaviour of unidirectional composites, many compressive failure mechanisms for unidirectional composites were analysed and observed.

The nature of compressive failure in unidirectional composite laminates has been examined by researchers. Orringer [27], Shuart [28] and Hahn [29], have presented reviews of compressive failure in these laminates. One of the main problems has been to develop suitable test methods. Existing common test methods have been reviewed previously in Section 2.3. In this section we deal with the failure mechanisms. It will be shown from the literature that the failure in unidirectional laminates is dominated by the geometric defects within the specimen.

2.6	Typical Failures

In BS EN ISO 14126:1999 [11] there is a list of allowable failures regarding the compressive test method, these are shown below in Figure 2.11.

Figure 2.11 – Acceptable failure mechanisms as stated by BS EN ISO 14126:1999-[11]

These failures are believed to originate from microbuckling within the fibres. The majority of the literature available concentrates on microbuckling as the primary failure initiator under axial compressive load. This research originated from the workings of Rosen in the mid 1960’s. Since Rosen’s [30] work, it is recognised that fibres in high volume fraction carbon fibre reinforced plastic unidirectional laminates deform in the shear mode of microbuckling. The in-plane buckling of the fibres places the matrix predominantly in shear, the fibres rotate and break in two places, forming a kink band. The fibres then rotate further until the matrix between the fibres fails, and the kink band and hence the laminate loses its load carrying capability.

According to Daniel and Hsiao [31], in all cases failure is matrix dominated. In the case of longitudinal loading, composite failure is triggered by matrix failure accompanied by fibre microbuckling and is greatly dependent on initial fibre misalignment. The longitudinal compressive strength shows a mild trend toward decreasing values with increasing thickness. Even if such a trend is significant, it was suggested that for initial fibre misalignments of the order of 1.5-2(, increasing laminate thickness would have a diminishing effect on strength

Jelf and Fleck [32] examined the compressive failure of unidirectional fibre composites, where they classified four failure mechanisms:

- fibre failure

- elastic microbuckling

- matrix failure

- plastic microbuckling

They found that plastic microbuckling was the dominant compressive failure mechanism in polymer matrix composites.

Compressive data are more difficult to generate than tensile data for carbon fibre reinforced composites. The material has a high ratio of compressive strength (in the direction of the fibres), to shear strength (in the planes parallel to the fibres). This causes problems with shear load input. For pure compression loading, transverse stresses are induced in the ends of the specimen due to Poisson deformation and this can cause brushing at the ends of the specimen. Instability is also a problem and is exacerbated by the low out-of-plane shear modulus of the composite.

With any particular procedure, failure will occur at the lowest possible strength and in the corresponding failure mode. The range of possible failure strengths implies that the ultimate compressive strength of a composite is not a precise term, but primarily one of definition. In the axial compression of unidirectional composites three basic failure modes can be observed [33]; local buckling of fibres (where production variations such as fibre waviness or non uniform fibre spacing can influence compressive strength, also known as complex failure), transverse rupture of the composite (due to differences in Poisson’s ratios of the material constituents and non uniform distribution of transverse strains over the specimen length, also known as transverse shear failure), and failure in compression (shearing of the fibres at an angle of 45 degrees with no local buckling of the fibres, also known as in-plane shear failure). These principal modes of failure can be accompanied by a series of other phenomena:

- inelastic and non-linear behaviour of fibres and matrix

- interlaminar stresses

- surface ply separation

- overall loss of stability

Different combinations of all these phenomena can make it very difficult to establish the failure mode or obtain consistent results even with the same material and test procedure.

2.6.1	Environment Induced Failures

Ewins and Ham [34] investigated failure mechanisms in carbon-epoxy as a function of temperature. They suggested that the failure mode of unidirectional carbon fibre composites at room temperature was shear failure and not microbuckling. At temperatures above 100(C, the reduction of matrix stiffness and matrix strength allowed the fibres to buckle so that the composite strength was determined by the matrix properties rather than by fibre strength. The tensile strength of the composite in the unidirectional orientation is a fibre-dominated property. In contrast, resin stiffness significantly influences compression strength and materials currently used tend to employ resins that have a lower stiffness. The main reason for this is that the higher the resin stiffness the more brittle the laminate tends to be.

Mei Li [35] concluded from experiments executed on materials for wind turbine blades that the compressive strength in the unidirectional orientation is a matrix dominated property and showed significant reductions under hot/wet conditions. It is concluded from the literature that environmental effects play a role in the determination of the compressive strength of a unidirectional carbon fibre composite.

2.7	Analytical Models

The compressive failure of long fibre composites is of major concern for the design of composite structures, since the compressive strength of practical laminates is significantly less than their tensile strength. Understanding the behaviour of materials/structures under compressive loading is essential for effective structural design. This is because the failure mechanism is controlled by compressive stresses in most cases.

In Section 2.6 it was previously discussed that many researchers believe that the initiator of failure under compressive loads is the fibre microbuckling mode, consequently the literature covering failure prediction models also use microbuckling as the primary failure initiator.

2.7.1	Mathematical Models

Compressive strength prediction has been the focal point of many investigators over the past few decades. Jones [36] presented the work of Rosen [30], in which it has been noticed that when fibre reinforced composites are compressed, the mode of failure appears to be fibre buckling.

Two modes of fibre buckling are possible:

- extension mode

- shear mode

Figure 2.12 – The two modes of fibre buckling – [30]

Rosen’s model is well known to overestimate the strength of some composites such as carbon/fibre epoxy. However, it has been the basis of many mathematical models that have evolved from it since the 1960’s.

Rosen [30] built the first analytical models based on two microbuckling modes (Figure 2.12). Fibres are treated as beams, and assumed to be perfectly straight. Matrix linear elasticity is also implicit. The critical stress is determined using an energy method [37]. For the shear or in-phase mode, the preferential mode for common high fibre volume fraction in composites, as obtained by Rosen is:

Equation 2.3 - [30]

Where Gm is the matrix shear modulus and FVF the fibre volume fraction. This expression overestimates the compression strength of carbon fibre reinforced composites, typically predicting values from 3 to 4 GPa. Non-linear matrix behaviour (matrix damage due to load) and fibre misalignments are usually held responsible for such overestimation.

Frost [38] proposed a theoretical model incorporating the features of Rosen’s model, but retaining the same kind of analytical treatment to determine the compressive strength of long fibre composite materials. The main assumption in his theory was that fibres are not straight but have initial curvature, which was represented by an infinite sinusoidal series. In his work, he suggested a theoretical model which described four compressive failure modes; a tensile failure mode causing longitudinal splitting in matrix or interface, shear failure mode in matrix or interface, fibre shear failure mode, and fibre axial compressive failure mode. His results using one value of normalised curvature agreed well with experimental measurements. Yet due to the geometrically linear formulations, other failure modes have to be imposed such as matrix shear, or interface debonding, which lack the adequate experimental support. In addition, the fibre misalignment angle range necessary to fit the data, generally 2-3(, does not agree with the experimental data.

A different approach was used by Budiansky [39] and Fleck and Budiansky [21,40], who modelled the propagation of the kink bands that are commonly observed in compression failed carbon fibre reinforced composites. They have extended the microbuckling models of Rosen [30] to include inelastic and misalignment effects, which gives:

Equation 2.4 – [40]

Where	 - initial fibre misalignment

- matrix yield stress in shear

This is actually very close to Rosen’s predictions given in Equation 2.3. If perfect plasticity and fibre misalignments are induced, the authors [21,39,40] obtained:

Equation 2.5 – [40]

Where k is approximately the composite shear yield stress (the stress at which the material begins to deform plastically) and  is the initial fibre misalignment angle. Similar mathematical models have been developed by other authors [41-43], and again the misalignment angles are predicted in the 2-3( range, which is unrealistic.

Camponeshi [44] and Schultheisz and Waas [45,46] have presented exhaustive reviews of the compressive behaviour of composites. They feel the main flaw is the geometrically linear nature of the formulation. In recent years, numerous models for the prediction of compressive behaviour of unidirectional composites have been developed.

2.7.2	Finite Element Analysis Approaches

The calculation of the lamina longitudinal compression strength remains an unsolved problem. Non-valid failure modes are commonly observed in compression tests of unidirectional specimen. Micromechanical modelling has also proven to be a difficult task. It is believed that failure is initiated by fibre microbuckling, and that non-linear matrix behaviour and fibre misalignments play a major role. The main obstacles are the non-linear nature of the composite and the scarcity of valid test data.

To date most analyses of localisation of failure in solids, including plastic microbuckling, are one-dimensional calculations based on the response of an infinite band as outlined by Rice [47]. For example, Hutchinson and Tvergaard [48] have performed infinite shear band analysis to estimate the plane strain ductility of metallic alloys. They found that the ductility is sensitive to the magnitude of imperfections (in the form of a lower yield strength within the infinite band) and that elastic and plastic bifurcation calculations grossly overestimate the strain to failure (and associated strength). Budiansky [39] and Budiansky and Fleck [21] came to the same conclusions for plastic microbuckling of fibre composites, in that imperfections are needed in the analysis in order to predict realistic compressive strengths. There are a number of sources of imperfection, including fibre waviness, and voids and cracks within the matrix.

The infinite band analyses described above suffer from two main limitations:

- They are unable to predict the width of the kink band, as the constitutive law contains no length scale

- They assume that the initial imperfection exists as an infinite band rather than as a finite region.

Fleck et al. [49] overcame the first limitation by performing an infinite band analysis using a constitutive law, which involved the fibre diameter as the pertinent length scale. They assumed that the fibres posses a finite bending resistance (which depends on the fibre diameter) and used couple stress theory to predict the broadening of the kink band from an initial infinite band of fibre misalignment. The final width of the kink band was set by fibre fracture: it was assumed that the fibres break when the maximum tensile bending strain in the fibres equals the tensile failure strain of the fibres.

Fleck et al. [49] predicted that the final width of the kink band was 10-20 fibre diameters, and that the width is relatively sensitive to both the constitutive properties of the composite, and the initial width and magnitude of fibre misalignment. In contrast, the compressive strength was found to be sensitive to the fibre misalignment angle and moderately sensitive to the width of the initial band of misaligned fibres.

Kyriakides et al. [50] used finite element analysis to study the early stages of microbuckling. They treated the fibres and matrix as discrete but perfectly bonded layers. This approach is useful when the initial region of fibre waviness extends over only a small number of fibres, but becomes prohibitively expensive in computer time when a large number of fibres are considered. However, Morais [37] developed 2D and 3D Finite Element (FE) models to predict lamina longitudinal compression strength (LLCS) of carbon composites. The models were simple and computationally inexpensive. Failure is assumed to be governed by fibre micro-instability. The results correlated well with known mathematical models, specifically Rosen [30]. His work however, highlighted that reliable strength data is essential to validate the models, and at this present time the compressive strength data are still a very controversial issue with many factors influencing the final results.

2.8	Summary

The optimum testing thickness based on previous literature is 2mm.

The investigations discussed above indicate that the compressive failure mode in carbon-epoxy composites is matrix dominated. The intrinsic compressive strength of the fibres is not fully utilised and failure of the composite laminate occurs by fibre microbuckling. Microbuckling is sensitive of fibre-matrix bond, material defects and initial fibre curvature. This is turn depends on the accuracy that has been applied to the manufacture of the compressive test specimens.

Analytical models and FEA models have similar underlying problems, this is because of the assumptions that are made initially. These present problems throughout the calculations, which tends to lead to over or underestimations when trying to predict the compressive strength of a carbon fibre reinforced composite. However, with the FEA models and the computational ability the model uses iterations to finally tune the outcome for more specific results.

# Text boxes

In Plane Shear

Complex

Through Thickness Shear

Splitting

Delamination