# Appendix 5.5 – 4-Ply laminate Data Batches 4 and 5

Batch 4

| Sample No. | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Maximum Force (N) | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1171.12 | 1.94 | 12.53 | 0.98 | 28467.84 | Through thickness shear then in plane on one half of the laminate |
| 2 | 1184.69 | 1.95 | 12.51 | 0.94 | 28899.90 | Ductile cup/cone failure |
| 3 | 1161.71 | 1.96 | 12.54 | 0.92 | 28552.94 | Through thickness for half then brittle failure |
| 4 | 1056.03 | 1.93 | 12.55 | 0.79 | 25578.72 | Through thickness shear with some splitting then brittle failure |
| 5 | 1129.37 | 1.92 | 12.56 | 0.85 | 27234.95 | Through thickness shear, in plane and some splitting and delamination |
| 6 | 1200.36 | 1.91 | 12.55 | 0.94 | 28773.34 | Through thickness shear then finally failed in brittle failure |
| 7 | 1195.10 | 1.89 | 12.5 | 0.92 | 28234.35 | BS- Complex |
| 8 | 1122.47 | 1.83 | 12.53 | 0.82 | 25738.02 | Through thickness shear then in plane and the top ply has delaminated in final failure |
| 9 | 1285.44 | 1.77 | 12.56 | 0.98 | 28576.95 | Through thickness shear 1/3 of the way then brittle failure via in plane shear |
| 10 | 1094.98 | 1.74 | 12.54 | 0.79 | 23891.95 | Split failure by through thickness shear on the upper half and lower half in opposite directions |

| Sample No. N=10 | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Young’s Modulus (GPa) | Maximum Force (N) |
| --- | --- | --- | --- | --- | --- | --- |
| Mean | 1160.13 | 1.884 | 12.54 | 0.89 | 138.06 | 27394.90 |
| Standard Deviation | 63.87 | 0.077 | 0.020 | 0.07 | 5.08 | 1735.23 |
| Variance | 5.51 | 4.11 | 0.16 | 8.17 | 3.68 | 6.33 |

Batch 5

| Sample No. | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Maximum Force (N) | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1216.84 | 1.95 | 12.59 | 0.97 | 29873.94 | Through thickness shear splitting and brittle failure |
| 2 | 1360.99 | 1.87 | 12.54 | 1.09 | 31914.95 | Through thickness shear and brittle failure |
| 3 | 1372.95 | 1.85 | 12.54 | 1.08 | 31851.16 | Delamination |
| 4 | 894.55 | 1.9 | 12.57 | 0.67 | 21364.61 | Complex and some in plane shear |
| 5 | 1373.64 | 1.93 | 12.58 | 1.12 | 33351.13 | End failure |
| 6 | 1333.31 | 1.94 | 12.54 | 1.10 | 32436.20 | End failure |
| 7 | 920.61 | 1.9 | 12.57 | 0.71 | 21987.02 | Complex and in plane shear |
| 8 | 1384.06 | 1.87 | 12.54 | 1.10 | 32455.99 | Complex |
| 9 | 1348.21 | 1.85 | 12.51 | 1.08 | 31202.35 | Complex |
| 10 | 1329.18 | 1.83 | 12.59 | 1.11 | 30623.92 | End failure |
| 11 | 1324.20 | 1.92 | 12.59 | 1.11 | 32009.52 | End failure |

| Sample No. N=10 | Compressive Strength (MPa) | Thickness (mm) | Width (mm) | Strain (%) | Young’s Modulus (GPa) | Maximum Force (N) |
| --- | --- | --- | --- | --- | --- | --- |
| Mean | 1259.87 | 1.892 | 12.56 | 1.01 | 135.58 | 29915.53 |
| Standard Deviation | 179.98 | 0.04 | 0.0272 | 0.16 | 2.68 | 4181.86 |
| Variance | 14.29 | 2.14 | 0.22 | 16.28 | 1.97 | 13.98 |